Multifunctional Mesoporous Hollow Silica Nanorod for Optical Imaging and Drug Delivery

Yanli Wu1*, Xiaogao Guan1, Xianzhu Xu2, Ruchun Yang1, Fangfang Kong1*, Xi Chen1, Qiang Xiao1

- Jiangxi Key Laboratory of Organic Chemistry, Jiangxi Science and Technology Normal University, Nanchang, 330013, China

- College of Life Science, Jiangxi Normal University, Nanchang 330031, China

Fig.S1 UV-vis spectra of IBU and IBU-MHSNR@Gd2O3:Eu

Fig.S2 presented the FTIR spectra of the hollow silica nanorod (curve 1) and Gd2(CO3)3:Eu coated hollow silica nanorod (curve 2) . In curve 1, all absorption peaks can be ascribed to the pure silica , the absorption band near 3420 cm–1 was determined as the tensile vibration of -OH, the peak of CHx (2924, 2850 cm-1)was from CTAB, the peak at 1640 cm–1 was caused by the bending vibration of H-O-H, the two strong peaks at 1080 and 795 cm–1 were due to the asymmetric and symmetric stretching of Si-O-Si, respectively, while the peak at 960 cm–1 corresponded to the symmetric stretch of Si-OH. In curve 2, except the mentioned above peaks, two absorption bands at 1506 cm-1, 1408 cm-1 appeared, which were ascribed to the bands of Vas O-C-O, this indicate the presence of the carbonate group.

Fig.S2  infrared spectrum of HSNR@Gd2(CO3)3