| Table 2. Synthesis of diverse aldehydes using Mn nano catalyst a |  |  |  |  |
| --- | --- | --- | --- | --- |
| Entry | Alcohol | Product b | Time (h) | Yield (%) |
| 1 |  |  | 1.6 | 96 |
| 2 |  |  | 1.6 | 90 |
| 3 |  |  | 1.2 | 88 |
| 4 |  |  | 1 | 95 |
| 5 |  |  | 1.6 | 98 |
| 6 |  |  | 1.4 | 85 |
| 7 |  |  | 2 | 60 |
| 8 |  |  | 3.5 | 73 |
| 9 |  |  | 3.5 | 82 |
| 10 |  |  | 4 | 67 |
| 11 |  |  | 1 | 95 |
| a The reactions were run with substrate (1 mmol), TBHP (2 mmol) and catalyst (2 mg) at 50 °C . b The products were identified by NMR spectra. |  |  |  |  |

| Table 3. Synthesis of diverse carbonyl compound using Mn nano catalyst a |  |  |  |  |
| --- | --- | --- | --- | --- |
| Entry | Alcohol | Product b | Time (h) | Yield (%) |
| 1 |  |  | 2 | 98 |
| 2 |  |  | 2.3 | 90 |
| 3 |  |  | 3 | 80 |
| 4 |  |  | 2.6 | 92 |
| 5 |  |  | 2.5 | 95 |
| 6 |  |  | 2.7 | 85 |
| a The reactions were run with substrate (1 mmol), TBHP (2 mmol) and Mn nano catalyst (2 mg) at 50 °C . b The products were identified by GC analysis and. The selectivity of products were>99% based on GC analysis. |  |  |  |  |

| Table 4. Synthesis of diverse sulfoxides using Mn nano catalyst a |  |  |  |  |
| --- | --- | --- | --- | --- |
| Entry | Sulfide | Product b | Time (h) | Yield (%) |
| 1 |  |  | 1 | 100 |
| 2 |  |  | 1.2 | 90 |
| 3 |  |  | 2 | 70 |
| 4 |  |  | 2 | 85 |
| 5 |  |  | 2.5 | 80 |
| a The reactions were run with substrate (1 mmol), TBHP (2 mmol) and catalyst (2 mg) at room temperature. b The products were identified by GC analysis and TLC. The selectivity of products were >99% based on GC analysis. |  |  |  |  |