The enhancing oxidation performance through a magnetic supported manganese system in low temperature

Content											Page

1HNMR of 2a											1

1HNMR of 2b											2

1HNMR of 2c											2

1HNMR of 2d											3

1HNMR of 2e											3

1HNMR of 2f											4

1HNMR of 2g											4

1HNMR of 2h											5

1HNMR of 2i											5

1 HNMR of 2j											6

1HNMR of 2k											6

1HNMR of (2a)

1HNMR of (2b)

1HNMR of (2c)

1HNMR of (2d)

1HNMR of (2e)

1HNMR of (2f)

1HNMR of (2g)

1HNMR of (2h)

1HNMR of (2i)

1HNMR of (2j)

1HNMR of (2k)

Table S1. Optimization conditions in oxidation of thioanisole

| Entry | Solvent | TBHP (mmol) | Catalyst (mg) | Time (min) | Yield (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | S.F | 2 | - | 80 | 30 |
| 2 | S.F | 2 | 10 | 90 | 95 |
| 3 | S.F | 2 | 20 | 60 | 100 |
| 4 | S.F | 2 | 30 | 60 | 100 |
| 5 | MeCN | 2 | 20 | 80 | 30 |
| 6 | H2O | 2 | 20 | 60 | 20 |
| 7 | EtOAc | 2 | 20 | 100 | 50 |
| 8 | EtOH | 2 | 20 | 100 | 60 |
| 9 | S.F | - | 20 | 60 | 10 |