Table 3 Wear morphology of rake and flank face of three milling inserts after cutting 100 times

| Milling insert | Morphology of flank wear | Morphology of rake face wear |
| --- | --- | --- |
| PcBN | Abrasive wear | Abrasive wear |
| C-PcBN | Abrasive wear | Abrasive wear |
| C-YG | Coating wear Coating peeling | Chipping |