Band structure and density of states

The electronic band structures of boron nitride and sulphur nanoparticle are shown in Fig 1(a) and Fig 1(b) and density states in Fig 2(a) and Fig 2(b). The BN nanosheets exhibited semiconducting properties with a calculated bandgap of 6.1 eV. The total and PDOS show that the top of the valence band consists of nitrogen atoms, whereas the conduction band is mainly composed of boron atoms, as shown in Figs. 2 (a) and 2 (b).

Fig 1(a) Electronic band structures of BN                          Fig 1(b) Electronic band structures of Sulphur

Fig 2(a) Density states for nano boron nitride             Fig 2(b) Density states for nano Sulphur

Atomic Force Microscope (AFM)

AFM images of green-synthesized nano boron nitride and nano sulphur particles are shown in Fig 3(a) and 3(b). The AFM height of a single layer was reported to increase to 2 nm.  Thus, the height profile measurements clearly suggested that these three h-BNNs consisted of a few layers (< 5 nm). The single-layer nano sheets are shown in Fig 3(a).

Fig 3(a)AFM images of green synthesised nano boron nitride particle

Fig 3(b)AFM images of green synthesised suplhur nanoparticle

AFM results confirm the successful exfoliation with the dominance of a single layer to a few layers of nano sheets. AFM images of the green-synthesized nanosulphur showed that small particles were closely anchored throughout the lm surface. The height curve along the line in the phase diagram shows the size distribution of the sulphur nanoparticles in the range of 10–60 nm, as shown in Fig 12 (b).

Experiment I- Impact of nanoparticles on sunflower shoot growth and root characteristics

Germination per cent, Mean days of germination (days), CVG and MDG (Table 1)

The treatments had a considerable impact on seed germination. Germination was higher with 2000 ppm nBN (GsP) (96.8%), 750 ppm nS (GsP) (96.2%), 1000 ppm nBN (GsP) (95.9%), 500 ppm nS (GsP) (94.8%), 750 ppm nS (CP) (94.6%), and 2000 ppm nBN (CP) (93.7%). The control treatment had a much greater mean day of germination (4.86 days) than the other treatments did. The lowest mean number of days of germination (2.56 days) was obtained in the 1000 ppm concentration of nBN (GsP). Among the various concentrations of nBN (CP), the 2000 ppm concentration had the lowest mean number of days of germination (3.01 days). Lower mean days of germination (2.72 days) were recorded in the 750 ppm treatment among different concentrations of nS (GsP), and the same concentration (750 ppm) also resulted in lower mean days of germination (2.98 days) among different concentrations of nS (CP). These findings demonstrated that there was considerable variation in the co-efficient of germination velocity. The greater the CVG value, the faster the germination. Compared to the control, 2000 ppm nBN (GsP) had significantly higher CVG (28.9), and the same concentration (2000 ppm) had significantly higher CVG (26.6) across various concentrations of nBN (CP) (13.7). A higher CVG (28.0) was recorded at 750 ppm among different concentrations of nS (GsP), and the same concentration (750 ppm) also recorded a higher CVG (25.6) among different concentrations of nS. (CP). In the case of MDG, 2000 ppm nBN (GsP) recorded a substantially higher MDG (20.2), and the same concentration (2000 ppm) also recorded a higher MDG (17.9) across different concentrations of nBN (CP), compared to the control (12.2). A higher MDG (19.7) was observed at 750 ppm among the different concentrations of nS (GsP), and the same concentration (750 ppm) also recorded a higher MDG (16.5) across different concentrations of nS (CP).

Table 1: Germination parameters of sunflower as influenced by different forms and levels

of nBN and nS

| Sl. No. | Treatments | Mean days of germination | Coefficient of velocity of germination (CVG) | Mean daily germination (MDG) | Germination ( %) |
| --- | --- | --- | --- | --- | --- |
| 01 | 250 ppm nBN (CP) | 3.78 | 14.1 | 12.3 | 78.6 |
| 02 | 500 ppm nBN (CP) | 3.69 | 16.8 | 13.8 | 82.2 |
| 03 | 750 ppm nBN (CP) | 3.62 | 22.2 | 15.8 | 86.4 |
| 04 | 1000 ppm nBN (CP) | 3.58 | 24.2 | 16.7 | 90.0 |
| 05 | 2000 ppm nBN (CP) | 3.01 | 26.6 | 17.9 | 93.7 |
| 06 | 3000 ppm nBN (CP) | 3.55 | 22.6 | 16.3 | 76.6 |
| 07 | 250 ppm nBN (GsP) | 3.51 | 15.4 | 12.8 | 87.2 |
| 08 | 500 ppm nBN (GsP) | 3.45 | 20.9 | 15.5 | 88.9 |
| 09 | 750 ppm nBN (GsP) | 2.68 | 22.5 | 15.9 | 89.0 |
| 10 | 1000 ppm nBN (GsP) | 2.56 | 26.7 | 18.0 | 95.9 |
| 11 | 2000 ppm nBN (GsP) | 2.88 | 28.9 | 20.2 | 96.8 |
| 12 | 3000 ppm nBN (GsP) | 3.01 | 23.1 | 16.7 | 88.6 |
| 13 | 250 ppm nS (CP) | 3.68 | 16.1 | 12.9 | 79.8 |
| 14 | 500 ppm nS (CP) | 3.25 | 19.4 | 15.5 | 88.7 |
| 15 | 750 ppm nS (CP) | 2.98 | 25.6 | 16.5 | 94.6 |
| 16 | 1000 ppm nS (CP) | 3.24 | 24.7 | 17.4 | 86.2 |
| 17 | 2000 ppm nS (CP) | 3.65 | 18.6 | 13.7 | 84.8 |
| 18 | 3000 ppm nS (CP) | 3.36 | 15.7 | 12.7 | 80.2 |
| 19 | 250 ppm nS (GsP) | 3.28 | 19.4 | 13.7 | 88.7 |
| 20 | 500 ppm nS (GsP) | 3.08 | 22.7 | 15.9 | 94.8 |
| 21 | 750 ppm nS (GsP) | 2.72 | 28.0 | 19.7 | 96.2 |
| 22 | 1000 ppm nS (GsP) | 2.89 | 21.3 | 15.7 | 89.0 |
| 23 | 2000 ppm nS (GsP) | 3.24 | 18.9 | 14.5 | 80.6 |
| 24 | 3000 ppm nS (GsP) | 3.67 | 16.3 | 13.5 | 76.8 |
| 25 | Control | 4.86 | 13.7 | 12.2 | 75.5 |
|  | SEm± | 0.18 | 0.21 | 0.11 | 1.24 |
|  | CD (P=0.01) | 0.58 | 0.68 | 0.36 | 3.98 |
|  | CV (%) | 3.26 | 3.98 | 4.12 | 5.86 |

4.1.2 Root and shoot length (cm) (Table 2)

In terms of root length, 2000 ppm nBN (GsP) (9.88 cm) was substantially longer than 750 ppm nS (GsP) (9.85 cm), 1000 ppm nBN (GsP) (9.38 cm), 2000 ppm nBN (CP) (9.28 cm), 750 ppm nS (CP) (8.86 cm), or 1000 ppm nS (CP) (8.79 cm) (3.56 cm). The maximum root length was measured 10 DAS with 2000 ppm nBN (GsP) (15.89 cm), which was comparable to 750 ppm nS (GsP) (15.01 cm), 1000 ppm nBN (GsP) (14.57 cm), 750 ppm nS (CP) (14.51 cm), and 2000 ppm nBN (CP) (14.21 cm) (8.44 cm). Similarly, the maximum shoot length was measured at 750 ppm nS (GsP) (12.01 cm), which was comparable to that of 2000 ppm nBN (GsP) (11.99 cm) and 1000 ppm nBN (GsP) (11.68 cm) (5.78 cm). At 10 DAS, 750 ppm nS (GsP) (17.81 cm) was substantially greater than 2000 ppm nBN (CP) (17.21 cm), 2000 ppm nBN (GsP) (16.99 cm), and 1000 ppm nBN (GsP) (16.89 cm) compared to the control (10.01 cm).

4.1.3 Seedling vigour index- I (SVI-I) and Seedling vigour index- II (SVI-II)

Seed treatment with various concentrations of green synthesized and commercial products of nBN and nS at various levels had a substantial effect on SVI-I and SVI-II (Table 3). SVI-I was significantly greater in 2000 ppm nBN (GsP) (2117) than in 750 ppm nS (GsP) (2103) or 1000 ppm nBN (GsP) (2103). (2019). SVI-I levels were greater in 2000 ppm nBN (GsP) because of the longer root and shoot lengths. Similarly, seed treatment with varying quantities of green synthesized and commercial products of nBN and nS had a substantial effect on SVI-II. Significantly higher SVI-II was recorded in 2000 ppm nBN (GsP) (2987), which was on par with 750 ppm of nS (GsP) (2898). Higher SVI-II was recorded in 2000 ppm nBN (GsP) owing to faster growth and higher dry matter accumulation.

Table 3:  Seedling vigour index of sunflower as influenced by different forms and levels of nBN and nS

| Sl No. | Treatments | 5 days after sowing |  |  | 10 days after sowing |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Root length (cm) | Shoot length (cm) | SVI-I | Root length (cm) | Shoot length (cm) | SVI-II |
| 01 | 250 ppm nBN (CP) | 3.69 | 5.49 | 722 | 8.71 | 10.23 | 1356 |
| 02 | 500 ppm nBN (CP) | 5.23 | 7.23 | 1024 | 9.89 | 11.69 | 1574 |
| 03 | 750 ppm nBN (CP) | 7.24 | 9.24 | 1424 | 12.12 | 14.89 | 2112 |
| 04 | 1000 ppm nBN (CP) | 8.11 | 9.89 | 1619 | 13.23 | 15.74 | 2235 |
| 05 | 2000 ppm nBN (CP) | 9.28 | 11.24 | 1922 | 14.21 | 17.21 | 2654 |
| 06 | 3000 ppm nBN (CP) | 7.69 | 9.87 | 1345 | 12.88 | 14.56 | 1980 |
| 07 | 250 ppm nBN (GsP) | 4.18 | 6.41 | 924 | 8.89 | 11.35 | 1745 |
| 08 | 500 ppm nBN (GsP) | 6.89 | 9.1 | 1421 | 11.87 | 13.87 | 2125 |
| 09 | 750 ppm nBN (GsP) | 7.26 | 9.43 | 1486 | 12.56 | 14.77 | 2368 |
| 10 | 1000 ppm nBN (GsP) | 9.38 | 11.68 | 2019 | 14.57 | 16.89 | 2844 |
| 11 | 2000 ppm nBN (GsP) | 9.88 | 11.99 | 2117 | 15.89 | 16.99 | 2987 |
| 12 | 3000 ppm nBN (GsP) | 8.09 | 10.01 | 1604 | 12.89 | 15.01 | 2354 |
| 13 | 250 ppm nS (CP) | 4.26 | 6.189 | 834 | 9.88 | 11.05 | 1589 |
| 14 | 500 ppm nS (CP) | 6.92 | 8.89 | 1403 | 10.99 | 13.21 | 1981 |
| 15 | 750 ppm nS (CP) | 8.86 | 10.87 | 1867 | 14.51 | 15.89 | 2331 |
| 16 | 1000 ppm nS (CP) | 8.79 | 10.81 | 1689 | 13.98 | 15.56 | 2001 |
| 17 | 2000 ppm nS (CP) | 5.12 | 7.12 | 1037 | 10.16 | 13.24 | 1755 |
| 18 | 3000 ppm nS (CP) | 4.12 | 6.19 | 827 | 9.23 | 11.25 | 1688 |
| 19 | 250 ppm nS (GsP) | 5.12 | 7.35 | 1105 | 10.54 | 13.66 | 1985 |
| 20 | 500 ppm nS (GsP) | 7.25 | 9.78 | 1614 | 12.65 | 14.87 | 2574 |
| 21 | 750 ppm nS (GsP) | 9.85 | 12.01 | 2103 | 15.01 | 17.81 | 2898 |
| 22 | 1000 ppm nS (GsP) | 7.14 | 9.19 | 1454 | 12.24 | 13.89 | 2126 |
| 23 | 2000 ppm nS (GsP) | 5.89 | 8.09 | 1127 | 10.81 | 12.88 | 1756 |
| 24 | 3000 ppm nS (GsP) | 4.89 | 7.24 | 932 | 9.81 | 11.24 | 1559 |
| 25 | Control | 3.56 | 5.78 | 705 | 8.44 | 10.01 | 1299 |
|  | SEm± | 0.38 | 0.21 | 35.7 | 0.58 | 0.64 | 41.8 |
|  | CD (P=0.01) | 1.21 | 0.68 | 110.8 | 1.82 | 1.92 | 129.8 |
|  | CV (%) | 4.39 | 3.89 | 4.67 | 4.16 | 4.88 | 5.12 |

4.1.4 Root parameters

The findings revealed a considerable variation in root characteristics (Table 4) as impacted by varied doses of green-synthesized and commercial nBN and nS seed priming. Seed treatment with 2000 ppm nBN (GsP) yielded a better average root diameter (1.21 mm), root volume (1.67 cm3), root length volume (106354 cm m3), surface area (69.61 cm2), and forks (4735), compared to 750 ppm nS. (GsP). The seeds treated with 750 ppm nS (GsP) had an average diameter of 1.02 mm, a root volume of 1.47 cm3, a root length volume of 106211 cm m3, a surface area of 69.04 cm2, and forks (4498). Higher average root diameter (0.61 mm), root volume (1.06 cm3), root length volume (97269 cm m3), surface area (67.24 cm2), and forks (4234) were found at 2000 ppm. At 750 ppm, increased average root diameter (0.89 mm), root volume (1.34 cm3), root length volume (85431 cm m3), surface area (67.54 cm2), and forks (4323) were reported.

Table 4 Root parameters of sunflower as influenced by different forms and levels of nBN and nS at 5 DAS

| Sl No. | Treatments | Average diameter (mm) | Root volume (cm3) | Root length volume1 (cm m-3) | Surface area (cm2) | Forks |
| --- | --- | --- | --- | --- | --- | --- |
| 01 | 250 ppm nBN (CP) | 0.29 | 0.72 | 49697 | 61.74 | 2595 |
| 02 | 500 ppm nBN (CP) | 0.35 | 0.77 | 57687 | 62.92 | 2947 |
| 03 | 750 ppm nBN (CP) | 0.40 | 0.83 | 77404 | 65.15 | 3611 |
| 04 | 1000 ppm nBN (CP) | 0.47 | 0.91 | 81912 | 66.26 | 3942 |
| 05 | 2000 ppm nBN (CP) | 0.61 | 1.06 | 97269 | 67.24 | 4234 |
| 06 | 3000 ppm nBN (CP) | 0.39 | 0.78 | 72567 | 65.91 | 3838 |
| 07 | 250 ppm nBN (GsP) | 0.54 | 0.94 | 63954 | 61.92 | 2649 |
| 08 | 500 ppm nBN (GsP) | 0.71 | 1.18 | 77881 | 64.90 | 3537 |
| 09 | 750 ppm nBN (GsP) | 0.88 | 1.31 | 86787 | 65.59 | 3742 |
| 10 | 1000 ppm nBN (GsP) | 0.97 | 1.41 | 104232 | 67.60 | 4341 |
| 11 | 2000 ppm nBN (GsP) | 1.21 | 1.67 | 106354 | 69.61 | 4735 |
| 12 | 3000 ppm nBN (GsP) | 0.53 | 0.94 | 86274 | 65.92 | 3841 |
| 13 | 250 ppm nS (CP) | 0.51 | 0.94 | 58236 | 62.91 | 2944 |
| 14 | 500 ppm nS (CP) | 0.69 | 1.12 | 72603 | 64.02 | 3275 |
| 15 | 750 ppm nS (CP) | 0.89 | 1.34 | 85431 | 67.54 | 4323 |
| 16 | 1000 ppm nS (CP) | 0.71 | 1.18 | 73336 | 67.01 | 4166 |
| 17 | 2000 ppm nS (CP) | 0.61 | 1.02 | 64320 | 63.19 | 3027 |
| 18 | 3000 ppm nS (CP) | 0.44 | 0.85 | 61865 | 62.26 | 2750 |
| 19 | 250 ppm nS (GsP) | 0.71 | 1.12 | 72750 | 63.57 | 3140 |
| 20 | 500 ppm nS (GsP) | 0.89 | 1.35 | 94337 | 65.68 | 3769 |
| 21 | 750 ppm nS (GsP) | 1.02 | 1.47 | 106211 | 69.04 | 4498 |
| 22 | 1000 ppm nS (GsP) | 0.94 | 1.29 | 77917 | 65.27 | 3647 |
| 23 | 2000 ppm nS (GsP) | 0.74 | 1.15 | 64357 | 63.84 | 3221 |
| 24 | 3000 ppm nS (GsP) | 0.65 | 0.98 | 57137 | 62.84 | 2923 |
| 25 | Control | 0.21 | 0.65 | 47608 | 61.47 | 2515 |
|  | SEm± | 0.04 | 0.06 | 61.26 | 0.41 | 78.23 |
|  | CD (P=0.01) | 0.19 | 0.21 | 210.34 | 1.34 | 256.6 |
|  | CV (%) | 4.12 | 3.91 | 4.36 | 3.33 | 4.87 |
|  | F-test | ** | ** | ** | ** | ** |

Experiment II- Impact of nanoparticles on sunflower shoot growth and root characteristics.

Table 5: Germination parameters of sunflower as influenced by different forms and levels of nBN and nS

| Sl No. | Treatments | Mean days of germination | Co- efficient of velocity of germination (CVG) | Mean daily germination (MDG) | Germination ( %) |
| --- | --- | --- | --- | --- | --- |
| 01 | 1000 ppm nBN (CP) | 3.61 | 24.1 | 16.8 | 90.4 |
| 02 | 1250 ppm nBN (CP) | 3.49 | 24.7 | 17.1 | 91.9 |
| 03 | 1500 ppm nBN (CP) | 3.32 | 25.2 | 17.6 | 92.6 |
| 04 | 1750 ppm nBN (CP) | 3.18 | 26.2 | 17.9 | 92.9 |
| 05 | 2000 ppm nBN (CP) | 2.98 | 27.1 | 18.1 | 93.8 |
| 06 | 2250 ppm nBN (CP) | 3.11 | 26.8 | 17.7 | 89.8 |
| 07 | 1000 ppm nBN (GsP) | 2.56 | 26.1 | 18.4 | 95.2 |
| 08 | 1250 ppm nBN (GsP) | 2.44 | 27.6 | 18.9 | 95.9 |
| 09 | 1500 ppm nBN (GsP) | 2.19 | 32.9 | 22.2 | 98.2 |
| 10 | 1750 ppm nBN (GsP) | 2.66 | 30.3 | 21.2 | 96.2 |
| 11 | 2000 ppm nBN (GsP) | 2.88 | 29.2 | 20.5 | 96.0 |
| 12 | 2250 ppm nBN (GsP) | 3.12 | 28.7 | 20.1 | 90.1 |
| 13 | 550 ppm nS (CP) | 3.25 | 19.1 | 15.6 | 89.6 |
| 14 | 600 ppm nS (CP) | 3.18 | 22.6 | 15.9 | 90.2 |
| 15 | 650 ppm nS (CP) | 3.12 | 24.8 | 16.2 | 91.8 |
| 16 | 700 ppm nS (CP) | 3.08 | 25.1 | 16.5 | 93.1 |
| 17 | 750 ppm nS (CP) | 2.98 | 26.1 | 16.9 | 94.8 |
| 18 | 800 ppm nS (CP) | 3.19 | 25.4 | 16.3 | 88.4 |
| 19 | 550 ppm nS (GsP) | 3.08 | 22.1 | 17.1 | 94.9 |
| 20 | 600 ppm nS (GsP) | 2.44 | 32.4 | 21.9 | 97.8 |
| 21 | 650 ppm nS (GsP) | 2.52 | 31.0 | 21.1 | 97.0 |
| 22 | 700 ppm nS (GsP) | 2.68 | 29.6 | 20.6 | 96.5 |
| 23 | 750 ppm nS (GsP) | 2.72 | 28.2 | 19.9 | 96.0 |
| 24 | 800 ppm nS (GsP) | 3.12 | 27.6 | 19.1 | 90.4 |
| 25 | Control | 4.98 | 13.9 | 12.4 | 74.6 |
|  | SEm± | 0.15 | 0.19 | 0.14 | 0.32 |
|  | CD (P=0.01) | 0.49 | 0.61 | 0.45 | 1.01 |
|  | CV (%) | 3.76 | 3.84 | 4.12 | 5.92 |
|  | F-test | ** | ** | ** | ** |

Table 6: Seedling vigour index of sunflower as influenced by different forms and levels of nBN and nS

| Sl No. | Treatments | 5 Days after sowing |  |  | 10 Days after sowing |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Root length (cm) | Shoot length (cm) | SVI-I | Root length (cm) | Shoot length (cm) | SVI-II |
| 01 | 1000 ppm nBN (CP) | 8.10 | 9.81 | 1619 | 12.01 | 15.08 | 2619 |
| 02 | 1250 ppm nBN (CP) | 8.28 | 9.98 | 1678 | 13.52 | 15.28 | 2820 |
| 03 | 1500 ppm nBN (CP) | 8.69 | 10.56 | 1783 | 14.22 | 15.86 | 2960 |
| 04 | 1750 ppm nBN (CP) | 9.01 | 10.89 | 1849 | 14.56 | 16.14 | 3027 |
| 05 | 2000 ppm nBN (CP) | 9.31 | 11.19 | 1923 | 15.49 | 16.56 | 3183 |
| 06 | 2250 ppm nBN (CP) | 7.80 | 8.89 | 1499 | 11.42 | 14.23 | 2473 |
| 07 | 1000 ppm nBN (GsP) | 9.41 | 11.71 | 2011 | 16.81 | 16.96 | 3394 |
| 08 | 1250 ppm nBN (GsP) | 9.59 | 11.88 | 2059 | 17.54 | 17.11 | 3504 |
| 09 | 1500 ppm nBN (GsP) | 10.98 | 12.99 | 2354 | 19.81 | 18.29 | 3922 |
| 10 | 1750 ppm nBN (GsP) | 9.97 | 12.01 | 2114 | 17.83 | 17.28 | 3559 |
| 11 | 2000 ppm nBN (GsP) | 9.89 | 11.65 | 2068 | 17.63 | 16.91 | 3497 |
| 12 | 2250 ppm nBN (GsP) | 9.00 | 11.02 | 1804 | 11.73 | 16.31 | 2696 |
| 13 | 550 ppm nS (CP) | 6.98 | 8.91 | 1424 | 11.28 | 14.66 | 2493 |
| 14 | 600 ppm nS (CP) | 7.24 | 9.02 | 1467 | 11.84 | 14.98 | 2589 |
| 15 | 650 ppm nS (CP) | 7.89 | 9.25 | 1573 | 13.45 | 15.22 | 2805 |
| 16 | 700 ppm nS (CP) | 8.56 | 9.89 | 1718 | 14.72 | 15.38 | 2978 |
| 17 | 750 ppm nS (CP) | 8.89 | 10.81 | 1868 | 16.43 | 16.21 | 3273 |
| 18 | 800 ppm nS (CP) | 8.20 | 9.75 | 1587 | 10.03 | 15.02 | 2381 |
| 19 | 550 ppm nS (GsP) | 9.56 | 9.81 | 1838 | 16.55 | 15.23 | 3195 |
| 20 | 600 ppm nS (GsP) | 10.87 | 12.89 | 2324 | 19.42 | 18.24 | 3873 |
| 21 | 650 ppm nS (GsP) | 9.92 | 12.31 | 2156 | 18.62 | 17.50 | 3687 |
| 22 | 700 ppm nS (GsP) | 9.89 | 12.11 | 2123 | 18.15 | 17.31 | 3604 |
| 23 | 750 ppm nS (GsP) | 9.80 | 12.08 | 2100 | 17.62 | 17.08 | 3512 |
| 24 | 800 ppm nS (GsP) | 8.87 | 10.12 | 1717 | 12.1 | 15.66 | 2680 |
| 25 | Control | 3.49 | 5.84 | 696 | 8.21 | 9.89 | 1491 |
|  | SEm± | 0.28 | 0.18 | 36.8 | 0.22 | 0.24 | 43.9 |
|  | CD (P=0.01) | 0.91 | 0.59 | 115.2 | 0.69 | 0.75 | 135.7 |
|  | CV (%) | 4.11 | 4.39 | 5.21 | 3.87 | 4.65 | 5.12 |
|  | F- test | ** | ** | ** | ** | ** | ** |

Table 7: Root parameters of sunflower as influenced by different forms and levels of nBN and nS at 5 DAS

| Sl No. | Treatments | Average diameter (mm) | Root volume (cm3) | Root length volume1 (cm m-3) | Surface area (cm2) | Forks |
| --- | --- | --- | --- | --- | --- | --- |
| 01 | 1000 ppm nBN (CP) | 0.45 | 0.89 | 81872 | 66.21 | 3938 |
| 02 | 1250 ppm nBN (CP) | 0.48 | 0.93 | 83569 | 66.38 | 3998 |
| 03 | 1500 ppm nBN (CP) | 0.52 | 0.97 | 87425 | 66.57 | 4087 |
| 04 | 1750 ppm nBN (CP) | 0.58 | 1.01 | 95236 | 66.78 | 4100 |
| 05 | 2000 ppm nBN (CP) | 0.63 | 1.04 | 97246 | 67.89 | 4244 |
| 06 | 2250 ppm nBN (CP) | 0.55 | 0.99 | 93654 | 66.61 | 4125 |
| 07 | 1000 ppm nBN (GsP) | 0.95 | 1.42 | 104323 | 67.49 | 4341 |
| 08 | 1250 ppm nBN (GsP) | 1.02 | 1.49 | 107256 | 67.98 | 4562 |
| 09 | 1500 ppm nBN (GsP) | 1.35 | 1.81 | 109989 | 70.89 | 4887 |
| 10 | 1750 ppm nBN (GsP) | 1.28 | 1.72 | 108569 | 70.12 | 4802 |
| 11 | 2000 ppm nBN (GsP) | 1.23 | 1.70 | 106359 | 69.63 | 4738 |
| 12 | 2250 ppm nBN (GsP) | 1.18 | 1.51 | 105231 | 69.14 | 4711 |
| 13 | 550 ppm nS (CP) | 0.71 | 1.18 | 72689 | 64.12 | 3279 |
| 14 | 600 ppm nS (CP) | 0.75 | 1.21 | 74568 | 64.89 | 3645 |
| 15 | 650 ppm nS (CP) | 0.81 | 1.27 | 78542 | 65.74 | 3987 |
| 16 | 700 ppm nS (CP) | 0.86 | 1.31 | 82236 | 66.91 | 4122 |
| 17 | 750 ppm nS (CP) | 0.91 | 1.35 | 85431 | 67.89 | 4333 |
| 18 | 800 ppm nS (CP) | 0.83 | 1.29 | 80241 | 66.54 | 4215 |
| 19 | 550 ppm nS (GsP) | 0.92 | 1.36 | 94337 | 67.98 | 3789 |
| 20 | 600 ppm nS (GsP) | 1.32 | 1.76 | 109796 | 70.86 | 4865 |
| 21 | 650 ppm nS (GsP) | 1.25 | 1.68 | 108745 | 70.18 | 4815 |
| 22 | 700 ppm nS (GsP) | 1.14 | 1.55 | 107451 | 70.12 | 4528 |
| 23 | 750 ppm nS (GsP) | 1.08 | 1.49 | 106211 | 69.05 | 4498 |
| 24 | 800 ppm nS (GsP) | 0.98 | 1.41 | 100589 | 68.23 | 4326 |
| 25 | Control | 0.23 | 0.78 | 65236 | 62.69 | 3451 |
|  | SEm± | 0.01 | 0.02 | 84.23 | 0.21 | 12.56 |
|  | CD (P=0.01) | 0.05 | 0.07 | 260.69 | 0.65 | 40.12 |
|  | CV (%) | 3.98 | 4.22 | 4.36 | 3.78 | 4.51 |
|  | F-test | ** | ** | ** | ** | ** |