Supplementary information to ZnFe2O4 Nanoparticles for Gas-Sensing Applications: Monitoring of Structural Parameters while Exposing the Ferrite in Gas Atmospheres

Zeyad M. Abdulhamid1, Aasif A. Dabbawala2, Thomas Delclos3, Rainer Straubinger4, Magnus Rueping5, Kyriaki Polychronopoulou2, Dalaver H. Anjum1,*

1Department of Physics, Khalifa University of Science and Technology, Abu Dhabi 127788, United Arab Emirates; Center for Catalysis and Separations (CeCaS Center), Khalifa University of Science and Technology, Abu Dhabi 127788, United Arab Emirates.

2Department of Mechanical Engineering, Khalifa University of Science and Technology, Abu Dhabi 127788, United Arab Emirates; Center for Catalysis and Separations (CeCaS Center), Khalifa University of Science and Technology, Abu Dhabi 127788, United Arab Emirates.

3Manager, Materials, and Surface Core Labs, Khalifa University of Science and Technology, Abu Dhabi 127788, United Arab Emirates

4Core Technology Platforms Operations, New York University, Abu Dhabi 129188, United Arab Emirates.

5KAUST Catalysis Center (KCC), King Abdullah University of Science and Technology, Thuwal 23955-6900, Saudi Arabia.

*Corresponding author email: dalaver.anjum@ku.ac.ae

Figure S1 Variation of lattice parameter with cos2θ/sinθ, and Williamson-Hall plots of (a)ZFO-1, (b) ZFO-2, (c) ZFO-3, and (d) ZFO-4, respectively.

Figure S2 TEM-EDS elemental analysis of ZnFe2O4 derived from (a) ZFO-2, (b) ZFO-3, and (c) ZFO-4.

Figure S3 XPS survey of the ZnFe2O4 derived from (a) ZFO-1, (b) ZFO-2, (c) ZFO-3, and (d) ZFO-4.

(b)

(a)

Figure S4 Unit cell of ZnFe2O4 (a) without and (b) with (001) surface termination.

(a)

(b)

Figure S5 (a) TEM images and (b)SAED of ZFO-3 during purging Argon gas for 30 minutes at 300 oC.

(a)

(b)

Figure S6 (a) TEM images and (b)SAED of ZFO-3 during purging CO2 gas for 30 minutes at 300 oC.

Table S1 TEM-EDS and EELS elemental composition of ZnFe2O4 NPs.

| Elements | Atomic Percent |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ZFO-2 |  | ZFO-3 |  | ZFO-4 |  |
|  | EDS-TEM | EELS | EDS-TEM | EELS | EDS-TEM | EELS |
| Zn | 11.13 | 11.3 | 7 | 7.1 | 4.11 | 4.8 |
| Fe | 42.20 | 46.3 | 26.27 | 29.4 | 26.07 | 35.3 |
| O | 46.67 | 42.4 | 66.72 | 64 | 69.81 | 60 |