Supplementary Information for

Extreme electron-blocking interface for garnet-based solid-state lithium-metal batteries with superior long lifespan

Chang Zhang1, Jiameng Yu1, Yinjie Lv1, Yue Zhang1, Tianyi Gao1, Yuxi He1, Xin Chen1, Yi Yu1,2 and Wei Liu1,2,3*

1School of Physical Science and Technology, ShanghaiTech University, Shanghai 201210, China

2Shanghai Key Laboratory of High-resolution Electron Microscopy, ShanghaiTech University; Shanghai, 201210, China

3Key Laboratory of Advanced Energy Materials Chemistry (Ministry of Education), Nankai University, Tianjin, 300071, China

* Corresponding author. E-mail: liuwei1@shanghaitech.edu.cn

Figure S1. Schematic illustration of KF buffer layer deposition process by vacuum thermal evaporation.

Figure S2. XRD patterns of (a) prepared LLZTO powder, LLZTO pellet and LLZTO-KF pellet.

Figure S3. (a), Cross-sectional SEM image of LLZTO-KF. (b), Corresponding EDS mappings of F elements.

Figure S4. CCD profiles of Li|KF-LLZTO-KF|Li and Li|LLZTO|Li symmetric cells of capacity-constant mode at RT.

Figure S5. CCD profiles of Li|KF-LLZTO-KF|Li and Li|LLZTO|Li symmetric cells of time-constant mode at 60 °C.

Figure S6. EIS curves of Li|KF-LLZTO-IL|NCM cells with different ionic liquids at RT.

Figure S7. EIS curves of Li|KF-LLZTO-IL|NCM cells with 2 M Li-TFSI in various ionic liquids at RT.

v

Figure S8. EIS curves of Li|KF-LLZTO-IL|NCM cells with 1 M Li-TFSI in PP13-TFSI ionic liquid at RT.

Figure S9. EIS curves of Li|KF-LLZTO-LE|NCM cells at RT. LE is liquid electrolyte, 1 M LiPF6 in EC/DMC (v/v=1:1) with 2%VC.

Figure S10. Long cycle performance of Li|KF-LLZTO-IL|NCM cells at 1C, RT.

Figure S11. Morphology and corresponding EDS mapping of LLZTO-KF pellet. (a), SEM image of LLZTO pellet with excess KF layer. (b) Corresponding EDS mappings of K, Zr and Ta elements.

Figure S12. Simulation cell geometry in COMSOL for LLZO-KF|Li interface (a) and LLZO|Li interface (b).

Table S1. Electronic conductivity comparation chart of our work with other literature reports.

| Solid state electrolyte | Modified methods | Electronic conductivity (S cm−1) | Reference |
| --- | --- | --- | --- |
| Al-doped Li7La3Zr2O12 | SPS | 6.4×10–8 | [1] |
| Li7La2.75Ca0.25Zr1.65Nb0.25Co0.1O12 | Doping | 6×10−8 | [2] |
| Li7La2.75Ca0.25Zr1.75Nb0.25O12 | Doping | 3.59×10−8 | [3] |
| Li6.2La3(Zr0.2Hf0.2Ti0.2Nb0.2Ta0.2)0.2O12 | Doping | 2.33×10–8 | [4] |
| Al-doped Li7La3Zr2O12 | Hot press | 2×10−8 | [5] |
| Li6.5La3Zr1.5Ta0.5O12 | Rapid sintering | 1.2×10−8 | [6] |
| (Li6.7La3Zr1.7Ta0.3O12 | Doping | 5.4×10−9 | [7] |
| Li6.4La3Zr1.4Ta0.6O12 | Ag-LiF | 5.0×10−9 | [8] |
| Li6.4La3Zr1.4Ta0.6O12 | AlN sinter additive | 2.6×10−9 | [9] |
| Li6.4Ga0.2La3Zr2O12 | Doping | 5×10−10 | [10] |
| Li6.4La3Zr1.4Ta0.6O12 | KF layer | 1.8×10-10 | This work |

Table S2. Critical current density (CCD), area specific resistance (ASR) and cycling life of the reported Li|LLZO|Li symmetrical cells with different interface layers at RT (25 °C) or other temperatures.

| Various LLZO solid state electrolytes | Interface layer | CCD (mA cm-2) | ASR (Ω cm2) | Cycle life (mA cm-2@h) | Year [Ref.] |
| --- | --- | --- | --- | --- | --- |
| Li5.9Al0.2La3Zr1.75W0.25O12 | Drawing graphite | N/A | 25 | 0.3@1000 | 2018[11] |
| Li6.5La3Zr1.5Ta0.5O12 | Li-C composite | 1.0 | 11 | 0.3@250 | 2019[12] |
| Li6.4La3Zr1.4Ta0.6O12 | Cu3N film | 1.2 | 83.4 | 0.1@1000 | 2020[13] |
| Li6.5La3Zr1.5Ta0.5O12 | Li-gC3N4 composite | 1.5 | 11 | 0.3@300 | 2020[14] |
| Li6.5La3Zr1.5Ta0.5O12 | liquid metal painting | 1.7 | 19.5 | 0.2@2000 (RT) | 2020[15] |
| Li6.4La3Zr1.4Ta0.6O12 | PAA | 54.5 | 1.2 | 0.2@1000 1@400 | 2021[16] |
| Li6.4La3Zr1.4Ta0.6O12 | 3D Li–Zn alloy | 2 | 1.9 | 0.1@1000 0.5@300 | 2021[17] |
| Li6.4La3Zr1.4Ta0.6O12 | LiF | 0.75 | 12.7 | 0.2@1500 0.4@300 | 2021[18] |
| Li6.75La3Zr1.75Ta0.25O12 | MgF2 | 0.65 | 25 | 0.3@1000 | 2022[19] |
| Li6.4La3Zr1.4Ta0.6O12 | LixC6 | N/A | 26.2 | 0.3@900 | 2022[20] |
| Li6.5La3Zr1.5Ta0.5O12 | Al2O3 | 1.0 | 16.8 | 0.3@1000 | 2022[21] |
| Li6.75La3Za1.75Ta0.25O12 | LiF/Li-Mxene | 1.5 | 5 | 0.3@600 | 2022[22] |
| Li6.75La3Za1.75Ta0.25O12 | Li2S/LixSn | 0.5 | 47 | 0.2@1000 | 2022[23] |
| Li6.4La3Zr1.4Ta0.6O12 | Ag-LiF | 0.75 | 5.8 | 0.2@600 0.5@130 | 2022[8] |
| Li6.4La3Zr1.4Ta0.6O12 | Li3PO4 | 0.8 (30 °C) | 13(30 °C) | 0.1@1000 (30 °C) 0.4@200 (30 °C) | 2022[24] |
| Li6.4La3Zr1.4Ta0.6O12 | AlN | 0.76 | 1 | 0.2@500 | 2022[9] |
| Li6.4La3Zr1.4Ta0.6O12 | KF | 1.0 (time mode) 1.4 (capacity mode) | 5.9 | 0.2@3000 0.5@350 | This work |

Table S3. The interface impedance values of Li|KF-LLZTO|NCM cells with various ionic liquids and liquid electrolyte.

|  | 0.3 M PY14 | 0.2 M PP13 | 0.2 M C4mim | 1 M PP13 | 1 M C4mim | 2 M PP13 | 2 M C4mim | 1 M LE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Interface impedance (Ω cm2) | 1720 | 1150 | 710 | 143 | 76 | 520 | 170 | 340 |

Table S4. Cycle performance comparation chart of our work with other literature reports.

| Cathode | Modifications | C-Rate | Cycle numbers | Retention (%) | Average coulombic efficiency (%) | Voltage range (V) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| LiFePO4 | 10 μL commercial liquid electrolyte | 1C | 900 | 85.4 | 99.98 | 2-4 | [25] |
| LiNi0.8Co0.1Mn0.1O2 |  | 0.5C | 200 | 89 | 99.95 | 3-4.3 |  |
| LiNi0.8Co0.1Mn0.1O2 | 7 μL liquid electrolyte, 1 M LiPF6 in EC/DEC | 0.2C | 50 | 87.7 | 99.74 | 2.7-4.3 | [26] |
| LiFePO4 |  | 1C | 835 | 80.6 | 99.97 | 2.5-4 |  |
| LiFePO4 | 7 μL SN+LiTFSI | 0.5C | 400 | 80.4 | 99.95 | 2.5-4 |  |
| LiNi0.8Co0.1Mn0.1O2 |  | 0.2C | 100 | 80.4 | 99.78 | 2.7-4.3 |  |
| LiNi0.83Co0.11Mn0.06O2 | N/A | 0.2C | 140 | 72.1 | 99.77 | 2.7-4.3 | [27] |
| LiNi1/3Co1/3Mn1/3O2 | ionic liquid, 2 M LiFSI in Pyr13FSI | 0.5C | 1700 | ~91 | 99.99 | 2.8-4.2 | [8] |
| LiFePO4 | 10 μL liquid electrolyte, 1 M LiFP6 in EC/DME/EMC | 0.2C | 80 | 95 | 99.94 | 2.5-4 | [28] |
| LiFePO4 | 6 μL liquid electrolyte, 1 M LiFP6 in EC/DEC | 0.1C | 100 | 90.4 | 99.90 | 2-4.2 | [23] |
| LiFePO4 | 3 μL ionic liquid, 0.3M LiTFSI in PY14TFSI | 0.1C | 500 | ~75 | 99.94 | 2.5-4 | [21] |
| LiNi0.83Co0.11Mn0.06O2 |  | 0.2C | 100 | 90.2 | 99.90 | 3-4.3 |  |
| LiNi0.83Co0.11Mn0.06O2 | liquid electrolyte | 0.2C | 100 | 75.9 | 99.72 | 3-4.3 |  |
| LiFePO4 | 3 μL liquid electrolyte, 1 M LiFP6 in EC/DME/EMC | 0.1C | 300 | 83 | 99.94 | 2.5-4.2 | [20] |
| LiFePO4 | 6 μL SN+LiTFSI | 0.3C | 100 | 75.9 | 99.72 | 2.5-4.2 | [19] |
| LiFePO4 |  | 0.1C | 100 | 98.3 | 99.98 | 2.5-4.2 |  |
| LiFePO4 | 10 μL liquid electrolyte, 1 M LiPF6 in EC/DEC | 0.5C | 100 | 94 | 99.94 | 2.5-4.2 | [22] |
| LiNi0.5Co0.3Mn0.2O2 | 15 μL liquid electrolyte | 1C | 300 | 85.5 | 99.95 | 2.8-4.3 | [29] |
| LiNi0.5Co0.3Mn0.2O2 |  | 2C | 200 | 80% | 97.61 | 2.8-4.3 |  |
| LiNi0.6Co0.2Mn0.2O2 | 10 μL liquid electrolyte, 1 M LiPF6 in EC/DMC | 0.2C | 100 | 88.43 | 99.88 | 2.8-4.5 | [30] |
| LiFePO4 | 3 μL ionic liquid, 0.2 M LiTFSI in PP13-TFSI | 0.1C (30 °C) | 150 | 81 | 99.86 | 3-4.2 | [24] |
| LiNi0.8Co0.1Mn0.1O2 | 3 μL ionic liquid, 1 M LiTFSI in C4mim-TFSI | 0.2C | 270 | 82.8 | 99.93 | 2.8-4.3 | This work |
| LiNi0.8Co0.1Mn0.1O2 |  | 1C | 1000 | 83.1 | 99.98 | 2.8-4.3 |  |
| LiNi0.8Co0.1Mn0.1O2 |  | 2C | 3000 | 72.1 | 99.99 | 2.8-4.3 |  |

Reference

[1]	Y. Zhu, J. Zhang, W. Li, Y. Zeng, W. Wang, Z. Yin, B. Hao, Q. Meng, Y. Xue, J. Yang, and S. Li, Journal of Alloys and Compounds 2023 967.

[2]	A. J. Samson;K. Hofstetter;E. Wachsman;V. Thangadurai, Journal of the Electrochemical Society 2018 165, A2303-A2311.

[3]	Y. L. Song;L. Y. Yang;W. G. Zhao;Z. J. Wang;Y. Zhao;Z. Q. Wang;Q. H. Zhao;H. Liu;F. Pan, Advanced Energy Materials 2019 9.

[4]	S. X. Han;Z. Q. Wang;Y. Ma;Y. Miao;X. M. Wang;Y. Wang;Y. Z. Wang, Journal of Advanced Ceramics 2023 12, 1201-1213.

[5]	E. Rangasamy;J. Wolfenstine;J. Sakamoto, Solid State Ionics 2012 206, 28-32.

[6]	L. Yang;Q. S. Dai;L. Liu;D. S. Shao;K. L. Luo;S. Jamil;H. Liu;Z. G. Luo;B. B. Chang;X. Y. Wang, Ceramics International 2020 46, 10917-10924.

[7]	M. Y. Yi;T. Liu;X. N. Wang;J. Y. Li;C. Wang;Y. C. Mo, Ceramics International 2019 45, 786-792.

[8]	S. Lee;K. S. Lee;S. Kim;K. Yoon;S. Han;M. H. Lee;Y. Ko;J. H. Noh;W. Kim;K. Kang, Science Advances 2022 8.

[9]	C. Zhang, X. C. Hu, Z. W. Nie, C. Wu, N. Zheng, S. J. Chen, Y. H. Yang, R. Wei, J. M. Yu, N. Yang, Y. Yu, and W. Liu, Journal of Advanced Ceramics 2022 11, 1530-1541.

[10]	M. Philipp;B. Gadermaier;P. Posch;I. Hanzu;S. Ganschow;M. Meven;D. Rettenwander;G. J. Redhammer;H. M. R. Wilkening, Advanced Materials Interfaces 2020 7.

[11]	Y. J. Shao, H. C. Wang, Z. L. Gong, D. W. Wang, B. Z. Zheng, J. P. Zhu, Y. X. Lu, Y. S. Hu, X. X. Guo, H. Li, X. J. Huang, Y. Yang, C. W. Nan, and L. Q. Chen, Acs Energy Letters 2018 3, 1212-1218.

[12]	J. Duan;W. Y. Wu;A. M. Nolan;T. R. Wang;J. Y. Wen;C. C. Hu;Y. F. Mo;W. Luo;Y. H. Huang, Advanced Materials 2019 31.

[13]	H. Y. Huo;Y. Chen;R. Y. Li;N. Zhao;J. Luo;J. G. P. da Silva;R. Mucke;P. Kaghazchi;X. X. Guo;X. L. Sun, Energy & Environmental Science 2020 13, 127-134.

[14]	Y. Huang;B. Chen;J. Duan;F. Yang;T. R. Wang;Z. F. Wang;W. J. Yang;C. C. Hu;W. Luo;Y. H. Huang, Angewandte Chemie-International Edition 2020 59, 3699-3704.

[15]	J. W. Meng;Y. Zhang;X. J. Zhou;M. Lei;C. L. Li, Nature Communications 2020 11.

[16]	H. Y. Huo, J. Gao, N. Zhao, D. X. Zhang, N. G. Holmes, X. N. Li, Y. P. Sun, J. M. Fu, R. Y. Li, X. X. Guo, and X. L. Sun, Nature Communications 2021 12.

[17]	Z. P. Wan;K. Shi;Y. F. Huang;L. Yang;Q. B. Yun;L. K. Chen;F. Z. Ren;F. Y. Kang;Y. B. He, Journal of Power Sources 2021 505.

[18]	S. J. Tang;G. W. Chen;F. C. Ren;H. C. Wang;W. Yang;C. X. Zheng;Z. L. Gong;Y. Yang, Journal of Materials Chemistry A 2021 9, 3576-3583.

[19]	J. L. Jiang;Y. H. Ou;S. Y. Lu;C. Shen;B. B. Li;X. Y. Liu;Y. Jiang;B. Zhao;J. J. Zhang, Energy Storage Materials 2022 50, 810-818.

[20]	C. Cui;Q. Ye;C. Zeng;S. H. Wang;X. W. Xu;T. Y. Zhai;H. Q. Li, Energy Storage Materials 2022 45, 814-820.

[21]	S. J. Guo, Y. T. Li, B. Li, N. S. Grundish, A. M. Cao, Y. G. Sun, Y. S. Xu, Y. L. M. Ji, Y. Qiao, Q. H. Zhang, F. Q. Meng, Z. H. Zhao, D. Wang, X. Zhang, L. Gu, X. Q. Yu, and L. J. Wan, Journal of the American Chemical Society 2022 144, 2179-2188.

[22]	J. Y. Wen;L. Q. Huang;Y. Huang;W. Luo;H. Y. Huo;Z. F. Wang;X. Y. Zheng;Z. Y. Wen;Y. H. Huang, Energy Storage Materials 2022 45, 934-940.

[23]	B. Zhao;W. C. Ma;B. B. Li;X. T. Hu;S. Y. Lu;X. Y. Liu;Y. Jiang;J. J. Zhang, Nano Energy 2022 91.

[24]	Z. Bi;Q. Sun;M. Jia;M. Zuo;N. Zhao;X. Guo, Advanced Functional Materials 2022 32.

[25]	B. Chen;J. Zhang;T. Zhang;R. Wang;J. Zheng;Y. Zhai;X. Liu, Advanced Science 2023 10, 2207056.

[26]	G. J. Lu;W. Liu;Z. G. Yang;Y. M. Wang;W. K. Zheng;R. R. Deng;R. H. Wang;L. Lu;C. H. Xu, Advanced Functional Materials 2023.

[27]	W. J. Ji, B. Luo, Q. Wang, G. H. Yu, Z. H. Liu, Z. W. Zhao, R. R. Zhao, S. B. Wang, X. W. Wang, B. Zhang, J. F. Zhang, F. Hou, and J. Liang, Advanced Energy Materials 2023 13.

[28]	J. X. Zhang;C. H. Wang;M. T. Zheng;M. H. Ye;H. Y. Zhai;J. Li;G. J. Tan;X. F. Tang;X. L. Sun, Nano Energy 2022 102.

[29]	T. R. Wang, J. Duan, B. Zhang, W. Luo, X. Ji, H. H. Xu, Y. Huang, L. Q. Huang, Z. Y. Song, J. Y. Wen, C. S. Wang, Y. H. Huang, and J. B. Goodenough, Energy & Environmental Science 2022 15, 1325-1333.

[30]	C. J. Zheng;J. M. Su;Z. Song;T. P. Xiu;J. Jin;M. E. Badding;Z. Y. Wen, Materials Today Energy 2022 27.