Supplementary Information

Unusual d-electron heavy-fermion behaviour in f-electron ferromagnetic antiperovskite Gd3SnC

Joonho Bang1‡, Jongho Park1‡, Kimoon Lee2, Minsoo Kim3,4, Wonshik Kyung3,4, Jonathan D. Denlinger5, Yeongkwan Kim6,7, Young Hee Lee1,8, Changyoung Kim3,4,*, and Sung Wng Kim1,8,*

Supplementary Fig. 1 | Calculated phonon band structure and DOS for Gd3SnC. a, Phonon band along R−Γ−M−X direction. b, Partial phonon DOS.

Supplementary Fig. 2 | Tricritical behaviour of Gd3SnC antiperovskite. a–d, Modified Arrott plots for the tricritical mean-field model (βArrott = 0.25, γArrott = 1) (a), mean-field model (βArrott = 0.5, γArrott = 1) (b), 3D-Ising model (βArrott = 0.325, γArrott = 1) (c), and 3D-Heisenberg model (βArrott = 0.365, γArrott = 1.336) (d). e, H/M versus M 2 curves for various T around the TC. The inset is an enlarged view of low-M 2 region. f, T-dependent Cmag and data fitting using Cmag (T) = C0 + A±(T/TC − 1)−α±, where C0, A, and α are constant, critical amplitude, and critical exponent, respectively. ± indicates above and below the TC.

Supplementary Fig. 3 | Temperature-dependent powder XRD results of Gd3SnC. a, Low-T XRD patterns in the temperature range between 85 and 300 K. b, T-dependent lattice constant a obtained from the XRD peak position.

Supplementary Fig. 4 | Temperature-dependent magnetic contribution to the heat capacity for Gd3SnC antiperovskite. a, Determination of the TK using the equation of Cmag/T = −(0.25/TK)ln(T/(βTK)) (Ref. Seaman, C. L. et al. Evidence for non-Fermi liquid behaviour in the Kondo alloy Y1−xUxPd3. Phys. Rev. Lett. 67, 2882–2885 (1991).), where β = 2.25 is obtained from the phonon background term βT 3 (inset of Fig. 3a). b, Cmag versus T curve. Blue and red areas represent the ΔS responsible for the singlet formation and FM ordering, respectively. Red curve is a fit of the FM contribution (Cmag ~ T 3/2). c, Cmag versus T curves under the different H. Dashed curves are the results of the Schottky model calculations for the electron spins of Gd. There is no H-driven Cmag shift ruling out the possibility of the Schottky anomaly due to the electron spins of Gd. d, Comparison of Cmag versus T curves between experimental data and the calculated data using the Schottky anomaly model for the nuclear spins of 117Sn and 119Sn. The fitting result shows that the required internal field is about −1287 kOe.

Supplementary Fig. 5 | Crossover from non-Fermi-liquid (NFL) to Fermi-liquid (FL) behaviour driven by an external magnetic field. a, ρ(T) in the low-T region under different applied H. Red curves are a single power-law fit ρ = ρ0 + AT n of the data, where ρ0 is the residual resistivity and A is a constant. b, The field-dependent n value. Blue and red coloured backgrounds represent NFL and FL regions.

Supplementary Fig. 6 | Electronic band structures. a, ARPES spectra along the Γ–X–Γ direction at various T. b–c, EDCs near EF. Each EDC is a momentum integrated spectrum from the grey area in a. c, EDCs are divided by the Fermi-Dirac distribution for better visualization of the flat band peak. d, Schematic illustration of the exchange splitting of the fast-dispersing band near TC. e, Schematic illustration of band hybridization between the fast-dispersing band (green colour) and weakly dispersing band (red colour) at the low-T region. f–g, Wide energy range ARPES data along the Γ–X–Γ direction at 13 K obtained with linear horizontal (π) and vertical () polarizations, respectively. h, Calculated band structure along the Γ–X–Γ direction. Two observed bands near EF (labeled as A and B) are well reproduced by the calculated band structure.

Supplementary Fig. 7 | Calculated electronic structure of Gd3SnC. a–d, The band structure calculated by GGA (a), GGA+SOC (b), GGA+U (c), and GGA+U+SOC (d) methods. Red and green colours represent the t2g and eg contributions of Gd 5d-orbitals, respectively. e–h, The band structure calculated by GGA+U+SOC method with different U values.

Supplementary Fig. 8 | Calculated COHP for antiperovskite Gd3SnC. pCOHP for various bonds between constituent elements in Gd3SnC.

Supplementary Table 1 | Lattice parameters of antiperovskite Gd3SnC and La3SnC from Rietveld refinement of XRD data.

| System | Gd3SnC | La3SnC |
| --- | --- | --- |
| Space group | Pm3m | Pm3m |
| Lattice parameter (Å) | a = 4.92895(7) d(Gd–Gd) = 3.48529(6) d(Gd–Sn) = 3.48529(6) d(Gd–C) = 2.46447(4) | a = 5.1351(14) d(La–La) = 3.6311(10) d(La–Sn) = 2.5675(8) d(La–C) = 3.6311(10) |
| Atomic position | Gd (0, 0.5, 0.5) Sn (0, 0, 0) C (0.5, 0.5, 0.5) | La (0, 0.5, 0.5) Sn (0, 0, 0) C (0.5, 0.5, 0.5) |
| V (Å) | 119.74660 | 135.40873 |
| Z | 1 | 1 |
| Rwp | 7.72 | 15.60 |
| Goodness of fit | 2.1 | 4.32 |

Supplementary Table 2 | List of −ICOHP values and bond lengths for various chemical bonds.

| Bond | −ICOHP (spin-up) (eV/bond) | −ICOHP (spin-down) (eV/bond) | Bond length (Calc., Å) | Bond length (Exp., Å) |
| --- | --- | --- | --- | --- |
| Gd–Gd | 0.52 | 0.45 | 3.50 | 3.49 |
| Gd–Sn | 0.59 | 0.61 | 3.50 | 3.49 |
| Gd–C | 1.43 | 1.53 | 2.47 | 2.46 |
| Sn–Sn | 0.02 | 0.01 | 4.95 | 4.93 |
| Sn–C | 0.01 | 0.01 | 4.29 | 4.27 |
| C–C | 0.06 | 0.06 | 4.95 | 4.93 |