Supporting Information for

Peroxidase-like Fe0@FeMn-NC for the efficient degradation of 4-CP: Critical role of Fe0

Xinxin Lv a, b, Huilai Liu a, b, Zhihao Li a, b, Minshu Cui a, Kangping Cui a, Zhengliang Dai c, Bei Wang c, Xing Chen a, b

a. Key Laboratory of Nanominerals and Pollution Control of Higher Education Institutes, School of Resources and Environmental Engineering, Hefei University of Technology, Hefei 230009, P. R. China;

b. Key Lab of Aerospace Structural Parts Forming Technology and Equipment of Anhui Province, Institute of Industry and Equipment Technology, Hefei University of Technology, Hefei, 230009, P. R. China;

c. Anqing Changhong Chemical Co., Ltd., Anqing, 246002, P. R. China

Table of contents

Figure S1. SEM images of (a) NC-900, (b) Fe-NC, and (c) Mn-NC.

Figure S2. XPS spectra of (a) Survey; (b) C 1s; (c) N 1s; (d) O 1s for Fe0@FeMn-NC.

Figure S3. Steady-state kinetic assay of NC-900 nano-enzyme. (a) Time-dependent absorption changes at 652 nm in the presence of different concentrations of H2O2; (b) The velocities were measured with different H2O2 concentrations; (c) Double reciprocal plots between velocity and H2O2 concentration.

Figure S4. Steady-state kinetic assay of Fe-NC nano-enzyme. (a) Time-dependent absorption changes at 652 nm in the presence of different concentrations of H2O2; (b) The velocities were measured with different H2O2 concentrations; (c) Double reciprocal plots between velocity and H2O2 concentration.

Figure S5. Steady-state kinetic assay of Mn-NC nano-enzyme. (a) Time-dependent absorption changes at 652 nm in the presence of different concentrations of H2O2; (b) The velocities were measured with different H2O2 concentrations; (c) Double reciprocal plots between velocity and H2O2 concentration.

Figure S6. Comparison of the kinetic parameters Km and Vmax of various nano-enzymes when hydrogen peroxide was used as a substrate in this study and the literature reports.

Figure S7. Effect of NBA, AA, and FFA on the degradation of 4-CP in the Fe0@FeMn-NC/H2O2 system.

Figure S8. Mass spectrum of by-products in the degradation of 4-CP.

Figure S9. Main degradation processes of 4-CP and its intermediates.

Figure S10. Degradation rates of 4-CP and TOC in five cycles.

Table S1. Specific surface area, pore volume and pore width of different samples.

Table S2. Comparison of kinetic parameters with other catalysts using H2O2 as substrate.

Table S3. Changes in indicators before and after the reaction of raw water in a chemical plant workshop.

References

Figure S1. SEM images of (a) NC-900, (b) Fe-NC, and (c) Mn-NC.

Figure S2. XPS spectra of (a) Survey; (b) C 1s; (c) N 1s; (d) O 1s for Fe0@FeMn-NC.

Figure S3. Steady-state kinetic assay of NC-900 nano-enzyme. (a) Time-dependent absorption changes at 652 nm in the presence of different concentrations of H2O2; (b) The velocities were measured with different H2O2 concentrations; (c) Double reciprocal plots between velocity and H2O2 concentration.

Figure S4. Steady-state kinetic assay of Fe-NC nano-enzyme. (a) Time-dependent absorption changes at 652 nm in the presence of different concentrations of H2O2; (b) The velocities were measured with different H2O2 concentrations; (c) Double reciprocal plots between velocity and H2O2 concentration.

Figure S5. Steady-state kinetic assay of Mn-NC nano-enzyme. (a) Time-dependent absorption changes at 652 nm in the presence of different concentrations of H2O2; (b) The velocities were measured with different H2O2 concentrations; (c) Double reciprocal plots between velocity and H2O2 concentration.

Figure S6. Comparison of the kinetic parameters Km and Vmax of various nano-enzymes when hydrogen peroxide was used as a substrate in this study and the literature reports (Chen et al., 2014; Ding et al., 2023; Gao et al., 2007; Hu et al., 2013; Jampaiah et al., 2016; Li et al., 2015; Liu et al., 2018; Peng et al., 2022; Wang, H. et al., 2021; Wang et al., 2018; Wang et al., 2019; Wang, Y. et al., 2021; Wang, Y.F. et al., 2021).

Figure S7. Effect of NBA, AA, and FFA on the degradation of 4-CP in the Fe0@FeMn-NC/H2O2 system.

Figure S8. Mass spectrum of by-products in the degradation of 4-CP.

Figure S9. Main degradation processes of 4-CP and its intermediates.

Figure S10. Degradation rates of 4-CP and TOC in five cycles.

Table S1. Specific surface area, pore volume, and pore width of different samples.

| Catalysts | Surface area (m2 g-1) | Pore volume (cm3 g-1) | Pore width (Å) |
| --- | --- | --- | --- |
| NC-900 | 1097.847 | 0.556 | 5.67 |
| Fe-NC | 648.315 | 0.289 | 5.93 |
| Mn-NC | 641.372 | 0.282 | 5.94 |
| Fe0@FeMn-NC | 657.721 | 0.295 | 5.90 |

Table S2. Comparison of kinetic parameters with other catalysts using H2O2 as substrate.

| Catalysts | Km (mM) | Vmax (10-8 M/s) | Ref. |
| --- | --- | --- | --- |
| NC-900 | 4.53 | 2.17 | This Work |
| Fe-NC | 3.38 | 7.33 |  |
| Mn-NC | 3.23 | 6.18 |  |
| Fe0@FeMn-NC | 0.25 | 4.5 |  |
| Au/Co3O4-CeOXNCs | 0.2724 | 0.3898 | (Liu et al., 2018) |
| Fe/CeO2 NRs | 47.6 | 16.6 | (Jampaiah et al., 2016) |
| g-C3N4 | 0.682 | 2.0 | (Wang et al., 2019) |
| FeNCP/NW | 8.02 | 31.28 | (Ding et al., 2023) |
| CDs@ZIF-8 | 0.737 | 1.22 | (Wang, Y. et al., 2021) |
| CDs@Cu-ZIF-8 | 0.232 | 0.2 | (Wang, Y.F. et al., 2021) |
| Co3O4 HNCs | 19.9 | 1.92 | (Wang, H. et al., 2021) |
| Cu NCs | 29.16 | 4.22 | (Hu et al., 2013) |
| BSA-Pt | 41.8 | 16.7 | (Li et al., 2015) |
| Co3(PO4)·8H2O | 0.073 | 1.2 | (Peng et al., 2022) |
| ZIF-67 | 3.52 | 0.28 | (Wang et al., 2018) |
| Au NPs/Cit-GNs | 25.08 | 21.5 | (Chen et al., 2014) |
| HRP | 3.7 | 8.71 | (Gao et al., 2007) |

Table S3. Changes in indicators before and after the reaction of raw water in a chemical plant workshop.

|  | pH | Turbidity (NTU) | COD (mg/L) | 4-CP (mg/L) | 4-NP (mg/L) | BPA (mg/L) | PCM (mg/L) | Phenol (mg/L) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| before | 9.5 | 1872 | 2023 | 24.97 | 38.71 | 13.25 | 9.32 | 43.71 |
| after | 4.0 | 563 | 876 | 2.38 | 4.76 | 1.92 | 2.10 | 2.63 |

References

Chen, X.M., Tian, X.T., Su, B.Y., Huang, Z.Y., Chen, X., Oyama, M., 2014. Au nanoparticles on citrate-functionalized graphene nanosheets with a high peroxidase-like performance. Dalton Transactions 43(20), 7449-7454. https://doi.org/10.1039/c3dt53316f.

Ding, S.C., Barr, J.A., Lyu, Z., Zhang, F.Y., Wang, M.Y., Tieu, P., Li, X., Engelhard, M.H., Feng, Z.X., Beckman, S.P., Pan, X.Q., Li, J.C., Du, D., Lin, Y.H., 2023. Effect of Phosphorus Modulation in Iron Single-Atom Catalysts for Peroxidase Mimicking. Advanced Materials. https://doi.org/10.1002/adma.202209633.

Gao, L.Z., Zhuang, J., Nie, L., Zhang, J.B., Zhang, Y., Gu, N., Wang, T.H., Feng, J., Yang, D.L., Perrett, S., Yan, X., 2007. Intrinsic peroxidase-like activity of ferromagnetic nanoparticles. Nature Nanotechnology. 2(9), 577-583. https://doi.org/10.1038/nnano.2007.260.

Hu, L., Yuan, Y., Zhang, L., Zhao, J., Majeed, S., Xu, G., 2013. Copper nanoclusters as peroxidase mimetics and their applications to H2O2 and glucose detection. Analytica Chimica Acta 762, 83-86. https://doi.org/10.1016/j.aca.2012.11.056.

Jampaiah, D., Srinivasa Reddy, T., Kandjani, A.E., Selvakannan, P.R., Sabri, Y.M., Coyle, V.E., Shukla, R., Bhargava, S.K., 2016. Fe-doped CeO2 nanorods for enhanced peroxidase-like activity and their application towards glucose detection. Journal of Materials Chemistry B 4(22), 3874-3885. https://doi.org/10.1039/c6tb00422a.

Li, W., Chen, B., Zhang, H., Sun, Y., Wang, J., Zhang, J., Fu, Y., 2015. BSA-stabilized Pt nanozyme for peroxidase mimetics and its application on colorimetric detection of mercury(II) ions. Biosensors & Bioelectronics 66, 251-258. https://doi.org/10.1016/j.bios.2014.11.032.

Liu, H., Ding, Y.N., Yang, B.C., Liu, Z.X., Liu, Q.Y., Zhang, X., 2018. Colorimetric and ultrasensitive detection of H2O2 based on Au/Co3O4-CeOx nanocomposites with enhanced peroxidase-like performance. Sensors and Actuators B-Chemical 271, 336-345. https://doi.org/10.1016/j.snb.2018.05.108.

Peng, L.J., Zhou, H.Y., Zhang, C.Y., Yang, F.Q., 2022. Study on the peroxidase-like activity of cobalt phosphate and its application in colorimetric detection of hydrogen peroxide. Colloids and Surfaces A-Physicochemical and Engineering Aspects 647. https://doi.org/10.1016/j.colsurfa.2022.129031.

Wang, H., Fu, W., Chen, Y., Xue, F., Shan, G., 2021. ZIF-67-derived Co3O4 hollow nanocage with efficient peroxidase mimicking characteristic for sensitive colorimetric biosensing of dopamine. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy 246, 119006. https://doi.org/https://doi.org/10.1016/j.saa.2020.119006.

Wang, S., Xu, D., Ma, L., Qiu, J., Wang, X., Dong, Q., Zhang, Q., Pan, J., Liu, Q., 2018. Ultrathin ZIF-67 nanosheets as a colorimetric biosensing platform for peroxidase-like catalysis. Analytical & Bioanalytical Chemistry(No.27), 7145-7152.

Wang, Y., Liu, R.L., Chen, G.N., Wang, L., Yu, P., Shu, H., Bashir, K., Fu, Q., 2019. Hemin-porous g-C3N4 hybrid nanosheets as an efficient peroxidase mimic for colorimetric and visual determination of glucose. Microchim. Acta 186(7), 10. https://doi.org/10.1007/s00604-019-3564-9.

Wang, Y., Liu, X., Wang, M., Wang, X., Ma, W., Li, J., 2021. Facile synthesis of CDs@ZIF-8 nanocomposites as excellent peroxidase mimics for colorimetric detection of H2O2 and glutathione. Sensors and Actuators B: Chemical 329, 129115. https://doi.org/https://doi.org/10.1016/j.snb.2020.129115.

Wang, Y.F., Wang, M.K., Wang, X.X., Ma, W.N., Liu, J.X., Li, J.Y., 2021. Designed synthesis of CD@Cu-ZIF-8 composites as excellent peroxidase mimics for assaying glutathione. Materials Chemistry Frontiers 5(16), 6125-6132. https://doi.org/10.1039/d1qm00702e.

Dr. Xing Chen

Institute of Industry and Equipment Technology, Hefei University of Technology, Hefei, 230009, P. R. China

Email: xingchen@hfut.edu.cn