Supplementary Material

Enhancing Enzyme Stability and Functionality: Covalent Immobilization of Trypsin on Magnetic Gum Arabic Modified Fe3O4 Nanoparticles

Yasaman Behshad1, Mohammad Pazhang*,1, Saeed Najavand1, Mohammad Sabzi* 2,3

1 Department of Cellular and Molecular Biology, Faculty of Science, Azarbaijan Shahid Madani University, Tabriz, Iran

2 Department of Mechanical Engineering, North Dakota State University, Fargo, North Dakota 58102, United States

3 Department of Chemical Engineering, Faculty of Engineering, University of Maragheh, 55181-83111, Maragheh, Iran

Corresponding authors email address:

Mohammad Pazhang: pazhang@azaruniv.ac.ir;

Mohammad Sabzi: m.sabzi1984@gmail.com

Figure S1. Comparison of the thermograms of (a) Fe3O4 nanoparticles and (b) GA modified Fe3O4 nanoparticles.

Table S1. Kinetic parameters of free and immobilized trypsin.

| Vmax [µmol mg-1min-1]* | Km [mg/mL] | Enzyme |
| --- | --- | --- |
| 20.00 | 2.00 | Free Trypsin |
| 10.50 | 3.65 | Immobilized Trypsin |

*Reaction conditions: free and immobilized trypsin (5 mg/mL), casein (0.25 mg/mL) in sodium phosphate buffer (7.5 mM, pH 5).