- Appendices

Tab. A.1 the relevant physical parameters of VOF simulations regarding the successive scanning thermal cycling in fig.2(a) and the multi-track thermal cycling in fig.2(b).

| Properties with units | Value |
| --- | --- |
| Density/kg m-3 | 4510 [54] |
| Thermal conductivity of solid / W m-1 K-1 | -0.797+18.2×10-3T-2.0×10-6T2 [55] |
| Heat capacity of solid/ J kg-1 K-1 | 415+0.1838T+5×10-7T2 2 [55] |
| Thermal conductivity of liquid/ W m-1 K-1 | 33.4 [55] |
| Heat capacity of liquid/ J kg-1 K-1 | 830 [55] |
| Liquidus temperature/ K | 1923 [55] |
| Boiling temperature/ K | 3133 [56] |
| Latent heat of fusion/ J kg-1 | 2.88×105 [56] |
| Latent heat of evaporation/ J kg-1 | 4.7×106 [56] |
| Laser radius/ mm | 0.06 |
| Laser absorptivity | 0.5 |
| Thickness of powder layer/ mm | 0.03 |
| Initial temperature/ K | 298 |
| Surface tension coefficient/ kg/s2K | -0.00026 [54, 56-57] |
| Convective heat transfer coefficient | 19 [54] |

- Tab. A.2  the temperature depending mechanical parameters of the fully thermal coupled FEM simulations regarding the multi-layer scanning thermal cycling in fig.2(c) and fig.17 [58].

| Temperature/ K | Linear expansion coefficient/ ×10-6K-1 | Young's modulus /GPa | yield strength/ MPa |
| --- | --- | --- | --- |
| 199 | 8.78 | 125 | 1000 |
| 175 | 9.83 | 110 | 630 |
| 480 | 10.0 | 100 | 630 |
| 592 | 10.7 | 110 | 525 |
| 703 | 11.1 | 80 | 500 |
| 814 | 11.2 | 74 | 446 |
| 925 | 11.7 | 55 | 300 |
| 1036 | 12.2 | 27 | 45 |
| 1147 | 12.3 | 20 | 25 |
| 1369 | 12.4 | 5 | 5 |
| 1925 | 12.5 | 0.1 | 0.1 |