Support Information for

Ultrafast Upgrading of Aniline-Based Redox-Active Organics via Electrolyte-Triggered In-Situ Polymerization for Advanced Magnesium-Ion Batteries

Chemical and Materials

1-aminoanthraquinone (1-AAQ, 97%) was purchased from Aladdin. 1,5-diaminoanthraquinone (1,5-DAAQ, 97%), anhydrous magnesium chloride (MgCl2, 99.99%) and magnesium bis(hexamethylsilazide) (Mg(HMDS)2, 97%) were purchased from Sigma-Aldrich. N-butyl-N-methyl-piperidinium bis((trifluoromethyl)sulfonyl)imide (PP14TFSI) was purchased from Lanzhou Central Kate Industry and Trade Co., Ltd. Anhydrous tetrahydrofuran (THF) was purchased from Alfa Aesar. Mg foils (0.05 mm thickness, 99.99%) were purchased from Huabei Magnesium Co. Ltd. All chemicals were used without further purification.

Preparation of the Mg(HMDS)2-4MgCl2/THF electrolyte

The Mg(HMDS)2-4MgCl2/THF electrolyte was prepared in an Ar-filled glovebox ([O2] < 0.1 ppm, [H2O] < 0.1 ppm) according to a modified process in the previous report.30 Briefly, 1.25 mmol of Mg(HMDS)2 (431.35 mg) and 5 mmol of anhydrous MgCl2 (476.05 mg) were added into 5 mL of anhydrous THF solution under continuous stirring. Then, 2.5 mL of PP14TFSI was added to the above solution and vigorously stirred for 50 h. The concentration of the as-prepared Mg(HMDS)2-4MgCl2/THF electrolyte is 0.83 M.

Electrochemical measurements

Briefly, 50 wt.% of the active material, 40 wt.% of super P carbon black, and 10 wt.% of polyvinylidene fluoride (PVDF) were mixed in N-methyl-2-pyrrolidone (NMP) solvent and stirred for 5 h to form a slurry. Afterward, the slurry was coated on carbon paper and dried under vacuum at 60 °C for 24 h. Then, the electrode was cut into small disks with a diameter of 14 mm. The areal loading of the active material was about 2.0 mg cm-2. The CR 2032 coin cells were assembled using Whatman glass fiber as the separator and Mg foil as the counter electrode in an Ar-filled glovebox. For the assembly of each coin cell, 40 μL of the as-prepared electrolyte was used. Galvanostatic discharge/charge measurements were conducted on a LAND CT2001A battery test system in a voltage range of 0.2-2.6 V (vs. Mg2+/Mg). Electrochemical impedance spectroscopy (EIS) measurements were performed in a frequency range from 100 kHz to 0.01 Hz on an electrochemical workstation (Chenhua, CHI-760E). The galvanostatic intermittent titration technique (GITT) tests were conducted at 100 mA g-1 for 20 min followed by a rest time of 30 min to reach the steady-state voltage.

Characterizations

Attenuated total reflectance Fourier transform infrared (ATR-FTIR) spectra were measured on a Nicolet iS50 spectrometer. UV-Vis absorption spectra in the solid state were collected in a wavelength range of 200-850 nm using BaSO4 as the matrix powder (Shimadzu UV-2600). A field-emission scanning electron microscope (FESEM, FEI Nova NanoSEM 450) coupled with an X-ray energy dispersive spectroscope accessory (EDS, Burker X-flash 6|30) were used to analyze the morphological and compositional features of the samples. In-situ Raman spectroscopy was performed on a Horiba JY Evolution Raman spectrometer coupled with an in-situ Raman characterization electrochemical cell during charge-discharge cycles at the current density of 100 mA g-1. To avoid the possible influence of photoluminescence, a laser source of 473 nm wavelength (blue) was used to excite the Raman signals. For ex-situ characterizations, the electrodes were discharged to 0.7 V, fully discharged to 0.1 V, or fully charged to 2.6 V at a current density of 100 mAh g-1, and then the electrodes were removed from the cell in a glovebox, and washed with THF three times to remove residual electrolyte. Then the electrodes were subsequently dried at 40℃ under vacuum for 6 h to remove residual THF. Ex-situ XPS spectroscopy was conducted on a PHI-5000 VersaProbe Ⅲ X-ray photoelectron spectrometer.

Figure S1. Digital photographs depicting that the electrode disks based on 1-AAQ (top) and 1,5-DAAQ (bottom) monomers contacted with Mg(HMDS)2 electrolyte can be spontaneously polymerized into PAAQ and PDAAQ, respectively.

Figure S2. Optical photographs were immediately taken after the addition of different amounts of Mg(HMDS)2 powder into 0.7 mL THF solution of (a) 1-AAQ or (b) 1,5-DAAQ (7.7 mg). The corresponding concentrations of Mg(HMDS)2 from No.1 to No.7 are 160 mM, 80 mM, 40 mM, 20 mM, 8 mM, 4 mM, 2 mM, and 0, respectively.

Figure S3. CV curves of the Mg||PAAQ battery at a scan rate of 0.1mV s-1.

Figure S4. EIS data of PAAQ and PDAAQ electrodes.

Figure S5. Long-term cycling test of PDAAQ electrodes at a high current density of 4000 mA g-1.

Figure S6. Cycling performances of (a) small molecule anthraquinone (AQ) cathode and (b) commercial PANI cathode at a current density of 100 mA g-1, respectively.

Figure S7. Ex-situ EDS patterns of PDAAQ electrode at different discharge/charge states after initial five cycles.

Table S1. Electrochemical performance comparisons of PDAAQ and PAAQ with other previously reported organic cathode materials for RMBs.

| Ref. | Material | Potential (vs. Mg2+/Mg) | Rate capability (mAh g-1) | Maximum discharge capacity (mAh g-1) | Capacity retention |
| --- | --- | --- | --- | --- | --- |
| This work |  | 1.5 V versus Mg/Mg2+ | 221.6 (100 mA g-1) 131.6 (500) 109.0 (1000) 84.6 (2000) 44.7 (4000) | 254 (100 mA g-1) | 8000 cycles, 64.5 mAh g-1 (2000 mA g–1) |
| This work |  | 1.8 V versus Mg/Mg2+ | 94.3 (100 mA g-1) 77.4 (500) 67.6 (1000) 60.3 (2000) | 124 (100 mA g-1) | 6000 cycles, 53.9 mAh g-1 (2000 mA g–1) |
| [17] |  | 1.6 V versus Mg/Mg2+ | 130 (100 mA g-1) 63.2 (500) | 130 (100 mA g-1) | 4000 cycles, 53.6 mAh g-1 (500 mA g–1) |
| [31] |  | 2.0 V versus Mg/Mg2+ | - | 226 (63.8 mA g-1) | 30 cycles, 74 mAh g-1 (63.8 mA g-1) |
| [5] |  | 1.5~0.5 V versus Mg/Mg2+ | 100 (500 mA g-1) | 225 (50 mA g-1) | 100 cycles, ~50 mAh g-1 (50 mA g-1) |
| [2] |  | 1.55 V versus Mg/Mg2+ | 122 (130 mA g-1) ~42 (650) | 122 (130 mA g-1) | 100 cycles, ~82 mAh g-1 (130 mA g-1) |
| [2] |  | 1.5 V versus Mg/Mg2+ | 133 (130 mA g-1) ~50 (650) | 133 (130 mA g-1) | 100 cycles, ~131 mAh g-1 (130 mA g-1) |
| [4] |  | 1.7 V versus Mg/Mg2+ | ~48 (500 mA g-1) | 85 (50 mA g-1) | 100 cycles, ~85 mAh g-1 (50 mA g-1) |
| [8] |  | 1.05 V versus Mg/Mg2+ | - | 81.2 (22.8 mA g-1) | 20 cycles, 20 mAh g-1 (22.8 mA g-1) |
| [10] |  | 1.45 V versus Mg/Mg2+ | 130 (150 mA g-1) 60 (1500) 48 (3000) | 130 (150 mA g-1) | 200 cycles, 120 mAh g-1 (150 mA g-1) |
| [32] |  | 1.6 V versus Mg/Mg2+ | 126 (200 mA g-1) ~58 (300) ~30 (500) | ~126 (200 mA g-1) | 150 cycles, 100 mAh g-1 (200 mA g-1) |
| [13] |  | 1.0 V versus Mg/Mg2+ | ~89 (100 mA g-1) ~87 (200) | ~90 (50 mA g-1) | 2000 cycles, 73 mAh g-1 (1000 mA g-1) |
| [13] |  |  |  |  |  |
| [33] |  | 2.0 V versus Mg/Mg2+ | ~80 (100 mA g-1) ~40 (1000) ~23 (2000) | ~80 (100 mA g-1) | 1000 cycles, 38 mAh g-1 (500 mA g-1) |
| [3] |  | 1.5 V versus Mg/Mg2+ | 132 (183 mA g-1) 87 (732) 73 (1830) 59 (3660) | 132 (183 mA g-1) | 8000 cycles, 39 mAh g-1 ~3660 mAh g-1 |
| [3] |  | 1.5 V versus Mg/Mg2+ | 161 (158 mA g-1) 118 (632) 84 (1580) 63 (3160) | 161 (158 mA g-1) | 8000 cycles, 42 mAh g-1 ~3160 mAh g-1 |

Abbreviations:

AN = acetonitrile

THF = tetrahydrofuran

DME = diglyme

DMSO = dimethylsulfoxide

APC = [AlCl3][PhClMg]

Mg(TFSI)2 = magnesium(II) bis(trifluoromethane sulfonyl)imide