Table 1 Summary of laboratory measurements before and after experiments. Sample characterization includes volume (V), sample length (l), mass (m), and density (ρ). Subscript A denotes Archimedean measurements. Total volume, Vtot, before experiments was estimated geometrically. Total volume after experiments was measured using μCT data. Reported uncertainties in parentheses are ±2σ. n.d. is not determined

| Sample | l (cm) |  | m (g) |  | ρA (kg m-3) |  | VA (mm3) |  | Vtot (mm3) |  | max T (°C) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | before | after | before | after | before | after | before | after | before | after |  |
| ϕx = 0 |  |  |  |  |  |  |  |  |  |  |  |
| F0-05 | 0.7834 | 1.0477 | 0.4927 | 0.4814 | 2454.9 (2.2) | 739.2 (2.4) | 200.7 (0.2) | 651.3 (2.0) | 204.1 | n.d. | 648 |
| F0-06 | 0.2844 | 0.3076 | 0.0816 | 0.0796 | 2461.9 (5.2) | 749.0 (5.8) | 33.2 (0.0) | 106.3 (0.8) | 33.6 | n.d. | 661 |
| F0-03 | 1.1811 | 1.5764 | 0.6716 | 0.6527 | 2460.6 (0.6) | 812.6 (2.6) | 273.0 (0.0) | 803.2 (2.6) | 273.9 | 910.6 (18.2) | 706 |
| F0-04 | 0.9033 | 1.2822 | 0.5845 | 0.5585 | 2456.9 (1.8) | 448.4 (4.0) | 237.9 (0.2) | 1245.6 (11.2) | 239.0 | n.d. | 778 |
| ϕx = 0.5 |  |  |  |  |  |  |  |  |  |  |  |
| F50-05 | 0.6744 | 0.9122 | 0.4091 | 0.4009 | 2319.1 (1.0) | 1187.4 (6.2) | 176.4 (0.0) | 337.6 (1.8) | 177.9 | n.d. | 705 |
| F50-02 | 1.1173 | 1.3180 | 0.6006 | 0.5929 | 2370.2 (1.2) | 1460.0 (2.6) | 253.4 (0.2) | 406.1 (0.8) | 257.2 | 444.5 (8.8) | 749 |
| F50-04 | 0.8548 | 1.3146 | 0.5263 | 0.5111 | 2333.0 (1.8) | 676.6 (4.8) | 225.6 (0.2) | 755.4 (5.2) | 226.9 | n.d. | 803 |
| ϕx = 0.6 |  |  |  |  |  |  |  |  |  |  |  |
| F60-04 | 1.1101 | 1.2397 | 0.6853 | 0.6766 | 2372.2 (1.2) | 2025.8 (0.8) | 288.9 (0.2) | 334.0 (0.2) | 292.9 | n.d. | 703 |
| F60-02 | 1.1605 | 1.3345 | 0.6457 | 0.6384 | 2405.0 (2.8) | 1823.0 (8.6) | 268.5 (0.4) | 350.2 (1.6) | 272.6 | 390.7 (7.8) | 754 |
| F60-03 | 1.0610 | 1.2283 | 0.5863 | 0.5765 | 2401.9 (1.0) | 1586.1 (10.6) | 244.1 (0.2) | 363.5 (2.4) | 247.7 | n.d. | 803 |
| ϕx = 0.7 |  |  |  |  |  |  |  |  |  |  |  |
| F70-04 | 1.1185 | 1.1310 | 0.7083 | 0.7014 | 2447.2 (1.6) | 2383.7 (1.8) | 289.4 (0.2) | 294.3 (0.2) | 292.9 | n.d. | 704 |
| F70-02 | 1.1092 | 1.1579 | 0.6159 | 0.6107 | 2487.7 (1.0) | 2297.2 (2.6) | 247.6 (0.2) | 265.9 (0.4) | 252.0 | 289.6 (5.8) | 755 |
| F70-03 | 0.9975 | 1.0654 | 0.6333 | 0.6270 | 2456.3 (1.4) | 2101.3 (6.0) | 257.8 (0.2) | 298.4 (0.8) | 261.8 | n.d. | 803 |
| ϕx = 0.8 |  |  |  |  |  |  |  |  |  |  |  |
| F80-01 | 1.1738 | 1.1775 | 0.6896 | 0.6855 | 2535.3 (1.4) | 2525.2 (1.6) | 272.0 (0.2) | 271.5 (0.2) | 276.1 | n.d. | 701 |
| F80-06 | 1.1251 | 1.1606 | 0.7306 | 0.7246 | 2518.8 (0.8) | 2473.1 (0.4) | 290.0 (0.0) | 293.0 (0.0) | 293.9 | 314.8 (6.2) | 754 |
| F80-07 | 1.0488 | 1.0886 | 0.6786 | 0.6732 | 2514.1 (1.6) | 2392.1 (0.6) | 269.9 (0.2) | 281.4 (0.0) | 274.9 | n.d. | 804 |
| F80-02 | 1.0961 | 1.1638 | 0.6384 | 0.6331 | 2537.9 (1.0) | 2369.9 (2.0) | 251.5 (0.2) | 267.1 (0.2) | 255.8 | n.d. | 855 |