Supplementary Table 1: Comparison of zero shear rate viscosity (η0), storage modulus (Pa) and loss modulus (Pa) between CLT and human cornea.

| S.No | Construct | Zero shear rate viscosity η0 (mPas) | Storage Modulus (Pa) | Loss Modulus (Pa) |
| --- | --- | --- | --- | --- |
| 1. | CLT | 1.07 x 105 | 61.9 | 0.74 |
| 2. | Human Cornea | 5.04 x 105 | 85.6 | 28.52 |