Supplementary Table 1: Comparison of zero shear rate viscosity (η0), storage modulus (Pa) and loss modulus (Pa) between CLT and human cornea.
	S.No
	Construct
	Zero shear rate viscosity η0 (mPas)
	Storage Modulus (Pa)
	Loss Modulus (Pa)

	1.
	CLT
	1.07 x 105
	61.9
	0.74

	2.
	Human Cornea
	5.04 x 105
	85.6
	28.52




