Table 5.1 Specific capacitance of Ni doped Co3O4 samples at various scan rates

| Sample | Specific capacitance of Ni doped Co3O4 samples (F/g) at various scan rates |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 100 mV/s | 50 mV/s | 20 mV/s | 10 mV/s | 5 mV/s |
| Co3O4:3%Ni | 111 | 147 | 182 | 254 | 299 |
| Co3O4:5%Ni | 95 | 148 | 179 | 208 | 244 |
| Co3O4:7%Ni | 67 | 94 | 140 | 204 | 236 |

Table 2 Specific capacitance of Ni doped Co3O4 samples at various current densities

| Sample | Specific capacitance of Ni doped Co3O4 samples (F/g) at various current densities |  |  |  |
| --- | --- | --- | --- | --- |
|  | 9 A/g | 6 A/g | 3 A/g | 1.5 A/g |
| Co3O4:3%Ni | 271 | 311 | 328 | 347 |
| Co3O4:5%Ni | 217 | 238 | 273 | 293 |
| Co3O4:7%Ni | 172 | 260 | 249 | 258 |