Table 5.1 Specific capacitance of Ni doped Co3O4 samples at various scan rates
	Sample
	Specific capacitance of Ni doped Co3O4  samples  (F/g) at various scan rates

	
	100 mV/s
	50 mV/s
	20 mV/s
	10 mV/s
	5 mV/s

	Co3O4:3%Ni
	111
	147
	182
	254
	299

	Co3O4:5%Ni
	95
	148
	179
	208
	244

	Co3O4:7%Ni
	67
	94
	140
	204
	236



Table 2 Specific capacitance of Ni doped Co3O4 samples at various current densities
	Sample
	Specific capacitance of Ni doped Co3O4  samples  (F/g) at various current densities

	
	9 A/g
	6 A/g
	3 A/g
	1.5 A/g

	Co3O4:3%Ni
	271
	311
	328
	347

	Co3O4:5%Ni
	217
	238
	273
	293

	Co3O4:7%Ni
	172
	260
	249
	258




