Exfoliation of an extruded Mg-4Li-1Ca alloy in presence of glucose and bovine serum albumin

Lei Cai a, Mei-Qi Zeng a, Meng-Jie Liu a, Jing-Yu Bao a, Yu-Qian Ren a, M. Bobby Kannan b, Lan-Yue Cui a, Cheng-Bao Liu a, Fen Zhang a, Shuo-Qi Li a, Rong-Chang Zeng a *

a Corrosion Laboratory for Light Metals, School of Materials Science and Engineering, Shandong University of Science and Technology, Qingdao 266590, China

b School of Engineering, University of Newcastle, Callaghan, New South Wales, 2308, Australia

* Corresponding author. E-mail: rczeng@foxmail.com (R.C. Zeng).

Fig. S1. Schematic illustration of different sections of extruded Mg-4Li-1Ca.

Fig. S2. Average grain size on different surfaces of Mg-4Li-1Ca.

Fig. S3. Local Average Misorientation map and Local misorientation distribution of Mg-4Li-1Ca alloy, (a) (d) surface section (SS); (b) (e) longitudinal section (LS) and (c) (f) transverse section (TS).

EBSD orientation data was used to determine local dislocations and the dislocation density, and the core average misorientation (KAM) methods were used to quantify the residual stresses within the material 1. In this study, all local dislocation angles greater than 2° were selected and excluded. The local misorientation of a point (500 nm × 500 nm) was determined based on the 24 points around it as follows (Eq. 1):

∆θi=1nj=1nθjsur-θi                                                                  (1)

where, θi represents the local misorientation at the point ‘i’ and θjsur is the misorientation at its neighboring point ‘j’. To extrapolate information about the GND (geometrically necessary dislocation) density, the strain gradient theory was employed using a straightforward method as described in reference (Eq. 2) 2:

ρGND=2∆θiμb=B∆θi                                                                    (2)

where, ρGND is the GND density at the point of interest; ∆θi represents the local misorientation; µ is the unit length of the point (500 nm); b is the Burgers vector. For Mg, the constant B is equal to 2μb=4b×1015 m2, which we used in the calculation 3,4. Fig. S3 shows the column charts that display the calculated GND density.

Fig. S4. HER curves of Mg-4Li-1Ca alloys immersed in different solutions for 72 h.

Fig. S5. Electrochemistry curves of the different faces of Mg-4Li-1Ca alloy.

Fig. S6. EDS of the corresponding points in Fig. 4j-l.

Fig. S7. EDS of the corresponding points in Fig. 4m-x.

Table S1. Chemical composition of solution for immersion test (g/L).

| Solution | NaCl | KCl | CaCl2 |  | NaHCO3 | Glu | MgCl2·6H2O | MgSO4·7H2O | KH2PO4 | Na2HPO4·12H2O | BSA |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 g/L Glu | 8.0 | 0.4 | 0.14 | 0.35 |  | 1 | 0.1 | 0.06 | 0.06 | 0.06 | - |
| 2 g/L Glu | 8.0 | 0.4 | 0.14 | 0.35 |  | 2 | 0.1 | 0.06 | 0.06 | 0.06 | - |
| 3 g/L Glu | 8.0 | 0.4 | 0.14 | 0.35 |  | 3 | 0.1 | 0.06 | 0.06 | 0.06 | - |
| 1 g/L Glu +BSA | 8.0 | 0.4 | 0.14 | 0.35 |  | 1 | 0.1 | 0.06 | 0.06 | 0.06 | 0.1 |
| 2 g/L Glu +BSA | 8.0 | 0.4 | 0.14 | 0.35 |  | 2 | 0.1 | 0.06 | 0.06 | 0.06 | 0.1 |
| 3 g/L Glu +BSA | 8.0 | 0.4 | 0.14 | 0.35 |  | 3 | 0.1 | 0.06 | 0.06 | 0.06 | 0.1 |

Table S2. Electrochemical parameters of polarization curves.

| Solution | 1 g/L Glu | 2 g/L Glu | 3 g/L Glu | 1 g/L Glu+BSA | 2 g/L Glu+BSA | 3 g/L Glu+BSA |
| --- | --- | --- | --- | --- | --- | --- |
| Ecorr (VSCE) | -1.49 | -1.54 | -1.67 | -1.56 | -1.52 | -1.50 |
| icorr (×10-5 A·cm-2) | 5.69 | 5.81 | 13.58 | 6.87 | 5.94 | 3.94 |

Table S3. Fitting results for EIS spectra of different surfaces.

| Surface | SS | LS | TS |
| --- | --- | --- | --- |
| Rs (Ω·cm2) | 90.60 | 147.50 | 155.5 |
| CPE (Ω-1·sn·cm-2) | 1.40×10-5 | 1.09×10-5 | 7.93×10-5 |
| n1 | 0.73 | 0.69 | 0.69 |
| Rf (Ω·cm2) | 148.30 | 144.2 | 108.70 |
| CPE2 (Ω-1·sn·cm-2) | 1.79×10-5 | 1.36×10-5 | 2.28×10-5 |
| n2 | 0.86 | 0.79 | 0.83 |
| Rct (Ω·cm2) | 3162 | 8375 | 2571 |
| L (H·cm-2) | 2.28×104 | 9.74×105 | 5.54×104 |
| Rl (Ω·cm2) | 1.47×104 | 2.66×104 | 1.89×104 |
| Chi | 1.65×10-3 | 1.28×10-3 | 1.42×10-3 |

Table S4. Fitting results for the EIS spectra in different solutions.

| Solution | 1 g/L Glu | 2 g/L Glu | 3 g/L Glu | 1 g/L Glu +BSA | 2 g/L Glu +BSA | 3 g/L Glu +BSA |
| --- | --- | --- | --- | --- | --- | --- |
| Rs (Ω·cm2) | 90.60 | 92.47 | 87.59 | 74.61 | 98.22 | 100.20 |
| CPE (Ω-1·sn·cm-2) | 1.40×10-5 | 1.28×10-5 | 1.62×10-5 | 8.39×10-6 | 1.11×10-5 | 8.35×10-6 |
| n1 | 0.73 | 0.73 | 0.72 | 0.82 | 0.85 | 0.85 |
| Rf (Ω·cm2) | 148.30 | 141.70 | 155.30 | 36.05 | 136.60 | 119.90 |
| CPE2 (Ω-1·sn·cm-2) | 1.79×10-5 | 1.61×10-5 | 1.64×10-5 | 2.07×10-5 | 9.84×10-6 | 9.59×10-6 |
| n2 | 0.86 | 0.87 | 0.87 | 0.80 | 0.88 | 0.86 |
| Rct (Ω·cm2) | 3162 | 2600 | 1424 | 1901 | 2637 | 3162 |
| L (H·cm-2) | 2.28×104 | 1.06×104 | 7.92×103 | 9.09×103 | 4.52×104 | 2.80×104 |
| Rl (Ω·cm2) | 1.47×104 | 9.30×103 | 9.62×103 | 1.20×104 | 2.26×104 | 1.75×104 |
| Chi | 1.65×10-3 | 1.68×10-3 | 1.42×10-3 | 5.29×10-4 | 7.20×10-4 | 1.03×10-3 |

References

1	Calcagnotto, M. E., Ponge, D., Demir, E. & Raabe, D. Orientation gradients and geometrically necessary dislocations in ultrafine grained dual-phase steels studied by 2D and 3D EBSD. Mater. Sci. Eng. A 527, 2738-2746 (2010).

2	Kubin, L. P. & Mortensen, A. Geometrically necessary dislocations and strain-gradient plasticity: a few critical issues. Scr. Mater. 48, 119–125 (2003).

3	Yan, Z. et al. Deformation behaviors and cyclic strength assessment of AZ31B magnesium alloy based on steady ratcheting effect. Mater. Sci. Eng. A 723, 212-220 (2018).

4	Gao, H., Huang, Y., Nix, W. D. & Hutchinson, J. W. Mechanism-based strain gradient plasticity-I. Theory. J Mech Phys Solids 47, 1239-1263 (1999).