# One-Step Fabrication of a Self-Driven Point-of-Care Device by Femtosecond Laser Direct Writing and Its Application in Cancer Cell H2O2 Detection via Semiconductor-Based SERS

Yue Wang1, Bo Lai2, Zhangrun Xu1,*, and Zhi Yu3,*

1Department of Chemistry, College of Science, Northeastern University, Shenyang 110819, People’s Republic of China

2 MOE Key Laboratory of Advanced Micro-structured Materials, Institute of Precision Optical Engineering (IPOE), Tongji University, Shanghai 200092, People’s Republic of China

3Shenyang National Laboratory for Materials Science, Institute of Metal Research, Chinese Academy of Sciences, Shenyang, 110016, People’s Republic of China

* E-mail: xuzr@mil.neu.edu.cn (Z.X.)

Email: zyu@imr.ac.cn (Z.Y.)

Experimental section

Theoretical method

The geometries of 5-Asa and the oxidation product 5-Asaox were optimized by using B3LYP methods of density functional theory with 6-311++G** basis set. Upon optimization of the molecular geometry, the excited state calculation and the frequency calculation were obtained at the same level. All calculations were carried out by the Gaussian 09 program.1

Additional Supplementary data

Fig. S1. Raman spectra of TiO2/5-Asa, TiO2/5-Asa/HRP, and TiO2/5-Asa/H2O2 systems at 532 nm laser excitation.

Fig. S2. Raman spectra of TiO2/5-Asa/HRP/H2O2 system with the excitations of 532 and 633 nm, respectively.

Fig. S3. (A) Raman spectra of TiO2/5-Asa/HRP/H2O2 systems with different volume ratios of colloidal TiO2 NPs to 5-Asa ranging from 1:5 to 1:12. (B) The plot of the SERS intensities of the band at 1408 cm-1 versus the volume ratio of TiO2 NPs to 5-Asa.

Fig. S4. The MTT-based cytotoxicity assay of TiO2 NPs toward MCF-7 breast cancer cells, the cells were incubated with TiO2 NPs for 24 h.

Table S1. Raman vibrational mode assignment for characteristic bands of azo-Asa in the 5-Asa/HRP/H2O2 and TiO2/5-Asa/HRP/H2O2 systems

| Theoretical wavenumber / cm−1 | Experimental wavenumber /cm−1 |  | Experimental wavenumber /cm−1 with TiO2 | Band assignments |
| --- | --- | --- | --- | --- |
| 405 |  | 395 |  | ρ(CCC), ρ(CCO) |
| 448 | 453 | 453 |  | τ(HOCC) |
| 470 | 470 |  |  | τ(HOCC) |
| 480 | 484 |  |  | ρ(CCO) |
| 735 | 735 | 734 |  | τ(CCCC), ω(OCCC), ω(NCCC) |
| 768 |  | 764 |  | ν(OC), ρ(CCC) |
| 935 |  | 912 |  | ν(CC), ν(OC), |
| 1157 | 1147 | 1141 |  | ν(NC) |
| 1186 | 1184 | 1184 |  | ν(NC) |
| 1236 | 1231 | 1249 |  | ρ(HCC) |
| 1276 | 1282 | 1282 |  | ν(NC), ρ(HCC) |
| 1338 | 1337 |  |  | ν(CC), ρ(HCC) |
| 1382 | 1384 | 1371 |  | ν(CC), ρ(HOC) |
| 1401 | 1418 | 1408 |  | ν(NN) |
| 1527 |  | 1534 |  | ν(CC) |
| 1605 | 1598 | 1581 |  | ν(CC), ρ(CCC) |

θ—stretching vibration, ρ—in-plane bending vibration, ω—out of plane bending vibration, τ—torsion.

References

1. M.J. Frisch, G.W. Trucks, H.B. Schlegel, G.E. Scuseria, M.A. Robb, J.R. Cheeseman, G. Scalmani, V. Barone, G.A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A.V. Marenich, J. Bloino, B.G. Janesko, R. Gomperts, B. Mennucci, H.P. Hratchian, J.V. Ortiz, A.F. Izmaylov, J.L. Sonnenberg, Williams, F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone, T. Henderson, D. Ranasinghe, V.G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J.A. Montgomery Jr., J.E. Peralta, F. Ogliaro, M.J. Bearpark, J.J. Heyd, E. N. Brothers, K.N. Kudin, V.N. Staroverov, T.A. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A.P. Rendell, J.C. Burant, S.S. Iyengar, J. Tomasi, M. Cossi, J.M. Millam, M. Klene, C. Adamo, R. Cammi, J.W. Ochterski, R.L. Martin, K. Morokuma, O. Farkas, J.B. Foresman, D.J. Fox, Gaussian 09 Rev. D.01, in, Wallingford, CT, 2013.