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Table 1. Fabricated epoxy molded electrodes.
Table 2. Required times for breakdown per 1mm.


[bookmark: _Hlk142343635]Table 1. Fabricated epoxy molded electrodes.
[image: ]






[bookmark: _Hlk142312043]Table 2. Required times for breakdown per 1mm.[image: ]













image1.emf
No.

Filler

[%]

Void φ

[mm]

T

i

[mm]

E

vmax

[kV/mm]

1

60 1.0

0.76 18.2

2 0.43 21.5

3 0.36 22.3

4 0.34 22.6

5 0.26 23.6
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Filler

[%]

Void φ

[mm]

E

vmax

[kV/mm]

Time for 

breakdown 

per 1mm, T

f60

[min]

60 1.0

18.2 3571.0

21.5 5237.0

22.3 1575.0

22.6 1844.0

23.6 2981.0


