List of Tables

Table 1

| Model | fitting equation | Rate constant kd (g/g.min) | Rate constant ka (min−1) | correlation coefficient Rd2 | correlation coefficient Ra2 |
| --- | --- | --- | --- | --- | --- |
| pseudo-second-order model (diffusion process) ln⁡(qe- qt) = lnqe- kat | [t/qt = −0.0033 + 0.0288t] | 0.23 | - | 0.996 | - |
| pseudo-first-order model (absorption process) tqt= 1kd qe2+tqe | [qt = 26.29 (1- e−20.61t)] | - | 21.83 |  | 0.998 |

Table 2

| Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- |
| qm (mg.g-1) | kl | R2 | kf | n | R2 |
| 94.87 | 0.169 | 0.988 | 39.17 | 2.107 | 0.996 |

Table 3

| Drug sample | fitting equation | rate constant kd (min-1) | correlation coefficient Rd2 |
| --- | --- | --- | --- |
| TCL | y = 0.979(1 - e−0.039t) | 0.039 | 0.987 |