Supporting Information

Free Radical Assisted Photocatalytic Degradation of Antibiotics in aqueous medium: Kinetics, Transformation Products, and Toxicity Assessment

A. Patidar, V.R. Dugyala, S. Chakma, M.N. Galodiya and A. S. Giri *

Indian Institute of Science Education and Research, Bhopal Bhauri, Bhopal-462066, INDIA

*Email: drasg82@gmail.com

Fig. S1 Effect of pH on removal of TCL in photocatalytic process. Experimental conditions: [TCL]0 = 100 mg/L, AC/TiO2 NC = 1.25 g/L and temperature = 25°C. Photo-reaction with an UV lamp of 15W.

Fig. S2 Effect of catalyst dose on removal of TCL in photocatalytic process. Experimental conditions: [TCL]0 = 100 mg/L, pH = 6.5 and temperature = 25°C. Photo-reaction with an UV lamp of 15W.

Fig. S3 Effect of UV-light irradiation on removal of TCL in photocatalytic process. Experimental conditions: [TCL]0 = 100 mg/L, pH = 6.5, AC/TiO2 NC = 1.25 g/L and temperature = 25°C.

Fig. S4 Zeta Potential curve of the AC/TiO2 Composite

Fig. S5 Mass spectra of TCL drug in aqueous solution after at 45 min photoreaction with an UV lamp of 15W. Experimental conditions: [TCL]0 = 100 mg/L, AC/TiO2 NC = 1.25 g/L, pH = 6.5, reaction time = 45 min and temperature = 25°C.

Table S1 Proposed intermediate products of TCL

| Molecule | m/z (Exact) | Mol. formula | Proposed structure | Mass error (g/mol) (Exact-proposed) | DBE¥ |
| --- | --- | --- | --- | --- | --- |
| TCL | 444.43 | C22H24N2O8 |  | 0.04 | 12 |
| D1 | 411.12 | C23H25O6 |  | 0.11 | 11 |
| D2 | 363.11 | C19H15O8 |  | 0.10 | 11 |
| D3 | 301.08 | C17H16O7 |  | -0.18 | 09 |
| D4 | 227.13 | C15H14O5 |  | 0.07 | 08 |
| D5 | 289.30 | C13H16O6 |  | 0.19 | 07 |
| D6 | 433.09 | C21H22O9N |  | 0.03 | 11 |
| D7 | 430.19 | C20H24O9N |  | -0.10 | 09 |
| D8 | 363.11 | C17H19O5 |  | 0.09 | 08 |
| D9 | 399.08 | C17H22O7 |  | -0.08 | 07 |
| D10 | 122.11 | C3H8O4 |  | -0.45 | 00 |
| D11 | 328.03 | C12H12O5 |  | 0.03 | 07 |
| D12 | 289.12 | C10H8O4 |  | 0.87 | 07 |
| D13 | 289.12 | C9H8O6 |  | -0.13 | 05 |
| D14 | 183.09 | C6H6O3 |  | -0.04 | 03 |

¥: Double bond equivalent: It is the summations of total number of pi bonds (π) and the residual ring(s). It signifies the degree of unsaturation of degraded products.