Table 1 | Optimization of catalytic depolymerizationa

| Entry | 2a (equiv.) | Catalyst | Solvent | Temp. (ºC) | 3 (%) | 4a (%) | 5 (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2 | KOH | DMI | 150 | 17 | 41 | 41 |
| 2 | 2 | K3PO4 | DMI | 150 | 12 | 54 | 56 |
| 3 | 2 | KOtBu | DMI | 150 | 12 | 62 | 62 |
| 4 | 2 | Cs2CO3 | DMI | 150 | 13 | 67 | 67 |
| 5 | 2 | DBU | DMI | 150 | 10 | 3 | 3 |
| 6 | 2 | P1-tBu-TP | DMI | 150 | 7 | 2 | 1 |
| 7 | 2 | P2-tBu | DMI | 150 | 14 | 61 | 66 |
| 8 | 2 | P4-tBu | DMI | 150 | 16 | 67 | 72 |
| 9 | 2.5 | P4-tBu | DMI | 150 | 7 | 74 | 73 |
| 10 | 2.5 | P4-tBu (5 mol%) | DMI | 150 | 12 | 58 | 58 |
| 11 | 2.5 | P4-tBu | DMI | 120 | 11 | 50 | 45 |
| 12 | 2.5 | P4-tBu | DMI | 100 | 12 | 37 | 31 |
| 13 | 2.5 | P4-tBu | PhCN | 150 | 28 | 32 | 12 |
| 14 | 2.5 | P4-tBu | Xylene | 150 | 19 | 11 | 2 |
| 15 | 2.5 | P4-tBu | DMAc | 150 | - | 95 | 84 |
| 16 | 2.5 | P4-tBu + K3PO4 (5 mol%) | DMAc | 150 | - | >99 (85) | >99 (61) |

a A mixture of 1 (powder, 0.1 mmol relative to the molecular weight of the monomer), thiol (0.2 mmol for entries 1-8, 0.25 mmol for entries 9-16), catalyst (0.01 mmol), and solvent (0.2 mL) was stirred for 16 h. Yields were determined by 1H NMR. Numbers in parentheses are isolated yields.

Table 2 | Scope or catalytic depolymerization of super engineering plasticsa

| Entry | Polymer | Productsb |
| --- | --- | --- |
| 1 | PSU, pellet (Mw 35000, Mn 16000) (6) | 7a, 89% 8, 94% |
| 2 | PSU, pellet (Mw 60000) (6’) | 7a, 99% 8, >99% |
| 3 | PEES, pellet (-) (9) | 7a, >99% 5, 80% |
| 4 | PPSU, powder (-) (10) | 7a, 95% 11, >99% |
| 5b | PESU, pellet (-) (12) | 7a, 22% 13, 21% 14, 13% |
| 6 | PEI, pellet (-) (15) | 16, 75% 8, >99% |

a A mixture of polymer (0.1 mmol relative to the molecular weight of the monomer), thiol (0.25 mmol), P4-tBu (0.01 mmol), K3PO4 (0.005 mmol) and DMAc (0.2 mL) was stirred for 16 h at 150 ºC. Isolated yields are shown. b 4-((4-(4-((4-((2-Ethylhexyl)thio)phenyl)- sulfonyl)phenoxy)phenyl)sulfonyl)phenol was obtained in 15% yield.