Supplementary:

Eco-friendly and cost-effective adsorbent derived from blast furnace slag with black liquor waste for hazardous remediation

Ahmed H. Naggar1*, Abdelghaffar Dhmees2, Tarek A. Seaf-Elnasr3, Kwok F. Chong4,

Gomaa A.M. Ali5, Hazim M. Ali3, Rasmih M. Kh. Alshamery3, Lubna H. M. AlNahwa3,

Al-Sayed A. Bakr2**

1 Department of Chemistry, College of Science and Arts, Jouf University, Al-Qurayyat, Saudi Arabia

2 Department of Analysis and Evaluation, Egyptian Petroleum Research Institute (EPRI), Nasr city, Cairo 11727, Egypt

3 Department of Chemistry, College of Science, Jouf University, Sakaka, Saudi Arabia

4 Faculty of Industrial Sciences and Technology, Universiti Malaysia Pahang, Gambang, 26300 Kuantan, Malaysia

5 Department of Chemistry, Faculty of Science, Al-Azhar University, Assiut 71524, Egypt

* Corresponding author email: ahayoub@ju.edu.sa

** Corresponding author email: als_water@yahoo.com

Table S1: Chemical composition of BFS

| Composition | SiO2 | CaO | Al2O3 | MgO | MnO2 | SO3 | Fe-oxides |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Wt. (%) | 33.35 | 40.54 | 11.51 | 5.05 | 6.30 | 2.75 | 0.5 |

Table S2: The XPS analysis of SBL and Th/SBL

| Name |  | SBL |  |  |  | Th/SBL |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Peak BE | Atomic % |  |  | Peak BE | Atomic % |
| C 1s |  | 287.22 | 5.43 |  |  | 290.35 | 13.20 |
| O 1s |  | 534.20 | 59.78 |  |  | 536.68 | 59.45 |
| Si 2p |  | 105.13 | 27.98 |  |  | 109.14 | 18.38 |
| Na 1a |  | 1073.32 | 5.84 |  |  | 1075.17 | 4.40 |
| Cl 2p |  | 200.45 | 0.97 |  |  | 200.45 | 0.51 |
| Th 4f |  | ……… | ……… |  |  | 339.86 | 4.06 |

Table S3: Sorption modeling of kinetics sorption

| Model | Equation | Parameters |
| --- | --- | --- |
| sPFOLE | logqe-qt=logqe-k1t2.303 | qe = the amount of Th(IV) ions adsorbed at equilibrium (mg/g), qt = the amount of Th(IV) ions adsorbed at time t, (mg/g), t = contact time (min), k1 = kinetic rate constants for pseudo-first-order (min–1), k2 = kinetic rate constants for pseudo-second-order (L/mg min), kint = rate constants for intra-particle diffusion kinetic (mg/g min0.5), C = the intercept, which indicates the thickness of the boundary layer |
| sPSOLE | tqt=1k2qe2+tqe |  |
| sIPDE (Weber & Morris) | qt=kintt0.5+C |  |

Table S4: Linearized sorption isotherms modeling

| Model | Equation | Parameters |
| --- | --- | --- |
| Langmuir | Ceqe=qeqmax+1bqmax | qe = amount of Th(IV) ions adsorbed at equilibrium (mg/g), Ce = equilibrium concentration of Th(IV) (mg/L), qmax = saturated monolayer adsorption (mg/g), b = the Langmuir constant (mL/mg), kF = the adsorption capacity (mg/g), n = Freundlich constant indicating adsorption intensity, KT = Temkin isotherm equilibrium binding constant (L/g), R = gas constant (8.314 J/mol K), bT = Temkin isotherm constant, AT = constant related to the sorption binding heat (J/mol) T = temperature (K) |
| Freundlish | logqe=logkF+1nlogCe |  |
| Temkin | qe=RTbTlnCe+RTbTlnKT AT=RTbT |  |

Table S5: Th(IV) desorption and sorption relative efficiencies for reusability and recycling

| Cycle no. |  | Desorption, (%) |  | Reusability, (%) |
| --- | --- | --- | --- | --- |
| 1 |  | 96.04 |  | 100* |
| 2 |  | 93.14 |  | 94.68 |
| 3 |  | 91.57 |  | 92.86 |
| 4 |  | 87.34 |  | 88.13 |
| 5 |  | 81.43 |  | 82.46 |

* Reference value for Th(IV) sorption efficiency (at 1st cycle).

Fig. S1: Mes-Si-NP manufacturing from sugarcane bagasse

Fig. S2: Thermodynamics of Th(IV) sorption using lnKd vs. 1/T relation

Fig. S3:  The relative proportion of Th(IV) at different pH values