Supplementary Information

Contact-electro-catalytic CO2 reduction from ambient air

Nannan Wang1‡, Wenbin Jiang2‡, Jing Yang3, Sheng Wang1, Bofan Li1, Jerry Zhi Xiong Heng1, Wai Chung Ong1, Hui Ru TAN2, Yong-Wei Zhang3, Daoai Wang5,6,*, Enyi Ye2*, Zibiao Li1,2,4,*

1 Institute of Sustainability for Chemicals, Energy and Environment (ISCE2), Agency for Science, Technology and Research (A*STAR), 1 Pesek Road, Jurong Island, Singapore 627833, Republic of Singapore;

2 Institute of Materials Research and Engineering (IMRE), Agency for Science, Technology and Research (A*STAR), 2 Fusionopolis Way, Innovis #08-03, Singapore 138634, Republic of Singapore;

3 Institute of High Performance Computing (IHPC), Agency for Science, Technology and Research (A*STAR), 1 Fusionopolis Way, #16-16 Connexis, Singapore 138632, Republic of Singapore;

4 Department of Materials Science and Engineering, National University of Singapore, 9 Engineering Drive 1, Singapore 117576, Singapore;

5 State Key Laboratory of Solid Lubrication, Lanzhou Institute of Chemical Physics, Chinese Academy of Sciences, Lanzhou 730000, China;

6 Shandong Laboratory of Yantai Advanced Materials and Green Manufacturing, Yantai 265503, China.

‡ These authors contributed equally.

*Correspondence and requests for materials should be addressed to Z. L. (E-mail: lizb@imre.a-star.edu.sg), E.Y. (E-mail: yeey@imre.a-star.efu.sg) and D. W. (E-mail: wangda@licp.cas.cn)

Sample characterization

Electrical output test of TENG. The output voltage was measured by using NI PCIe-6259 DAQ card (National Instruments) with a load resistance of 100 MΩ, while the short-circuit current (Isc) was measured by using an SR570 low-noise current amplifier (Stanford Research System). During the electrical output test of the TENGs, an impact force of 5 N was maintained, and the frequency was 5 Hz. In order to prevent the possible influence of copper wires on CO2RR, all wire clips were sealed.

Infrared spectroscopy test of quaternized CNF film under different humidity. Fourier transform infrared spectroscopy (FTIR) spectra of CNF films were recorded on an FTIR spectrometer (Nicolet 6700, Themo Fisher Scientific Inc) from 4000 to 400 cm-1 at a resolution of 4 cm-1 with the temperature of 100 ℃ to ensure the free water evaporated from the surface of the quaternized CNF film.

Henry’s CO2/N2 selectivity. CO2 adsorption/desorption measurement were performed on a TG-MS analyzer (TA Q600- HIDEN HPR 20). Before measurement, the sample was activated by heating at 200 ℃ for 2 h under an Ar steam. After the furnace temperature was cooled and stabilized at 35 ℃, the gas was switched to the 50% CO2 and 50% N2 (volume percentage) mixture gas for adsorption. After 2 h, the temperature then was increased to 200 ℃ with a rate of 20 ℃ /min under an Ar steam and kept for 2 h for desorption. CO2/N2 selectivity was determined according to the ratio of the integral area of CO2 to that of N2, recorded by MS.

Thermogravimetric analyses. Thermogravimetric analyses (TGA) were carried out with a TA Q5000 (V3.15 Build 263) thermogravimetric analyzer. The test was carried out under a nitrogen atmosphere, and the temperature was raised from 40°C to 600°C at a rate of 10°C/min.

Fig. S1 (a) Schematic diagram of the preparation process of quaternized CNF. (b) Physical photo of quaternized CNF film. (c) SEM and TEM of quaternized CNF.

Synthesis of quaternized CNF film. The procedure for synthesizing quaternized CNF was conducted based on the previous study1, with slight modifications introduced. 30 g of aqueous CNF suspension was centrifuged and the water supernatant was removed. Then, 30 ml of acetone was added and the mixture was vortexed and centrifuged again to remove the acetone and residual water. The resulting solid CNF pellet was then dispersed in 100 ml DMSO and added to a round bottom flask. 1 g TBAH was added to the vessel and the contents were degassed under N2 for 30 min. Then, 2.49 ml GTMAC was injected into the vessel and the temperature was increased to 65 ◦C. The product redispersed in water was centrifuged and the DMSO supernatant was removed. Then, 30 ml of acetone was added and the mixture was vortexed and centrifuged again to remove acetone and residual DMSO. The purified quaternized CNF pellet was then redispersed in water. The quaternized CNF film was obtained by suction filtration on a PVDF filter film with a pore size of 0.5 μm. The preparation process of quaternized CNF is shown in Fig. S1a, and the photo of the quaternized CNF film is shown in Fig. S1b. The SEM and TEM images of quaternized CNF is shown in Fig. S1c.

Fig. S2 Schematic diagram of specific reaction process of CO2 on the electrode surface of TENG.

Fig. S3 (a) Schematic diagram of the preparation process of Cu-PCN. (b) Physical photo of Cu-PCN powder.

Synthesis of Cu-anchored polymeric carbon nitride (Cu-PCN). Cu-PCN samples were prepared by modifying our previously reported method.2 In the standard process, urea (30 g) was dissolved in hot water (7 mL, 95 °C) under continuous magnetic stirring. An aqueous solution of CuCl2 (1 mL, 0.1 M) was then added to the mixture to obtain a transparent solution. After being kept at 95 °C for 5 min under continuous stirring, the solution was immediately cooled down using an ice-water bath, leading to the formation of solid crystals. The resulting crystals was dried in an oven at 70 °C for 12 h, ground into powder and dried further at 100 °C for 2 h. Subsequently, it was calcined at 550 °C for 4 h (with a heating rate 5 °C/min) in a muffle furnace. The obtained pale-yellow Cu-PCN powder with a Cu loading of 0.53 wt.% (weight percentage) was collected for further use. The Cu loading in the sample can be easily adjusted by using CuCl2 precursor solutions with different concentrations, including 0.25 M (0.13 wt.%), 0.5 M (0.26 wt.%) and 2.0 M (1.06 wt.%). Pure PCN samples were prepared by the direct polymerization of urea at 550 °C for 4 h (with a heating rate 5 °C/min) in a muffle furnace. The yield for all the polymerization processes was approximately 4 wt.%.

Fig. S4 (a) Physical photo of Cu-PCN@PVDF electrospun membrane. (b) TEM image of reunited Cu-PCN and reunited Cu-PCN@PVDF electrospinning solution.

Fig. S5 (a) TEM photo of Cu-PCN@PVDF. (b) Carbon element, (c) fluorine element, (d) nitrogen element and (e) copper element. (f) EDS of Cu-PCN@PVDF.

Fig. S6 Fourier-transformed magnitudes of the k3-weighted Cu K-edge EXAFS spectra from Cu-PCN and the corresponding fitting analysis.

EXAFS fitting parameters. The obtained XAFS data was processed in Athena (version 0.9.26) for background, pre-edge line and post-edge line calibrations. Then Fourier transformed fitting was carried out in Artemis (version 0.9.26). The k3 weighting, k-range of 3 - 12 Å-1 and R range of 1 - 3 Å were used for the fitting of foil; k-range of 2 - 11 Å-1 and R range of 1 - 3 Å were used for the fitting of sample. The four parameters, coordination number, bond length, Debye-Waller factor and E0 shift (CN, R, σ2, ΔE0) were fitted without anyone was fixed, constrained, or correlated.

Fig. S7 (a) Current output of quaternized CNF-Cu-PCN@PVDF-based TENG under different humidity. (b) 100°C-IR spectra of quaternized CNF film at 15%RH and 95%RH.

Moisture resistance performance and mechanism. High humidity severely degrades the electrical output performance of conventional polymer-based TENGs. However, for the quaternized CNF based TENG, the electrical output increases with the increase of humidity, because the hydroxyl groups in the CNF can form hydrogen bonds with the water molecules in the high-humidity environment, so that the water molecules participate in the triboelectrification together.3 When the humidity is increased from 15% RH to 95%RH, the current of quaternized CNF based TENG increases from 2.9 μA to 18.6 μA (Fig.S7a), showing an enhanced electrical output property under high humidity. In order to determine the mechanism during this process, IR spectra of quaternized CNF films after water absorption at different humidity were tested. The results show that the -OH absorption peak of quaternized CNF film that stay in 95% RH shift from 3339.1 cm-1 to 3348.1 cm-1 compared with the film that was in 15% RH (Fig.S7b).4

Fig. S8 (a) Current and (b) voltage comparison of Pure CNF-Cu-PCN@PVDF based and quaternized CNF-Cu-PCN@PVDF based TENG. (c) Current and (d) voltage comparison of quaternized CNF-Cu-PCN@PVDF fiber-based and quaternized CNF-Cu-PCN@PVDF membrane-based TENG.

The quaternized CNF-based TENG displays better electrical output performance than the pure CNF-based TENG because the quaternized CNF contains positive charges5, as shown in Fig.S8a and 8b. Pure CNF-PVDF fiber based TENG's output current and voltage are 4.1 μA and 84 V, respectively. The quaternized CNF-based TENG's output current and voltage were 10.4 μA and 227 V, respectively, showing that the presence of positive charges in the quaternary ammonium salt increases the TENG's electrical output. Additionally, for electronegative PVDF, films and electrospun fibers also significantly affect the electrical output of TENG. The electrical output of the quaternized CNF-PVDF film based TENG is 6.8 μA and 143 V, whereas that of the quaternized CNF-PVDF fiber based TENG is 10.4 μA and 227 V (Fig. S8c and 8d).

Fig. S9 TGA comparison of pure CNF and quaternized CNF films.

Fig. S10 (a) Spectra of CO2 (MS:44) and N2 (MS:28) collected by MS within 130 min. (b) Henry’s law CO2/N2 selectivity.

Fig. S11 Real-time current output of quaternized CNF-Cu-PCN@PVDF based TENG under Ar environment.

Table S1 EXAFS fitting parameters at the Cu K-edge (Ѕ02=0.88)

| Sample | Path | C.N. | R (Å) | σ2×103 (Å2) | ΔE (eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Cu foil | Cu-Cu | 12* | 2.54±0.01 | 8.1±2.9 | 4.0±0.6 | 0.002 |
| Cu | Cu-N | 5.4±1.8 | 1.95±0.02 | 4.7±3.0 | 2.6±4.1 | 0.018 |

C.N.: coordination numbers; R: bond distance; σ2: Debye-Waller factors; ΔE: the inner potential correction. R factor: goodness of fit. * Fitting with fixed parameter.

Table S2 Quaternized CNF-Cu-PCN@PVDF based TENG catalyzes CO2RR in CO2/Ar mixed gas with 20% CO2 content.

| Sample | Injection volume/mL | Container volume/L | Catalyst weight/mg | Q /mC | Time /h | Production rate/nmolh-1 | EFco | Peak area | Yield /nmol |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Standard | 0.25 |  |  |  |  |  |  | 426.26 | 2.23 |
| TENG | 1 | 5 | 0.68 | 31.5 | 5 | 31.42 | 96.24% | 6 | 157.1 |

The calculation formula of Faraday efficiency is as follows:

FECO=2n×FQ×100%

Where FECO is CO Faraday efficiency; n is CO production (mol); F is Faraday constant (F=96485 C/mol); Q is transferred charge (C).

Table S3 Quaternized CNF-Cu-PCN@PVDF based TENG catalyzes CO2RR in air.

| Sample | Injection volume/mL | Container volume/L | Catalyst weight/mg | Q /mC | Time /h | Production rate/nmolh-1 | EFco | Peak area | Yield /nmol |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Standard | 0.25 |  |  |  |  |  |  | 426.26 | 2.23 |
| TENG | 1 | 5 | 0.68 | 48.4 | 10.5 | 22.44 | 93.95% | 9 | 235.6 |

Calculation of CO yield. In the fabrication process of the quaternized CNF-Cu-PCN@PVDF based TENG, a precise amount of 7 mg of Cu-PCN was blended with 0.7 g of PVDF to facilitate the subsequent electrospinning procedure. The dimensions of the aluminum foil membrane, which acted as the substrate for electrospinning, were measured at "11 cm × 15 cm". Subsequently, a section of the electrospun membrane, measuring "4 cm × 4 cm", was excised to serve as the electronegative friction layer within the TENG assembly. As a result of these preparations, the calculated weight of the Cu-PCN material amounted to 0.68 mg. As shown in Table S3, the CO production rate in the air is 22.44 nmolh-1, so the yield of CO is 33 μmolg-1h-1.

References

1	Quinlan, P. J., Tanvir, A. & Tam, K. C. Application of the central composite design to study the flocculation of an anionic azo dye using quaternized cellulose nanofibrils. Carbohydr. Polym. 133, 80-89, (2015).

2	Jiang, W. et al. Integration of single‐atom catalyst with Z‐scheme heterojunction for cascade charge transfer enabling highly efficient piezo‐photocatalysis. Adv. Sci., 2303448 (2023).

3	Sun, W. et al. Humidity-resistant triboelectric nanogenerator and its applications in wind energy harvesting and self-powered cathodic protection. Electrochim. Acta 391, 138994 (2021).

4	Wang, N. et al. New hydrogen bonding enhanced polyvinyl alcohol based self‐charged medical mask with superior charge retention and moisture resistance performances. Adv. Funct. Mater. 31, 2009172 (2021).

5	Rana, S. S. et al. Cation functionalized nylon composite nanofibrous mat as a highly positive friction layer for robust, high output triboelectric nanogenerators and self-powered sensors. Nano Energy 88, 106300 (2021).