Supplementary Information

Heterojunction interface engineering for stable and effective porous Fe3O4-ZnO nanocomposites: A highly efficient synergistic Catalyst for oxygen evolution reaction

Aniruddha Mondal1*, Mohd Afzal2 Sudip Mondal3*

1Department of Chemical Engineering and Biotechnology, Tatung University, No. 40, Sec. 3, Chungshan North Rd., Taipei City 104, Taiwan

2Department of Chemistry, College of Science, King Saud University, Riyadh 11451, Saudi Arabia.

3Post Graduate Department of Chemistry, Seth Kesarimal Porwal College of Arts, Science and Commerce, Kamptee 441001, Maharashtra, India

Email: aniruddhacsmcri@gmail.com , sudipmondal5555@gmail.com

Figure S1: (a) Raman and (b) FTIR spectra of the synthesized materials

Figure S2: Survery Spectrum of the synthesized material Fe3O4-ZnO

Figure S3: EDX spectra of the synthesized material

Figure S4: Overpotenital values at different current density of the synthesized materials

Figure S5: (a-c) Cyclic voltammetry at non faradaic zone and (d-f) capacitive properties of the synthesized materials

Electrochemically active surface areas (ECSA) is directly proportional to the electrochemical double layer capacitance (Cdl). Electrochemical cyclic voltammograms from 1.1V to 1.3V along with multiple scan rates (10, 20, 30, 40, 50 and 60 mV/sec) in the non-faradic regions utilized to measure the Cdl and formulae used to calculate the corresponding ECSA as follows:

AECSA=Capacitance Double layer (Cdl)0.040 mF/ cm2(Cs)  per cm2

Fe3O4-A_ECSA= 92 cm2

ZnO-A_ECSA= 45 cm2

Fe3O4-ZnO-A_ECSA= 115 cm2

It was assumed that the specific capacitance of flat standard surface with 1 cm2 of real surface which was assume the value around 40 μF/ cm2 (J. Am. Chem. Soc. 2015, 137, 4347−4357). The calculated values of the corresponding samples (Fe3O4, ZnO and Fe3O4-ZnO) are given in Table 1

Roughness factor (Rf) Calculation:

The following formulae has been used to calculate the Roughness factor (Rf)

Fe3O4-Rf = 55

ZnO-Rf = 30

Fe3O4-ZnO-Rf = 93