Supplementary Materials for

# Ultrastrong exciton-plasmon couplings in WS2 multilayers synthesized with a random multi-singular metasurface at room temperature

Tingting Wu1,#, Chongwu Wang1,#, Guangwei Hu1,#, Zhixun Wang1, Jiaxin Zhao2, Zhe Wang1, Ksenia Chaykun2, Lin Liu1, Mengxiao Chen3, Dong Li4, Qihua Xiong5, Zexiang Shen2, Huajian Gao4, Francisco J. Garcia-Vidal6,7,*, Lei Wei1,*, Qi Jie Wang1,2,* and Yu Luo1,*

1School of Electrical and Electronic Engineering, Nanyang Technological University, Singapore, Singapore.

2School of Physical and Mathematical Sciences, Nanyang Technological University, Singapore, Singapore.

3Zhejiang Provincial Key Laboratory of Cardio-Cerebral Vascular Detection Technology and Medicinal Effectiveness Appraisal, Zhejiang University, Hangzhou, China

4School of Mechanical and Aerospace Engineering, Nanyang Technological University, Singapore, Singapore.

5State Key Laboratory of Low-Dimensional Quantum Physics and Department of Physics, Tsinghua University, Beijing, China.

6Departamento de Física Teorica de la Materia Condensada and Condensed Matter Physics Center (IFIMAC), Universidad Autónoma de Madrid, 28049 Madrid, Spain

7Institute of High Performance Computing, Agency for Science, Technology and Research (A*STAR), Connexis, 138632, Singapore

#These authors contributed equally: Tingting Wu, Chongwu Wang, Guangwei Hu.

*emails: fj.garcia@uam.es; wei.lei@ntu.edu.sg; qjwang@ntu.edu.sg; luoyu@ntu.edu.sg

## Dense packing of sub-nanometer plasmonic gaps by cold-etching technique

Two main paths are identified to achieve sub-nanometer gaps. The first is to apply a stress to the PEI substrate that exceeds the critical value (to ensure the onset of the fracture across the metal strip/domain at width Lc) while approaching saturation (where the fracture across the metal strip/domain stops as the stress transferred from the PEI substrate is insufficient to further break the existing fragment strip/domain at width Ls<Lc) by selecting appropriate mechanical loadings1. The critical stress applied to the PEI substrate to break the fragment strip/domain with thickness of h, width of L (perpendicular to the loading direction), and fracture strength of σ* (which is a constant or varies slightly with the thickness of the metal film) is σc=2hσ*L, showing that a narrower strip/domain requires a greater applied stress to break under the condition of fixed thickness. Thus, an appropriate mechanical loading can generate a new crack near the centre of a preformed strip/domain, while the stress transferred from the PEI substrate has an opportunity to saturate somewhere in the narrow region of the strip/domain, and the corresponding crack does not extend too far and stops before the narrow region completely breaks into two parts, resulting in a sub-nanometer fracture gap in the preformed strip/domain (Fig. S3). It should be noted that the strip/domain is not uniform in width (wider at some random locations and narrower at others due to the intergranular fracture), and the tensile stress is maximum at the centre of the strip/domain under mechanical loadings, which are the reasons why the newly generated crack starts from the centre of the wide part of the strip/domain. The second path is to use biaxial intergranular fractures to create sub-nanometer distances between adjacent fragment domains, where the deflected crack edges of one fragment domain are dragged close to the crack edges of the adjacent fragment at sub-nanometer spacings (Fig. S4).

In order to elucidate the mechanism of the packing of sub-nanometer plasmonic gaps in the cold-etched plasmonic metasurfaces, the fracture morphology and the stress-strain relationship were characterized in detail from a geometrical point of view. The strain-stress behaviour of the gold-amorphous PEI polymers with different gold film thicknesses is shown in Fig. S5a. In the x-directional stretching (Fig. S5a), the necking process is located in the middle strain range with constant stress, and the strain is localized in this region. The advantage of necking in plastic polymers is that, compared to elastic polymers (without the necking process), the fragmenting of metal films can be well controlled with roughly homogeneous fracture strips2. The zigzag crack deflection angles (from the mechanical loading direction) were between 55° and 65° (Fig. S6), analogous to the crack deflection angles for mixed local thinning and intergranular fracture3. The strain-stress curve during the y-directional (2nd) stretching (Fig. S5b) behaves as in elastic polymers, where the stress in the polymer increases with increasing strain without necking because the polymer chains are already well aligned during necking, and the plastic polymer film (plastic refers to the irreversible deformation of the polymer when the tensile force is released) stretches homogeneously over the entire length.

The packing density of the sub-nanometer plasmonic gaps in the gold film under tension is expected to be determined by the mechanical properties of the plastic polymer used for cold-etching (Fig. S5), the thickness of the deposited gold film, and the fracture strain of the gold film/polymer sample. The SEM images of the fracture morphology clearly show the packing of sub-nanometer plasmonic gaps.

## Geometrical and optical isotropy

We have investigated the isotropic/anisotropic properties of the WS2 monolayer coupled multi-singular metasurface system from geometrical and optical perspectives, by exploring the fracture morphology and the corresponding polarization dependence of the PL emission and the coupling strength (between the WS2 excitons and plasmons). Geometrical isotropy/anisotropy refers to the average fragment domain size in different directions, which depends on the elongation extents of the biaxial stretching. Anisotropy here means that the average fragment domain size is different in one direction than in the other. When the elongation is 0%, the gold film breaks into approximately uniform strips with the greatest geometrical anisotropy (Fig. S7d). The geometrical anisotropy decreases and becomes isotropy at about 80% of elongation (Fig. S7a-c) as it increases from 0% to 80%, and the opposite geometrical anisotropy appears above 80% (Fig. S7e,f). It should be noted that the cracks under mechanical loading are along random grain boundaries of the gold film, so only two perpendicular mechanical loadings can produce isotropic cold-etched metallic metasurfaces. The polarization-resolved coupling strength (Fig. S11) confirms the isotropic/anisotropic optical properties. The coupling strength between WS2 excitons and plasmons was fitted by the full Hopfield Hamiltonian. The isotropic and anisotropic behaviour of the coupling strength is in good agreement with the geometrical perspective (Fig. S7), i.e., for metasurfaces with different gold film thicknesses, the coupling strength is isotropic at 80% y-directional elongation, for the 20 nm thick metasurface case, the maximum anisotropy occurs at 0% y-directional elongation, and the opposite anisotropy occurs at 100% y-directional elongation. Thus, there is a one-to-one correspondence between optical isotropy/anisotropy and geometrical isotropy/anisotropy. Among the geometrically isotropic metasurfaces, the metasurface with a 20 nm thick gold film has the best coupling. This best performance is provided by the smallest plasmonic mode volume of the 20 nm thick gold isotropic metasurface due to its dense sub-nanometer plasmonic gaps and a certain thickness of the gold film.

Our results show that cold-etching is effective in modifying the in-plane fracture behaviour (i.e., in-plane crack extension) of metal thin films by controlling the packing of the sub-nanometer plasmonic gaps of the plasmonic metasurfaces, and the corresponding isotropic/anisotropic properties. The cold-etched metasurface has a unique ease of manufacture and a high degree of tunability.

## WS2 coupled antennas fabrication

The bowtie and dimer antennas were fabricated using the electron beam lithography (EBL) lift-off process. EBL patterning was achieved by a series of line exposures at 30 kV energy and 15 pA beam current on 80 nm-thick PMMA e-beam resist, followed by cold development in a mixture of MIBK and isopropyl alcohol. A 20 nm-thick gold film was then deposited on the sample using an e-beam evaporator, and the lift-off pattern transfer was performed in acetone for 10 min. WS2 monolayers were transferred to the antennas using a dry transfer method.

Fig. S1| Schematic illustration of the fabrication process of the WS2 monolayer coupled multi-singular plasmonic metasurface. A thin gold film was deposited on a PEI polymer substrate (125 μm thick, smooth on both sides) using an electron beam evaporator at a deposition rate of 2 Ås-1. During the evaporation, the temperature of the vacuum chamber was kept below 60 °C throughout the whole process, to prevent the thermal expansion or deformation of the PEI film due to built-in stress, which would cause wrinkles or defects in the gold film. For cold-etching, the first stretch was conducted by stretching the gold/PEI film in the x-direction. The second 2D stretch was conducted by re-stretching the as-fabricated film in the y-direction. After the cold-etching, the resulting gold nanopattern was transferred to a flexible TPU polymer substrate (2 mm thick) using a dry peel-off method. WS2 monolayers were mechanically exfoliated from the purchased commercial bulk WS2 crystals using a PDMS tape and transferred to the gold nanopatterns (on TPU) using a dry transfer method (optical microscopy images of the plasmonic system are shown in Fig. S2).

Fig. S2| Optical microscopy images of two representative WS2 monolayer coupled multi-singular plasmonic metasurfaces. Top: mechanically exfoliated WS2 monolayer (1L) on PDMS tape. Bottom: WS2 monolayer on flexible plasmonic metasurface substrates.

Fig. S3| Transmission electron microscopy (TEM) images of the 20 nm thick gold multi-singular metasurface showing the densely packed sub-nanometer plasmonic gaps from the first path. A new crack is created in the preformed strip/domain, extends and stops before the strip/domain completely breaks into two53, resulting in a sub-nanometer fracture gap in the preformed domain.

Fig. S4| TEM images of the 20 nm thick gold multi-singular metasurface showing the densely packed sub-nanometer plasmonic gaps from the second path. Biaxial intergranular fractures are used to create sub-nanometer distances between adjacent fragment domains, where the deflected fracture edges of one fragment domain is dragged close to the fracture edges of the adjacent fragment domains at sub-nanometer spacing.

Fig. S5| Stress-strain curves. Stress-strain curves for the gold film (20 nm thick )/PEI (125 μm thick) substrate in a, x-directional and b, y-directional stretching processes, respectively.

Fig. S6| Statistical analysis of the zigzag crack deflection angles (from the loading direction) in the x-directionally stretched plasmonic metasurface. The gold film thicknesses are a, 10 nm, b, 20 nm, and c, 30 nm, respectively. The zigzag crack deflection angles are between 55° and 65°.

Fig. S7| SEM images of the metasurface with different y-directional elongation. a-c, SEM images of cold-etched isotropic metasurfaces with metal layer of (a) 10 nm, (b) 20 nm, and (c) 30 nm, respectively. Isotropic refers to the case where the y-directional stretching has the same elongation as the x-directional stretching (~80%). d-f, SEM images of the anisotropic metasurface with a gold layer thickness of 20 nm with y-directional elongation at 0% (d), 56% (e), and 100% (f), respectively. Anisotropy here means that the average fragment domain size is different in one direction than in the other.

Fig. S8| Dark-field scattering spectra of the metasurface a, with different gold film thicknesses (from bottom to top, the gold film thickness (tAu) increases from 17 nm to 24 nm) and b, at different angles of incidence (0° to 30° with Au thickness is 22 nm).

Fig. S9| a, Reprehensive scattering spectra of the plasmonic metasurface (without WS2 monolayer on top) at different strains. The plasmonic resonance is continuously red-shifted from 645 nm to 653 nm with increasing positive strain from 0 to 0.75% and blue-shifted from 645 nm to 634 nm with decreasing negative strain from 0 to -1%. The gold film thickness is 20 nm. b, Plasmons enhanced Raman scattering intensity of the WS2 monolayer at different strains.

Fig. S10| The simulated mapping of the coupling strength using the near-field of the gap plasmons in Fig. 1f in the main paper.

Fig. S11| Coupling strength (right panel) for different plasmonic systems. The percentage indicates the y-directional elongation extent. Curves in the figure labelled only with the thickness value but not with elongation extent represent isotropic samples.

Fig. S12| Active ultrastrong coupling of different plasmonic metasurfaces from Fig. 3 of the main paper. a, Representative dark field scattering spectra at different uniaxial strains. The strain value gradually increases from red (-1%) to blue (0.75%) and the interval is ~0.06%. b, Dark field scattering spectra as a function of excitation wavelength and strain. c, Normalized coupling strength as a function of the uniaxial strain. The horizontal dashed line marks the onset of ultrastrong coupling.

Fig. S13| Strong exciton-plasmon coupling in a WS2 monolayer coupled to bowtie and dimer antennas. The upper and lower polariton branches of the WS2 coupled bowtie (circles) and dimer (triangles) antenna systems are fitted (solid lines) with a coupling strength of 80.9 meV and 86 meV, respectively, in the Tavis-Cummings Hamiltonian, respectively. The plasmonic mode frequencies for the two traditional plasmonic systems are almost overlap (oblique dashed lines). The scale bar is 100 nm.

Fig. S14| Tunable resonant polariton-enhanced second-order nonlinearity in WS2 monolayer. a, Schematic energy diagram describing the polariton-enhanced second harmonic generation (SHG) in the WS2 monolayer arising from the two-photon resonances in the vicinity of the two hybridized polaritonic states between 2D excitons and surface plasmons. b, Resonant polariton-enhanced second harmonic (SH) signal intensity (ISH) from WS2 as a function of the SHG energy. The peak of the ISH in the WS2 monolayer on polymer originates from the two-photon exciton resonance enhanced SHG. The peaks and splittings of the ISH in the WS2 monolayer coupled to a multi-singular metasurface are due to the two-photon resonances provided by the hybridized polaritonic states. Compared to the SC, USC provides broader and higher SHG enhancement. c, Polarized polariton-enhanced SHG from the WS2 monolayer. A typical 6-fold symmetric petal SHG pattern is well fitted by ISH=Ccos23θ showing the isotropic property of the multi-singular plasmonic metasurface, where C is the maximum SHG intensity, and θ is the rotation angle of the sample. The intensity of the SHG emission from the WS2 on PDMS is amplified by a factor of three for a clear view. The polariton-enhanced SHG from the WS2 monolayer is around 15 times stronger than that on PDMS. The polarization-independent polariton-enhanced SHG is promising because it eliminates the need to align the crystal orientation of the WS2 for effective polariton-enhanced nonlinearity, in contrast to the polarization-dependent SHG in the WS2 coupled bowtie antenna system where maximum enhancement occurs only when the pump field is polarized along the longitudinal symmetry axis. d, SHG intensity under different uniaxial strains. Error bars are standard errors from multiple samples. In c and d, the laser wavelength is fixed at 800 nm. Note that the isotropic metasurface has very uniformly distributed nanometer-sized plasmonic gaps (see Fig. S7) and the laser beam has a fairly large spot size, so that each SHG measurement sees an average effect, resulting in particularly reproducible SHG intensity under different uniaxial strains.

Fig. S15| Normalized photoluminescence (PL) intensity under different strains. We find no splitting in the PL emissions of the coupled plasmonic system; instead, we observe a noticeable red shift of the PL emission peak position as in other previous work4. Our inability to observe Rabi splitting in the PL measurements is due to the large laser spot size (diameter~4 μm) and the resulting high fraction of background PL contribution (emission from the uncoupled exciton, dashed line).

Fig. S16| Effect of strain on WS2 exciton energy. Dark field scattering spectra of WS2 monolayer on PDMS substrate under different strains.

Fig. S17| Comparison of the normalized coupling strength (gωex) measurements (triangles for 0% strain, circles for -2% strain) with simulation. The solid lines are the simulation results for different WS2 layer number.

Table S1. Emitter thickness and corresponding normalized coupling strength (g/ωex), coupling strength (g), and exciton energy (ωex) in this work (purple), TMDs (red), organic molecules (blue), and inorganic quantum dots (QD, green) with a thickness less than 20 nm.

| System | Thickness (nm) | g/ωex | g(meV) | ωex(eV) |
| --- | --- | --- | --- | --- |
| This work | 0.618 1.854 2.472 | 0.12 0.147 0.164 | 240.4 295.5 328.5 | 2.0189 2.01 2.003 |
| 1L WSe2/PC | 0.649 | 0.006 | 9.5 | 1.65 |
| 1L MoSe2/DBR | 0.646 | 0.014 | 23 | 1.666 |
| 1L MoSe2/DBR | 0.646 | 0.005 | 7.6 | 1.667 |
| 1L WS2/DBR | 0.618 | 0.01 | 20.8 | 28 |
| 1L WS2/DBR | 0.618 | 0.01 | 20.3 | 2.0789 |
|  | 0.618 | 0.01 | 19.8 | 2.072 |
|  | 0.618 | 0.009 | 18.8 | 2.05 |
|  | 0.618 | 0.009 | 18.3 | 2.042 |
| 1L WS2/DBR | 0.618 | 0.008 | 16.5 | 210 |
| 1L MoS2/DBR | 0.615 | 0.015 | 28 | 1.85511 |
| 1L WS2/Ag microcavity | 0.618 | 0.025 | 50 | 1.9812 |
| 1L WS2/Ag Prism | 0.618 | 0.023 | 48 | 2.0513 |
| 1L MoS2/Ag NP on Au film | 0.615 | 0.051 | 95 | 1.86414 |
| 1L WSe2/Ag Nanorod | 0.649 | 0.015 | 24.75 | 1.65915 |
| 1L WS2/Au Nanorod | 0.618 | 0.027 | 53 | 1.95016 |
| 1L MoS2/Ag disk array | 0.615 | 0.033 | 63 | 1.93717 |
| 1L WS2/Au metasurface | 0.618 | 0.012 | 24 | 2.0118 |
| 1L WS2/Au Prism | 0.618 | 0.041 | 82 | 1.9919 |
| 1L WS2/Au nanoantenna | 0.618 | 0.035 | 69 | 220 |
| 1L WS2/Au nanoantenna | 0.618 | 0.032 | 64 | 2.0221 |
| 1L WS2/Ag particle | 0.618 3.708 | 0.032 0.036 | 65 73.82 | 2.0322 |
| 1L WS2/Chirped Ag nanogroove array | 0.618 | 0.028 | 56.82 | 2.02823 |
| 1L,2L,4L,16L WS2/Ag nanorod array | 0.618 1.236 2.472 9.888 | 0.012 0.014 0.019 0.025 | 24.39 29.02 39.00 50.03 | 2.02324 |
| 1L WS2/Au nanorods | 0.618 | 0.015 | 28.64 | 1.9625 |
| 1L WSe2/Au nanorods | 0.649 | 0.03 | 49.78 | 1.6726 |
| 1L WS2/Au@Ag nanocuboid | 0.618 | 0.024 | 48.98 | 2.02127 |
| 1L, 2L, 3L, 4L, 8L WSe2/Au bi-pyramids | 0.649 1.298 1.947 2.596 5.491 | 0.027 0.027 0.03 0.031 0.031 | 44.71 45.84 49.86 52.07 51.85 | 1.6728 |
| 1L MoS2/Au bi-pyramids | 0.615 | 0.022 | 42.3 | 1.8829 |
| 1L, 7L WS2/Au nanodisks | 0.618 4.326 | 0.033 0.047 | 64.62 93 | 1.96330 |
| 1L WS2/Ag nanoprisms | 0.618 | 0.037 | 73.53 | 2.01231 |
| 12L WSe2/Au NPs on Au film | 7.788 | 0.044 | 71.36 | 1.6332 |
| 1L WSe2/Ag nanocubes on Ag film | 0.649 | 0.017 | 28.08 | 1.6633 |
| 1L WS2/Ag nanocubes on Ag film | 0.618 | 0.041 | 84.04 | 2.0234 |
| 1L MoS2/Au nanospheres on Au film | 0.615 | 0.035 | 65.11 | 1.8654 |
| 1L WS2/Ga NPs on Au film | 0.618 | 0.041 | 83.16 | 2.0235 |
| TDBC J-aggregates/Ag nanorods | 2 | 0.025 | 52.6 | 2.1136 |
| TDBC J-aggregates/Ag nanoprisms | 2 | 0.067 | 142.21 | 2.1137 |
| TDBC J-aggregates/Ag nanoprisms | 3 | 0.095 | 200.39 | 2.1138 |
| PIC J-aggregates/Au@Ag cuboid nanorods | 1 | 0.053 | 113.39 | 2.1639 |
| TDBC J-aggregates/Au@Ag nanorings | 2 | 0.053 | 111.3 | 2.11640 |
| DPDC J-aggregates in PVA/Au nanodisk dimers | 15 | 0.078 | 140.09 | 1.7941 |
| Cyanine dye J-aggregates/Au NP dimers | 5 | 0.043 | 91.55 | 2.1442 |
| J-aggregates/Au nanocubes on Au film | 3 | 0.048 | 91.73 | 1.9143 |
| Atto 532 molecules/Ag nanocubes on Ag film | 9 | 0.032 | 84.75 | 2.6644 |
| CdSe/ZnS QDs/Ag nanobowties | 8 | 0.06 | 108.66 | 1.845 |
| CdSe/ZnS QDs/Ag nanobowties | 8 | 0.067 | 119.95 | 1.846 |
| CdSe/CdS QDs/Au NP dimer | 8 | 0.09 | 188.52 | 2.0947 |
| CdSe/CdS QDs/Au NPs on Ag film | 6 | 0.06 | 115.97 | 1.9248 |
| CdSe/ZnS QDs/Au tip above Au substrate | 5 | 0.046 | 86.09 | 1.8749 |
| Carbon QDs/Au NPs on Au film | 0.34 | 0.039 | 71.59 | 1.8250 |

References

- Yanaka, M., Tsukahara, Y., Nakaso, N. & Takeda, N. Cracking phenomena of brittle films in nanostructure composites analysed by a modified shear lag model with residual strain. J. Mat. Sci. 33, 2111-2119 (1998).

- Li, T. & Suo, Z. Ductility of thin metal films on polymer substrates modulated by interfacial adhesion. Int. J. Solids Struct. 44, 1696-1705 (2007).

- Hutchinson, J. W. & Suo, Z. Mixed mode cracking in layered materials. Adv. Appl. Mech. 29, 63-191 (1991).

- Liu, X. et al. Nonlinear valley phonon scattering under the strong coupling regime. Nat. Mater. 20, 1210-1215 (2021).

- Zhang, L., Gogna, R., Burg, W., Tutuc, E. & Deng, H. Photonic-crystal exciton-polaritons in monolayer semiconductors. Nat. Commun. 9, 1-8 (2018).

- Lundt, N. et al. Optical valley Hall effect for highly valley-coherent exciton-polaritons in an atomically thin semiconductor. Nat. Nanotechnol. 14, 770-775 (2019).

- Dufferwiel, S. et al. Valley-addressable polaritons in atomically thin semiconductors. Nat. Photon. 11, 497-501 (2017).

- Liu, X. et al. Nonlinear optics at excited states of exciton polaritons in two-dimensional atomic crystals. Nano Lett. 20, 1676-1685 (2020).

- Liu, X. et al. Control of coherently coupled exciton polaritons in monolayer tungsten disulphide. Phys. Rev. Lett. 119, 027403 (2017).

- Gu, J., Chakraborty, B., Khatoniar, M. & Menon, V. M. A room-temperature polariton light-emitting diode based on monolayer WS2. Nat. Nanotechnol. 14, 1024-1028 (2019).

- Chen, Y. J., Cain, J. D., Stanev, T. K., Dravid, V. P. & Stern, N. P. Valley-polarized exciton–polaritons in a monolayer semiconductor. Nat. Photon. 11, 431-435 (2017).

- Sun, Z. et al. Optical control of room-temperature valley polaritons. Nature Photonics 11, 491-496 (2017).

- Munkhbat, B. et al. Electrical control of hybrid monolayer tungsten disulfide–plasmonic nanoantenna light–matter states at cryogenic and room temperatures. ACS Nano 14, 1196-1206 (2020).

- Hou, S. et al. Manipulating coherent light–matter interaction: continuous transition between strong coupling and weak coupling in MoS2 monolayer coupled with plasmonic nanocavities. Adv. Opt. Mater. 7, 1900857 (2019).

- Zheng, D. et al. Manipulating coherent plasmon–exciton interaction in a single silver nanorod on monolayer WSe2. Nano Lett. 17, 3809-3814 (2017).

- Wen, J. et al. Room-temperature strong light–matter interaction with active control in single plasmonic nanorod coupled with two-dimensional atomic crystals. Nano Lett. 17, 4689-4697 (2017).

- Lee, B. et al. Electrical tuning of exciton–plasmon polariton coupling in monolayer MoS2 integrated with plasmonic nanoantenna lattice. Nano Lett. 17, 4541-4547 (2017).

- Chervy, T. et al. Room temperature chiral coupling of valley excitons with spin-momentum locked surface plasmons. ACS Photon. 5, 1281-1287 (2018).

- Qin, J. et al. Revealing strong plasmon-exciton coupling between nanogap resonators and two-dimensional semiconductors at ambient conditions. Phys. Rev. Lett. 124, 063902 (2020).

- Liu, L. et al. Strong plasmon–exciton interactions on nanoantenna array–monolayer WS2 hybrid system. Adv. Opt. Mater. 8, 1901002 (2020).

- Liu, L. et al. Plasmon-induced thermal tuning of few-exciton strong coupling in 2D atomic crystals. Optica 8, 1416-1423 (2021).

- Yankovich, A. B. et al. Visualizing spatial variations of plasmon–exciton polaritons at the nanoscale using electron microscopy. Nano Lett. 19, 8171-8181 (2019).

- Sang, Y. et al. Tuning of two-dimensional plasmon–exciton coupling in full parameter space: a polaritonic non-Hermitian system. Nano Lett. 21, 2596-2602 (2021).

- Wang, S. et al. Limits to strong coupling of excitons in multilayer WS2 with collective plasmonic resonances. ACS Photon. 6, 286-293 (2019).

- Jiang, Y. et al. Resonance coupling in an individual gold nanorod–monolayer WS2 heterostructure: photoluminescence enhancement with spectral broadening. ACS Nano 14, 13841-13851 (2020).

- Wen, J. et al. Room-temperature strong coupling between dipolar plasmon resonance in single gold nanorod and two-dimensional excitons in monolayer WSe2. Chinese Phys. B 27, 096101 (2018).

- Wang, S. et al. Coherent coupling of WS2 monolayers with metallic photonic nanostructures at room temperature. Nano Lett. 16, 4368-4374 (2016).

- Stuhrenberg, M. et al. Strong light–matter coupling between plasmons in individual gold bi-pyramids and excitons in mono-and multilayer WSe2.  Nano Lett. 18, 5938-5945 (2018).

- Lawless, J. et al. Influence of gold nano-bipyramid dimensions on strong coupling with excitons of monolayer MoS2. ACS Appl. Mater. Interfaces 12, 46406-46415 (2020).

- Geisler, M. et al. Single-crystalline gold nanodisks on WS2 mono-and multilayers for strong coupling at room temperature. ACS Photon. 6, 994-1001 (2019).

- Cuadra, J. et al. Observation of tunable charged exciton polaritons in hybrid monolayer WS2- plasmonic nanoantenna system. Nano Lett. 18, 1777-1785 (2018).

- Kleemann, M. E. et al. Strong-coupling of WSe2 in ultra-compact plasmonic nanocavities at room temperature.  Nat. Commun. 8, 1296 (2017).

- Sun, J. et al. Light-emitting plexciton: exploiting plasmon–exciton interaction in the intermediate coupling regime. ACS Nano 12, 10393-10402 (2018).

- Han, X. et al. Rabi splitting in a plasmonic nanocavity coupled to a WS2 monolayer at room temperature. ACS Photon. 5, 3970-3976 (2018).

- Deng, F. et al. Strong exciton–plasmon coupling in a WS2 monolayer on Au film hybrid structures mediated by liquid Ga nanoparticles. Laser Photonics Rev. 14, 1900420 (2020).

- Zengin, G. et al. Approaching the strong coupling limit in single plasmonic nanorods interacting with J-aggregates. Sci. Rep. 3, 1-8 (2013).

- Zengin, G. et al. Realizing strong light-matter interactions between single-nanoparticle plasmons and molecular excitons at ambient conditions. Phys. Rev. Lett. 114, 157401 (2015).

- Wersall, M., Cuadra, J., Antosiewicz, T. J., Balci, S. & Shegai, T. J. N. l. Observation of mode splitting in photoluminescence of individual plasmonic nanoparticles strongly coupled to molecular excitons. Nano Lett. 17, 551-558 (2017).

- Liu, R. et al. Strong light-matter interactions in single open plasmonic nanocavities at the quantum optics limit. Phys. Rev. Lett. 118, 237401 (2017).

- Li, N. et al. Strong plasmon–exciton coupling in bimetallic nanorings and nanocuboids. J. Mater. Chem. C 8, 7672-7678 (2020).

- Schlather, A. E., Large, N., Urban, A. S., Nordlander, P. & Halas, N. J. Near-field mediated plexcitonic coupling and giant Rabi splitting in individual metallic dimers. Nano Lett. 13, 3281-3286 (2013).

- Roller, E.-M., Argyropoulos, C., Högele, A., Liedl, T. & Pilo-Pais, M. J. Plasmon–exciton coupling using DNA templates. Nano Lett. 16, 5962-5966 (2016).

- Chen, X. et al. Mode modification of plasmonic gap resonances induced by strong coupling with molecular excitons.  17, 3246-3251 (2017).

- Huang, J., Traverso, A. J., Yang, G. & Mikkelsen, M. H. Real-time tunable strong coupling: from individual nanocavities to metasurfaces. Nano Lett. 6, 838-843 (2019).

- Santhosh, K., Bitton, O., Chuntonov, L. & Haran, G. J. Vacuum Rabi splitting in a plasmonic cavity at the single quantum emitter limit. Nat. Commun. 7, 11823 (2016).

- Bitton, O. et al. Vacuum Rabi splitting of a dark plasmonic cavity mode revealed by fast electrons.  Nat. Commun. 11, 487 (2020).

- Luo, Y. et al. Colloidal Assembly of Au–Quantum Dot–Au Sandwiched Nanostructures with Strong Plasmon–Exciton Coupling. J. Phys. Chem. 11, 2449-2456 (2020).

- Leng, H., Szychowski, B., Daniel, M.-C. & Pelton, M. J. Strong coupling and induced transparency at room temperature with single quantum dots and gap plasmons. Nat. Commun. 9, 4012 (2018).

- Park, K.-D. et al. Tip-enhanced strong coupling spectroscopy, imaging, and control of a single quantum emitter. Sci. Adv. 5, 5931 (2019).

- Katzen, J. M. et al. Strong coupling of carbon quantum dots in plasmonic nanocavities. ACS Appl. Mater. Interfaces 12, 19866-19873 (2020).