Supporting Information

Towards a deep understanding of the biomass fractionation in respect of lignin nanoparticles formation

Jiayun Xu1,2, Rui Liu2, Luyao Wang2, Andrey Pranovich2, Jarl Hemming2, Lin Dai1*, Chunlin Xu2*, Chuanling Si1*

1State Key Laboratory of Biobased Fiber Manufacturing Technology, Tianjin Key Laboratory of Pulp and Paper, College of Light Industry and Engineering, Tianjin University of Science and Technology, Tianjin 300457, China

2Laboratory of Natural Materials Technology, Åbo Akademi University, Turku FI-20500, Finland

*Corresponding authors.

E-mail: dailin@tust.edu.cn (L. Dai); Chunlin.Xu@abo.fi (C. Xu); sichli@tust.edu.cn (C. Si).

Table of Contents

1. Supplementary Text

Text S1. Methods for Quantitative 13C NMR measurements.

2. Supplementary Figures

Figure S1. 13C NMR spectra of the HWMF and SWMF samples.

Figure S2. 31P NMR spectra of the HWMF and SWMF samples.

3. Supplementary References

1. Supplementary Text

Quantitative 13C NMR measurements. About 170 mg of HWMF and SWMF sample were dissolved in 550 μL DMSO-d6 containing 0.0016 M Chromium (Ⅲ) acetylacetonate as the relaxation regent. The 13C NMR analysis was performed using a Bruker AVANCE Ⅲ 500 MHz spectrometer equipped with a 5 mm Z-gradient Broadband Observe CryoProbe. 13C NMR spectra were acquired using the inverse-gated decoupling pulse (zgig) sequence with a 2 s relaxation delay and acquisition time of 1.1 s, and 20000 scans were recorded.

The degree of condensation (DC, in %Ar) is calculated by the following Equation S1[1,2]:

(I163-103)non-acetylated-(I125-103)non-acetylated+(I193-191)non-acetylated

The integral value for the total aromatic carbons (163.0-103.0 ppm) in the spectrum of quantitative 13C NMR was set to 612 as the base of all calculations. The integrations of two clusters at δC 125–103 ppm, and δC 193–191 ppm were assigned as theoretical aromatic methine carbons (CAr-H) in non-condensed lignin units, and vanillin, respectively.

2. Supplementary Figures

Figure S1. 13C NMR spectra of the HWMF and SWMF samples.

Figure S2. 31P NMR spectra of the HWMF and SWMF samples.

3. Supplementary References

1. Capanema EA, Balakshin MY, Kadla JF (2004) A comprehensive approach for quantitative lignin characterization by NMR spectroscopy. J Agric Food Chem 52 (7):1850-1860. doi:10.1021/jf035282b

2. Wang L, Lagerquist L, Zhang Y, Koppolu R, Tirri T, Sulaeva I, Schoultz Sv, Vähäsalo L, Pranovich A, Rosenau T, Eklund PC, Willför S, Xu C, Wang X (2020) Tailored Thermosetting Wood Adhesive Based on Well-Defined Hardwood Lignin Fractions. ACS Sustainable Chemistry & Engineering 8 (35):13517-13526. doi:10.1021/acssuschemeng.0c05408