Supplementary Information

Interface states of metal‒oxide‒semiconductor devices based on aligned carbon nanotube arrays

Yifan Liu1, Sujuan Ding2, Weili Li3, Zirui Zhang1, Zipeng Pan1, Yumeng Ze1, Bing Gao2, Yanning Zhang3, Chuanhong Jin2, Lian-Mao Peng1* and Zhiyong Zhang1*

1Key Laboratory for the Physics and Chemistry of Nanodevices and Center for Carbon-based Electronics, School of Electronics, Peking University, Beijing 100871, China.

2State Key Laboratory of Silicon and Advanced Semiconductor Materials, School of Materials Science and Engineering, Zhejiang University, Hangzhou 310027, China.

3Institute of Fundamental and Frontier Sciences, University of Electronic Science and Technology of China, Chengdu 610054, China

*Correspondence to: lmpeng@pku.edu.cn; zyzhang@pku.edu.cn.

Supplementary Figure 1. Cross-sectional STEM image of the typical A-CNT array, showing the side view of as-prepared A-CNT array on SiO2 substrate used in this work. Scale bar: 5 nm.

(b)

(a)

Supplementary Figure 2. The comparison of two kinds of A-CNT MOS structures. a, FET-like semi-vertical MOS structure. b, Traditional full-vertical MOS structure.

Traditional back-contacted MOS structure is easy to fabricate but not suitable for A-CNT arrays since large area CNT-metal interface could interfere with CNT-dielectric interface by inducing Schottky barrier, metal-induced-gap-states (MIGS), Fermi-level pinning (FLP) and high floor metal-insulator-metal (MIM) capacitance. Thus, the electrical contacts to A-CNT arrays should be present only at the edges, and a FET-like semi-vertical MOS structure in Fig. 1a or Supplementary Figure 2a should be used, in order to lowering the CNT-metal interface area and well excluding those irrelevant influences. Such an A-CNT MOS structure is still an equilibrium system and follows the band diagram in Fig. 1b since no net voltage is applied in the carrier transport direction, and charges can be injected into the A-CNT arrays from both source and drain electrodes when giving a gate bias.

(b)

(c)

(a)

Supplementary Figure 3. Equivalent circuits of the A-CNT MOS structure. a, The complete equivalent circuit of the A-CNT MOS structure. b, The effective equivalent circuit within 1 GHz. c, The simplified effective equivalent circuit, neglecting border trap capacitance & resistance (Cbt & Rbt) because border traps have weaker and indirect influence on the gate electrostatics than interface states, also shown in Figure 1a.

The intrinsic parameters of A-CNT MOS structures include oxide capacitance (Cox), quantum capacitance of the A-CNT array (Cq), interface state capacitance and resistance (Cit and Rit), and border trap capacitance and resistance (Cbt and Rbt). Geometry and process related parasitic effects mainly include parasitic capacitance (Cpara) and resistance (Rpara), the former consists of the fringe capacitance (Cgs/d) between gate and source/drain electrodes, and the latter includes the gate resistance (Rg), contact resistance (Rc), extension resistance (Rext, resistance of the ungated channel gap between contacts and gate), and channel resistance (Rch). Besides, Lg and Ls/d are the gate and source/drain inductance, respectively, which is usually neglected within 1 GHz. Gleak is the leakage conductance, which can also be neglected in a well optimized MOS structure.

Supplementary Note 1 Geometry and process design of A-CNT MOS structures.

The goal for geometry and process design of A-CNT MOS structures is to minimize Cpara and Rpara, which involves multiple parameters and needs carefully consideration.

Cpara between gate and contact electrodes is proportional to the channel width (Wch) and inversely proportional to the ungated or extension channel length (Lext), while Rext is proportional to Lext and inversely proportional to Wch. Since both of them will cause an overestimation of interface states and an extraction error of other parameters, a design balance of both Lext and Wch should be made. A slightly larger Lext also makes sure that possible Schottky barrier at contacts will not be under gate control, thus keeping a Vg-independence Rc and simplifying the problem. Besides, the measurement is also sensitive to the channel length (Lch), because that a Lch longer than twice the average length of CNT (LCNT, about 2 μm) 1 will increase Rch significantly by incorporating many CNT-CNT tunneling junctions (see Fig. 1c top inset), while a short Lch (< 1 μm empirically) will reduce total capacitance and induce a large noise. Considering parasitics, gating effect of Schottky barrier, CNT-CNT tunneling junctions, and measurement noises, design parameters including the Lext between 50 nm to 150 nm, Wch between 100 μm to 400 μm, and Lch between 0.8 μm to 3 μm are adopted in this work

An ideal Ohmic contact helps reducing Rc and increasing charge injection efficiency, thus Palladium (Pd) or Scandium/Yttrium (Sc/Y) with suitable metal work functions and CNT-wetting properties should be used to form high-quality P-type or N-type CNT-metal contacts2.To avoid oxidation of contact metal in processing, Pd with high work function and relatively good stability is used to form P-type A-CNT MOS structures in this work. By doing so, charge traps in the band-gap and valence band can be analyzed accurately while traps in the conduction band are blurred by the electron Schottky barrier. Although a discussion for N-type A-CNT MOS structures is necessary, it basically follows the same procedures as for P-type devices, but needs a more careful contact protection, therefore beyond the scope of this work. Another important process consideration involves the dielectric thickness. While thin high-κ dielectrics (< 6 nm) are frequently used in constructing high performance CNT MOSFETs to maintain high electrostatic effeciency1,3,4, a thick dielectric is more suitable for studying MOS structures with a focus on the CNT-dielectric interface. In this work, we use a relatively thick Hafnium oxide (about 7 ~ 9 nm) to suppress the gate leakage, the influence of gate-dielectric interface traps on channel, and the interaction between oxide traps and gate metal which were reported in some MOS systems5,6. This simplification is quite common and useful when dealing with complicated MOS systems7.

(a)

(b)

(c)

(d)

(e)

Supplementary Figure 4. Structural details of A-CNT MOS structures, a, Cross-sectional scanning transmission electron microscopy (STEM) images and corresponding EDS mapping of a typical A-CNT MOS structure. b-e, A-CNT MOS structures with designed Lg of 0.8 μm, 1 μm, 2 μm, and 3 μm, respectively; and fluctuating Lext between 80 nm to 130 nm. The source and drain electrodes are in-situ short-connected to prevent the external connection noise.

(d)

(a)

(b)

(e)

(c)

(f)

F

A

B

C

D

E

Supplementary Figure 5. The C-V hysteresis at 1 MHz. a-c, high-density A-CNT MOS structures (F (a), A (b), and B (c)). d-f, low-density A-CNT MOS structures (C (d), D (e), and E (f)). Generally, C-V hysteresis decreases as interface quality improves.

(b)

(a)

Supplementary Figure 6. The gate leakage measurement. a, The gate leakage of high-density A-CNT MOS structures. b, The gate leakage of low-density A-CNT MOS structures. Gate leakage (Ig-Vg) curves of all devices are small enough to approach the lower detection limit. Considering that the MOS gating area is as large as 300 μm2, such small leakage can be ignored.

Supplementary Figure 7. Independently measured parasitic capacitance curves, including four A-CNT MOS structures with different extension length and channel width (str-1: Lext = 125 nm & Wch = 400 μm; str-2: Lext = 150 nm & Wch = 300 μm; str-3: Lext = 150 nm & Wch = 150 μm; str-4: Lext = 150 nm & Wch = 100 μm).

A-CNT arrays in four MOS geometries are completely etched to ensure that all capacitance responses are fringe capacitances without the field effect. The shapes of Cpara are flat as expected but their values deviate from the theoretical formula of plate capacitor (), which can be explained by a patterning alignment variation. The influence of Cpara on Dit extraction can be estimated through analytical calculations:

With geometry variations, however, the maximum Cpara is still less than 150 fF, which only accounts for about 3% overestimation of interface states according to above calculations. Frequently used de-embedding process of Cpara is directly subtracting it from Cm because that Cpara is in parallel connection with all other parts in the equivalent circuit (see Fig. 1a and Supplementary Figure 3). However, the Cm in depletion limited by Cq (approaching 0 in band-gap, see Fig. 3f) could be smaller than presumed Cpara due to patterning variations. Thus, to avoid extravagant de-embedding and negative C-V data, Cpara can be ignored and left as an acceptable systematic error (about 3% in this work).

(b)

(a)

Supplementary Figure 8. Illustration of the influence of Rpara in accumulation. a, Simulated C-V curves with small Rpara and negligible frequency dispersion. b, Simulated C-V curves with magnified Rpara and small frequency dispersion. Ctot and Gtot are the simulated total capacitance and conductance of the A-CNT MOS structure, respectively. Only a very large Rpara in A-CNT MOS structures can cause obvious frequency dispersion in accumulation.

(b)

(a)

Supplementary Figure 9. The parasitic resistance extraction. a, The linear fitting of parasitic resistance from strong accumulation (below) to mid-gap (up). Each voltage bias contains six frequency points from 5 MHz to 10 MHz. b, Parasitic resistance measurement and extrapolation results of a typical A-CNT MOS structure. The extrapolation is only valid away from mid-gap and agrees well with high frequency measurement.

Rpara can be directly measured at a frequency as high as possible, for example 10MHz in this work. By biasing the MOS structure into strong accumulation, Rpara can also be determined by the linear fit of measured resistance (R) and reactance (X) values between 5 MHz to 10 MHz, where the intersect on Y axis when X equals to 0 indicates the frequency-independent series resistance8. Rpara curves obtained by different methods both follow the behavior of field-effect Rch, and are very consistent in accumulation and in the lower-half of band gap. Values of Rpara in accumulation are very small due to CNT’s high mobility and multiple conducting channels in A-CNT arrays.

(b)

(a)

(c)

(d)

Supplementary Figure 10. Rpara De-embedding comparison. a, as-measured multifrequency C-V curves. b, de-embedded multifrequency C-V curves. c, as-measured multifrequency G-V curves. d, de-embedded multifrequency G-V curves.

The de-embedding process of Rpara follows Eq. 9, where Cc and Gc are the de-embedded capacitance and conductance, respectively. By comparing C-V and G-V curves with and without Rpara de-embedding, no obvious change is observed thanks to our high-quality Ohmic contact and carefully designed MOS geometry. In general, the reliability of admittance analysis will not be hindered by parasitic effects in this work.

(b)

(a)

Supplementary Figure 11. Frequency dispersions of the admittance data. a, The C-F trends under different biases in accumulation, and the capacitance dispersion follows a quasi-log relation. b, The G-F trends under different biases in accumulation, and the conductance dispersion follows a quasi-linear relation. Both of them agree with the distributed equivalent circuit model of border traps10.

(a)

(b)

(c)

(d)

Supplementary Figure 12. The interface morphology characterization of unoptimized A-CNT MOS structures with the baseline ALD condition. a, b, Another two examples showing similar ADF and BF STEM images as Fig. 2a and Fig. 2b in A-CNT MOS structures before ALD improvement, yellow arrows showing obvious un-conformal dielectrics (a) even with pin-holes (b). Scale bar: 5 nm. c, d, The statistical results of HfO2 thickness on A-CNT arrays and SiO2 substrate, respectively, for A-CNT MOS structures shown in Fig. 2a, Fig. 2b, Supplementary Figure 12a and Supplementary Figure 12b.

Supplementary Note 2 The simulation of A-CNT/HfO2 interface

The bulk amorphous-HfO2 (a-HfO2) structure is constructed through the “melt and quench” approach employing the ab initio molecular dynamics (AIMD). During the whole AIMD simulation, the plane-wave cutoff energy is set as 500 eV, and the Brillouin zone is sampled at the Γ point. The generation of the a-HfO2 structure is initiated with a 2×2×4 supercell of cubic HfO2 structure consisted of 192 atoms, which is classically melted at an artificial low density (9 g/cm3, by rescaling every basis vector by a factor of 1.064) at 6000 K for 20 ps with the time step of 1 fs, providing well melt intermixing. Then, the lattice constant of a-HfO2 structure is instantaneously changed to match the 1×1×3 supercell of the CNT, and melted at 6000 K for 10 ps with the time step of 1 fs. Subsequently, the a-HfO2 structure amorphization is produced by linearly quenching back to 300 K for 10 ps with the time step of 1 fs, then further equilibrating for 5 ps followed by the structural relaxation optimization to obtain the optimal a-HfO2 structure. Then, the a-HfO2 slab with thickness of 1 nm is generated by breaking the boundary condition in the z direction and introducing a vacuum region with a width larger than 10Å, and the A-CNT/HfO2 interface can be established on the surface. The whole structure is fully optimized until the force on each atom and total energy variations are smaller than 0.02 eV/Å and 1 × 10-6 eV, respectively. The ideal A-CNT/HfO2 interface structure is shown in the Supplementary Figure 13. Herein, defective A-CNT/HfO2 interfaces with the oxygen vacancies (VO) or oxygen interstitials (IO) can be investigated. According to the atomic coordination number of the O atom, there are two kinds of oxygen vacancies (VO2 and VO3) at the interface which easily evolute into together, so the Vo in the following indicates that two adjacent asymmetric oxygen vacancies (VO2 and VO3) are both present.

The defect formation energy at the A-CNT/HfO2 interface shown in Supplementary Figure 14c, is defined as Edefect+nμO-Eideal/n , in which Edefect and Eideal are the total energy of the defective and ideal interface, the oxygen chemical potential μO is calculated as the half of the total energy of an isolated oxygen molecule with correction, n is the number of defect atoms.

(b)

(a)

(c)

(d)

(e)

(f)

Supplementary Figure 13. The structures and the differential charge density distributions of different A-CNT/HfO2 interface types. a, The ideal structure, the red and big yellow balls in the ball-and-stick model represent oxygen and hafnium atoms, and the small yellow balls represent carbon atoms, two blue balls mark out positions of two asymmetric oxygen vacancies (VO), and green balls mark out the bonding Hf and O atoms with the interstitial oxygen (IO). b, The three-view drawing of the differential charge density (DCD) distribution of the ideal structure. c-f, The three-view drawing of the DCD distribution of the defect structure with two nearest adjacent oxygen vacancies (2-coordinated VO and 3-coordinated VO) (c), with the nearest oxygen interstitial (d), with the nearest 2-coordinated oxygen vacancy (VO2) (e), and with the nearest 3-coordinated oxygen vacancy (VO3) (f), respectively.

(a)

(b)

(c)

(d)

Supplementary Figure 14. Detailed electronic properties of different A-CNT/HfO2 interface types a, b, Averaged distribution of the DCD along the vertical direction of A-CNT/HfO2 interface (a); and Partial density of states (PDOS) versus energy (b) for the A-CNT/HfO2 interface systems without defects, with oxygen vacancies, and with oxygen interstitials, respectively. c, The average formation energy for different defects at the interface. d, The discrete trap energy levels (ET) for different defects at the interface extracted from the energy bands. VB and CB represent the valence band and the conduction band, respectively; VBO and CBO represent the valence band offset and the conduction band offset, respectively; VBM and CBM represent the valence band edge and the conduction band edge, respectively.

(a)

(b)

Supplementary Figure 15. Bipolar C-V and G-V curves caused by strong N-doping after Hf precursor soak. a, Bipolar C-V curves with high symmetry. b, Bipolar G-V curves.

(a)

(b)

Supplementary Figure 16. Detailed characterization of the interface morphology in A-CNT MOS structures based on the improved ALD process. a, b, Cross-sectional STEM images showing dielectric thickness and conformality, spacing between CNT clusters or stacks, and a typical magnification image of the CNT cluster or stack in high-density (a) and low-density (b) A-CNT MOS structures after ALD improvement. Compared with the well-arranged monolayer A-CNT morphology shown in Supplementary Figure 1, A-CNT arrays after the device fabrication show stronger morphology variations despite the dielectric morphology has been improved. In high-density samples, the morphology variation mainly reflects as CNT agglomeration and tube pitch variation. In low-density samples, however, nearly all CNTs are directly contacted with adjacent CNTs and stacked into the bundles, thus having much smaller but uniform tube-to-tube distance (close to the Van der Waals distance between CNTs), and inevitably suffered from the electrostatic screening effect.

Supplementary Note 3 Modelling process of A-CNT MOS structures

Supplementary Figure 17. Modelling process of A-CNT MOS structures, mainly including four parts: extraction and analysis of electrostatic parameters, extraction and analysis of dynamic charge traps, evaluation of the overall electrical quality, and ideal performance simulation.

The electrostatics, including potential analysis and the charge statistics, are first evaluated since they directly affect device performance and provide necessary information for analyzing charge traps, such as ET. The potential analysis focuses on the surface potential φs (i.e., EF/q) of the A-CNT channel and FLE, which reflects the gate control efficiency without SCEs. The mid-gap voltage (Vmid-gap) can be experimentally determined by plotting (1/C)2 versus Vg and finding the minimum point of its second-order derivative11 (see Supplementary Fig. 18). The oxide capacitance (Cox) can be estimated by analytic formulas for two extreme morphologies12 (see Supplementary Fig. 19). Based on Vmid-gap, Cox, and CLF, the Berglund method is conveniently used to obtain φs and FLE curves for A-CNT MOS structures13. For the charge statistics, a more accurate capacitance integration method14 to assess both free carriers and trapped charges is now available for A-CNT MOS structures for the first time. Since MOS electrostatics are always related to the basic electronic properties of channel materials, we also extract the channel Cq through a capacitance network model (see Supplementary Fig. 20), aiming to provide some physical insights into the differences between ideal and realistic A-CNT arrays.

Specifically, the mid-gap voltage was determined by a graphical method, and Cox was estimated as 1.2× the maximum high-frequency capacitance, which was systematically located in the range between the plate capacitor model and MCC capacitor model values. The average φs over the entire channel area was calculated from13 , which neglected complicated localized surface potential variations. The FLE was calculated from . Cit approximately equalled , and Cq was roughly extracted from  or  according to the effective capacitance network. The free carrier density Nq was calculated from . The total charge density Ntotal was calculated from . The trapped charge density Ntrapped was calculated from. To provide an intuitive understanding, we also transformed the absolute values of Ntrapped to relative ratios (Ntrapped ratio = Ntrapped/Ntotal). General trends and magnitudes of charge statistics can be analysed with high fidelity as long as Dit is not very large. Device F, however, has a minimum Dit larger than 5 × 1012 cm−2eV−1; thus, the use of this method is not suitable.

Based on electrostatic analyses, the energy-dependent charge trap density can be quantitatively calculated through the high-low frequency (HFLF) method and conductance method9,15. The HFLF method, which is susceptible to shallow oxide traps with a maximum depth of approximately 1.5 nm (see Supplementary Fig. 21), is used here to estimate the near-interface trap density (Dt) instead of Dit, keeping consistent with A-CNT MOS physics. In depletion, Dt serves as a reliable reference to verify Dit, whereas in accumulation, Dt possibly incorporates some shallow oxide traps and differs from Dit, providing a quick examination of the dominant charge trapping mechanism. Meanwhile, the conductance method is adopted to strictly extract Dit based on G-V data and is modified for time constants (τit) and capture cross sections (σ) (see Supplementary Note 4 for theoretical discussions). For border traps (Nbt), a distributed equivalent circuit model10 is modified to cover both interface states and oxide traps (see Supplementary Note 5 for model details), giving a better fitting effect (see Supplementary Fig. 22) and thus a reliable extraction of the effective activated Nbt. Through extraction and analyses of Dit, Dt, and Nbt, the physical origin of charge traps in A-CNT MOS structures can be revealed and elucidated. The modelling process can be used as a universal process to comprehensively analyse the interface trap state for other low-dimensional semiconductor-based MOS systems.

Specifically, the conductance method was used to extract Dit, τit, and σ. First, the normalized conductance under every bias and every frequency was calculated from , in which ω was the circular frequency. With the formula , the magnitudes of the normalized conductance represent the trap response strength. Thus, Dit and τit were calculated from  and  under the assumption that the trap energy levels follow a quasicontinuous distribution, which works well in most circumstances9,15. The theoretical formula of τit in this work was extended into the valence band, described by  when and  when , where σ was the capture cross section, vT was the carrier thermal velocity, and Nq was the free carrier density. To verify the Dit extraction and check if there was any dominant trapping mechanism other than interface states, the HFLF method was used to calculate Dt from . To quantitively evaluate slow charge traps, the time constants of border traps (τbt) were simulated as , and the differential trap admittance was modelled as , where f0 was the Fermi-Dirac distribution function, κ was the tunnelling attenuation coefficient, and x was the tunnelling distance. The differential equation  was established based on the distributed equivalent circuit model10 and numerically solved with the boundary condition, where Yit was the interface state admittance. Nbt was extracted from the best fitting of simulated admittance data  to experimental admittance data . Since device F (E) has a too fast (slow) τit, their Nbt extractions have large errors and are thus unavailable.

(a)

(b)

(c)

Supplementary Figure 18. Determination of the mid-gap Voltage. a, Bipolar C-V curves with high symmetry through N-doping. b, The (Cox/Cm)2 curve and its first order derivative. c, The second-order derivative of (Cox/Cm)2 curve.

Vmid-gap is affected by multiple factors, mainly including metal/semiconductor work function difference, interface states, border traps, and fixed charges. Thus, it is difficult to model Vmid-gap through an analytical formula. Besides, the discrete nature of energy bands of A-CNT arrays further complicates the situation. Thus, a graphical method directly determining Vmid-gap from experimental C-V data is more appropriate for A-CNT MOS structures. By plotting (1/Cm)2 or (Cox/Cm)2 versus Vg and finding the minimum point of its second-order derivative11,16, Vmid-gap can be extracted, about 0.5 V for example in Supplementary Figure 18. Theoretically, Cm used in this method can be either high or low frequencies, if Dit near the mid-gap changes not too fast. However, by forming P-type A-CNT MOS structures, large series resistance caused by the electron Schottky barrier leads to a frequency dispersion in inversion region. Thus, a low-frequency C-V curve is more suitable to extract Vmid-gap because of its relatively high fidelity near the mid-gap.

Supplementary Figure 19. Estimation of the oxide capacitance Cox.

An overestimation of Cox leads to an overestimation of φs and an underestimation of Dit towards valance band, while the underestimation of Cox leads to the opposite results. Since Cox is highly correlated to the morphology of both A-CNT arrays and oxide dielectric, independent measurement of Cox is impossible for A-CNT MOS structures. Besides, due to nonlinear Cq and complicated relationship between Cox and oxide thickness or dielectric constant12, Cox values traditionally obtained by linearly fitting Cm curves or extrapolating 1/Cm curves with oxide thickness are also misleading. Fortunately, the theoretical formulas of Cox under two extreme interface morphologies, i.e., plate capacitor formula for 2D flat interface and multiple-cylindrical-channel (MCC) capacitor formula12 for periodic omega-shape interface, provide us an effective estimation method. In Supplementary Figure 19, by setting a practical lower limit (1 × Cm_max), an ideal lower limit (plate capacitor), a practical upper limit (1.3 × Cm_max) and an ideal upper limit (MCC capacitor), the range and intermediate value (empirically 1.2 × Cm_max) of Cox can be restricted and determined. Although there is still a certain degree of Cox estimation error, it can be regarded as a stable systematic error and does not affect the comparison between MOS structures. More accurate modeling of Cox is necessary but involves complex electrostatic modeling of nanoscale interface morphology, thus out of the scope of this work.

Supplementary Figure 20. The effective capacitance network of A-CNT MOS structures.

Quantum capacitance Cq can be roughly extracted from Eq. .

This method accompanies with a systematic variation firstly introduced in Cox, and Cq could be overall underestimated or overestimated a little, thus we do not draw any conclusion about Cq magnitudes. However, by comparing Cq between different devices with different array density and morphologies, general trends and patterns of Cq can be discussed without any doubt.

(a)

(b)

Supplementary Figure 21. Determination of the maximum depth of shallow oxide traps captured by the HFLF method. a, Tunneling time constants and b, Characteristic frequencies for oxide traps with different distribution depth.

As will be discussed in Supplementary Note 4, tunneling time constants for oxide traps can be calculated considering the time constant of accumulation interface states and oxide material properties. Using first-order approximation and neglect the Fermi distribution function, we can derive an estimation of tunneling time constants. As shown in Supplementary Figure 21a, oxide traps with depth of 3 nm need tens of seconds to trap and de-trap which is comparable to the measurement time, thus 3 nm represents the approximate spatial limit of active border traps. As shown in Supplementary Figure 21b, oxide traps with depth of about 1.5 nm reach to the lower limit (1 kHz) of detecting frequencies, thus 1.5 nm represents the approximate spatial limit of detectable near-interface traps. These spatial limits are marked in the band diagram (see Figure 1c).

Supplementary Note 4 Discussion about the conductance method for Dit extraction

The conductance method is traditionally confined to a limited energy range in semiconductor’ s Eg. This confinement is based on two obvious considerations. One is that time constants of interface states very close to or even inside energy bands can be too small to be measured using common instruments like LCR meters, thus the normalized conductance peaks of interface states cannot be observed and fitted. The other is that it is questionable that whether interface states are present in the valence band or conduction band in traditional Si-based MOS systems. In contrast, A-CNT MOS structures have no such worries. First, the possible interface traps caused by dielectric defects can spread over a much wider energy range compared to CNT’s Eg, hence the necessity to discuss interface states in CNT’s valence or conduction band. Furthermore, low DOS nature of CNT makes time constants large enough to be measured, just like some III-V semiconductor based MOS systems17,18. Lower DOS compared to bulk semiconductors also hinders the detection of very slow interface states around the mid-gap, thus only semiconductors with a small Eg are capable to perform a complete analysis at room temperature. CNT has a diameter dependent Eg, which is smaller than 0.6 eV in our case (see Fig. 3f), thus suitable for admittance measurements covering the whole Eg and most of the first sub-bands of CNT.

Based on these justifications, the conductance method is extended to a wider energy range in this work. When dealing with charge traps inside energy bands, theoretical formulation of time constants also needs to be re-examined. According to the Schottky-Read-Hall (SRH) statistics19,20, time constants are exponentially varying with respect to the energy difference between the trap energy level (ET) and band edges. For charge traps inside energy bands, however, there is almost no energy barrier during charge capture and emission processes, thus time constants should solely depend on the capture cross section (σ), carrier thermal velocity (vT), and effective density of states (NV) or free carrier density (Nq), while exponential energy term approximately equals to unity. The EF trace of characteristic frequencies in the normalized conductance map (see Fig. 1g) also supports our analysis, in which fit or τit firstly moves with ET moving, then stays almost unchanged inside the valance band. Integrating two parts together, time constant formulation of hole traps can be re-expressed as Eq. . The electron or acceptor-like traps follow a similar theoretical paradigm.

Based on this extended theoretical formulation and measurement results, σ, another important parameter reflecting the microscopic reaction range of charge traps, can be extracted using Eq.  for the first time in CNT-based electronics.

In Eq. , vT, only related to the effective mass of CNT, can be theoretically calculated21, and accurate τit and Nq can be experimentally extracted in this work.

Supplementary Note 5 The distributed equivalent circuit model for Nbt extraction

Following an elastic tunneling assumption, the time constant of border traps (τbt) at a certain depth away from the interface can be determined by the Fermi-Dirac distribution function (f0), the time constant of interface states in accumulation (τ0), tunneling attenuation coefficient (κ), tunneling effective mass (m*), valance band edge of oxide material (), reduced Planck constant (ℏ), and tunneling distance (x), expressed as Eq. 10.

Since τbt varies exponentially with tunneling distance, border traps’ admittance response can be very different when applied frequency varies. To capture this frequency dependence and to extract border trap density (Nbt) accurately, we use the distributed equivalent circuit model proposed by Yuan et al10. In this model, border traps can be regarded as a series combination of the incremental capacitance ΔCbt (E,x) and conductance ΔGbt (E,x) (equivalent to 1/ΔRbt (E,x)) with both energy and spatial location dependences.

By integrating over the full energy range, total incremental admittance ΔYbt (x) of border traps can be simplified to Eq. .

By further breaking the oxide capacitance into infinite serial segments connected with ΔYbt (x), total admittance can be solved through a differential equation and a boundary condition (see Eq. ).

By numerically fitting the total admittance (Eq. ) to as-measured C-V and G-V curves at different frequencies, Nbt at different voltage biases can be extracted and discussed. In the original model, the boundary condition solely consists of the semiconductor capacitance10, which is not precise in large Dit systems. By incorporating Cq and interface state admittance Yit together, fitting effect can be much better for A-CNT MOS structures. Generally speaking, this method is only valid in accumulation since the tunneling time would be too large to be detected in depletion and involve more inelastic scattering events.

Fitting procedures:

- Given the gate voltage and the corresponding Fermi level, all gate oxide parameters and channel parameters are fixed.

- In strong accumulation, fits C-F and G-F curves at every dc bias.

(a)

(b)

(c)

(d)

Supplementary Figure 22. Fitting effect of the modified distributed equivalent circuit model of border traps. a, C-F fitting only with Nbt, failing to capture the high frequency feature. b, C-F fitting only with Dit, failing to capture the low frequency feature. c, C-F fitting with both Nbt and Dit. d, G-F fitting with both Nbt and Dit. The fitting parameters used here are as following: tox = 8 nm, kox = 10 ~ 11, m* = 0.15·m0, EV_HfO2 = Ei_SiO2 + 3.16 eV, Ei_CNT = Ei_SiO2 + 4.6 eV, EF = Ei_CNT + (0.5 ~ 0.54) eV, κ = 3.212 ~ 3.236 nm-1 , Cq = 0.0537 ~ 0.0595 F/m2, τ0 ≈ 0.1 ~ 0.2 μs, Rs = 150 Ω.

(b)

(a)

(c)

(d)

(e)

(f)

(g)

(h)

(i)

Supplementary Figure 23. As-measured C-V & G-V curves and the corresponding normalized conductance maps of high-density A-CNT MOS structures. a, b, c device F. d, e, f, device A. g, h, i, device B. The 50 frequencies from the top (bottom) curve to the bottom (top) curve of C-V (G-V) data are between 1 kHz and 1 MHz with a logarithmic interval.

(b)

(a)

(c)

(d)

(e)

(f)

(g)

(h)

(i)

Supplementary Figure 24. As-measured C-V & G-V curves and the corresponding normalized conductance map of low-density A-CNT MOS structures. a, b, c, device C. d, e, f, device D. g, h, i, device E. The 50 frequencies from the top (bottom) curve to the bottom (top) curve of C-V (G-V) data are between 1 kHz and 1 MHz with a logarithmic interval.

(b)

(a)

(c)

(d)

(e)

(f)

(g)

(h)

Supplementary Figure 25. Nbt fitting details for device A (a, b), device B (c, d), device C (e, f), and device D (g, h). The circles are experiment data (Cm & Gm), and fitted Gtot is slightly higher than Gm, indicating extracted Nbt represents an upper limit.

Supplementary Table 1 Sample conditions for A-CNT MOS structures.

| Device number | F | A | B |
| --- | --- | --- | --- |
| A-CNT density | ~ 380 CNTs/μm | ~ 380 CNTs/μm | ~ 380 CNTs/μm |
| ALD condition (TDMAH pulse/ N2 /H2O pulse/N2) | (500 ms / 20 s / 200 ms / 20 s) × 56 cycles | H2O-presoak + (500 ms / 20 s / 250 ms / 20 s) × 56 cycles | H2O-presoak + (500 ms / 20 s / 250 ms / 20 s) × 56 cycles |
| Device number | C | D | E |
| A-CNT density | ~ 200 CNTs/μm | ~ 200 CNTs/μm | ~ 200 CNTs/μm |
| ALD condition (TDMAH pulse/ N2 /H2O pulse/N2) | (500 ms / 20 s / 200 ms / 20 s) × 56 cycles | H2O-presoak + (500 ms / 20 s / 250 ms / 20 s) × 56 cycles | H2O-presoak + (500 ms / 20 s / 250 ms / 20 s) × 56 cycles |
| H2O-presoak: (250 ms H2O pulse / 20 s N2 purge) × 20 cycles |  |  |  |

(c)

(b)

(a)

Supplementary Figure 26. Extraction of other electrostatic parameters of A-CNT MOS structures. a, Gate oxide capacitance statistics of 63 devices in total, showing two distinct trends during ALD process improvement. b, The free carrier density (Nq) curves for high-density A-CNT MOS structures. c, The free carrier density (Nq) curves for low-density A-CNT MOS structures.

The improved ALD conditions increase the Cox for high-density devices mainly owing to improvements in both the compactness and conformality of the HfO2 film. For low-density devices, the improved ALD conditions aggravate the agglomeration of A-CNTs (see Supplementary Fig. 16b), which lowers the effective gating area of A-CNTs and then decreases Cox (D and E).

(a)

(b)

Supplementary Figure 27. Extreme samples with very low Rch tuning ratio. a, b, Two typical devices with such large Dit that their Rch, the only parasitic resistance with voltage-dependence included within the Rpara, have very small tuning ratio even below 300%, which should be orders of magnitudes in normal situations.

(a)

(b)

Supplementary Figure 28. The near-interface trap density Dt of A-CNT MOS structures extracted by the high-low frequency method. a, Energy dependent Dt in high-density A-CNT MOS structures (F, A, B). b, Energy dependent Dt in low-density A-CNT MOS structures (C, D, E).

(c)

(d)

(a)

(b)

Supplementary Figure 29. The detailed features of charge traps in A-CNT MOS structures. a, Time constants of interface states or border traps at different energy levels. The black line inside the lower half of the band gap indicates the theoretical time constants of the hole capture-emission process. b, Capture cross-section statistics of 63 devices in total. c, d, Time constants of interface states or border traps in high-density (c) and low-density (d) A-CNT MOS structures.

Since device F (E) has a too fast (slow) τit, their τbt extractions have large errors and are thus unavailable. The τ consists of both quasicontinuous and discretely distributed points; the former conform to surface trapping and SRH statistics22 thus denotes as τit; while the latter conform to tunnelling trapping of border traps23 thus denotes as τbt. τit in device C is much higher and has a steeper slope than that in high-density devices, which is attributed to lower Nq and Eg. With ALD improvement, τit in device D significantly decreases, meaning easier charge trapping, partially offsetting the advantage from the lower Dit.

(a)

(b)

Supplementary Figure 30. Raman spectrum measurements. a, Raman spectrum for high-density A-CNT arrays after annealing and rinsing. b, Raman spectrum for low-density A-CNT arrays after annealing and rinsing.

Supplementary Note 6 Admittance simulation for A-CNT MOS structures

Since A-CNT arrays have both linear DOS fluctuations caused by CNT pitch variations and nonlinear DOS fluctuations caused by electronic interactions between adjacent CNTs, the interface morphology of A-CNT MOS structures has complicated mesoscopic disorders, and the dielectric constant of quasi two-dimensional A-CNT arrays is unknown yet, it is difficult to directly solve the Poisson equation between channel charges and the surface potential. Therefore, we have established an equivalent circuit model of A-CNT MOS structures, as described in Supplementary Figure 3. Through analyzing this admittance/impedance network, we can simultaneously simulate the electrostatic parameters (surface potential, free carriers and trapped charges) and dynamic parameters (Dit, Nbt). The model simulation and analysis mainly include two steps: 1. Calibrate the model with experimental parameters, and obtain basically consistent data as experimental results (see Supplementary Fig. 31 for comparison); 2. Simulate process optimization to reduce interface states and border traps, analyze changes of key physical quantities, and predict ideal device performance (see Fig. 4c-e and Supplementary Fig. 32). Specifically, the admittance simulation consists of dc simulation and ac simulation. When performing multifrequency measurement at each voltage point, the scanning delay time is enough to ensure that the A-CNT MOS structure enter the equilibrium state, so the dc characteristic of C-V curves is independent of ac signal frequency. Therefore, a frequency-independent dc simulator is established based on Eq. .

By pre-setting Vmid-gap, Cox, Cq, and Dit, we can calculate φs and Nq curves, which provides basic information for ac simulation. On this basis, only by expanding Cit to a frequency varying Yit, and by solving the ODE equation for border traps, multi-frequency C-V and G-V curves can be simulated from Eq. .

The AC simulator can be expressed as following pseudocodes:

(e)

(a)

(b)

(f)

(c)

(g)

(d)

(h)

Supplementary Figure 31. Calibration for admittance simulations. a-d, simulated and e-h, experimental C-V (a, e), G-V (b, f), φs (c, g) and Nq (d, h) curves. Simulation results are highly resembling to experiment results, proving model validity. Simulation parameters: minimum Dit of 5 × 1012 cm-2eV-1, maximum Dit of 5 × 1013 cm-2eV-1, and average Nbt of 4 × 1019 cm-3eV-1. Experiment results: minimum Dit of 4.2 × 1012 cm-2eV-1, maximum Dit of 3.7 × 1013 cm-2eV-1, and average Nbt of 5.1 × 1019 cm-3eV-1.

(b)

(a)

(c)

(d)

(e)

(f)

(g)

(h)

(i)

(j)

(k)

(l)

Supplementary Figure 32. Simulation details. a-e, pre-set parameters, including ideal Cq of A-CNT arrays (a); averaged Cox of baseline and CET improved condition (b); theoretical τit according to SRH model (c); Dit of baseline and improved condition (d); Nbt of baseline and improved condition (e); f-l, simulated results as supplementary contents to Fig. 4c-d, including φs curves of three conditions (f); G-V curves of baseline condition (g); G-V curves of traps improved condition (h); G-V curves of both traps and CET improved condition (i); Nq curves of baseline condition (j); Nq curves of traps improved condition (k); C-V curves of traps improved condition (l);

Supplementary Table 2 The energy-efficiency comparison.

|  | Limit24 | Si CMOS (10 nm, 0.7 V)24 | s-CNT FET (10 nm, 0.4 V)24 | A-CNT FET (10 nm, 0.65 V) |
| --- | --- | --- | --- | --- |
| Gate delay (fs) | 40 | 220 | 57 | 87 |
| EDP (Js/μm) | / | 6.79 × 10-29 | 1.88 × 10-30 | 7.4 × 10-30 |

Supplementary Figure 33. CET measurement for 90 cycles HfO2 using the 250 °C ALD process. For three devices each, measured C-V curve at 1 MHz shows a maximum normalized capacitance of 1.27 μF/cm2 in the A-CNT MOS structure and an average normalized capacitance of 1.5 μF/cm2 in the metal-insulator-metal (MIM) structure, both indicating a CET about 2.3 nm. Thus, for 80 cycles (about 8 nm) HfO2 used in A-CNT MOSFETs shown in Fig. 5, the CET is approximately about 2 nm if following a linear scaling trend.

(a)

(b)

(c)

(d)

(e)

(f)

(g)

(h)

(i)

(j)

(k)

(l)

Supplementary Figure 34. Electrical properties of A-CNT FETs with 150 nm Lg. a, Transfer curves, b, output curves and c, Vth (Vds = -0.7 V) extracted by linear fitting method of the same device shown in Fig. 5a. d, g, j, Transfer curves, e, h, k, output curves and f, i, l, Vth (Vds = -0.65/-0.7/-0.7 V) extracted by linear fitting method of another three A-CNT FETs with 150 nm Lg.

(a)

(b)

(c)

(e)

(f)

(d)

(g)

(h)

(i)

Supplementary Figure 35. Electrical properties of A-CNT FETs with 90 nm Lg. a, Transfer curves, b, output curves and c, Vth (Vds = -0.7 V) extracted by linear fitting method of the same device shown in Fig. 5b. d, g, Transfer curves, e, h, output curves and f, i, Vth (Vds = -0.7 V) extracted by linear fitting method of another two A-CNT FETs with 90 nm Lg.

(a)

(c)

(b)

Supplementary Figure 36. Rc extraction for A-CNT FETs with 90 nm Lg. a, Output curves showing the minimum total resistance (Rtot = 360 Ω·μm). b, Output curves showing the maximum total resistance (Rtot = 450 Ω·μm). c, I-V curves of 10 devices with shorted source and drain electrodes, containing parasitic resistances (Rpara = 120 Ω·μm) from metal electrodes, connect lines and pads. Since Rtot = 2Rc + Rch + Rpara, contact resistance Rc can be as low as 120 Ω·μm when ignoring channel resistance Rch in A-CNT FETs working under the quasi-ballistic transport.

(a)

(b)

(c)

(d)

Supplementary Figure 37. SEM images showing structures of A-CNT FETs. a, The A-CNT FET with Lg ≈ 150 nm. b, The A-CNT FET with Lg ≈ 90 nm. c, The A-CNT FET with Lch ≈ 95 nm. d, The same A-CNT FET shown in (c) with Lsp ≈ 15 nm.

(a)

(b)

Supplementary Figure 38. Electrical properties of the A-CNT FET with 80 nm Lg and 15 nm Lsp. a, output curves and b, Vth (Vds = -0.7 V) extracted by linear fitting method of the same device shown in Fig. 5c.

Supplementary Figure 39. Schematic of A-CNT MOS interface challenges.

Five interrelated interface challenges in A-CNT MOS structures are summarized according to the interface depth and degree of localization. First, morphology disorder of A-CNT arrays is found throughout the entire channel area, regardless of whether it is caused by A-CNT assembly defects or various film-forming stresses. Nonuniform surface morphology and reactivity directly degrade electrostatic properties and complicate ALD growth. Second, activated border traps with an interface depth up to 3 nm severely deteriorate the stability and reliability by enhancing the hysteresis, bias-temperature instability (BTI) effects, and gate leakage in MOS devices. Third, oxide structural defects in intimate contact with CNTs very likely contribute to Dit. Fourth, the residual π-bonding polymer from CNT preparation partially covers the CNT surface (see Supplementary Fig. 40), either increasing Dit and charge transferring or serving as initial nucleation sites for ALD growth. Fifth, random fixed charges at the atomic scale will cause φs and VT variations between multiple CNTs and degrade the SS25. Depending on the distance between EF and ET, interface states and fixed charges can also interconvert into each other; thus, systematic optimization is required26. These interface challenges are universally faced by all low-dimensional semiconductor-based FETs, thus requiring continuous and in-depth research on post-Moore electronics.

Supplementary Figure 40. High Resolution TEM image illustrating polymer residuals on the CNT surface. The CNT was dispersed and suspended onto the micro grid to get a clear image, and polymer residuals seem to partially wind around the CNT.

Supplementary Table 3 The benchmarking details of Dit and Nbt.

| Gate Stack | Dit (cm-2eV-1) | Extraction method and Ref. | Nbt (cm-3eV-1) | Extraction method and Ref. |
| --- | --- | --- | --- | --- |
| Si/SiO2 | 1E9 | DLTS (C-V) 27 | 1E15 | Charge-pumping 28 |
|  | 2E9 | ESR 29 | 5E15 ~ 1E17 | C-V 30 |
| Si/SiO2/High-κ |  |  | 2E17 | Charge-pumping 31 |
|  |  |  | 4E17 ~ 4E18 | Charge-pumping 32 |
| Si/High-κ | 2E10 | Conductance (C-V & G-V) 33 | 1E19 ~ 1E20 | Charge-pumping 28 |
|  | 3E11 | DLTS (C-V) 34 |  |  |
|  | 4.1E11 | DLTS (C-V) 35 |  |  |
| Ge/GeO2 | 6E10 | Conductance (C-V & G-V)36 |  |  |
|  | 3E11 | Conductance (C-V & G-V) 37 |  |  |
| Ge/Ge2O3/High-κ |  |  | 2E19 | C-V & G-V 38 |
|  |  |  | 3E19 | C-V & G-V 39 |
| InGaAs/High-κ | 2E12 | C-V 40 | 2.2E19 ~ 4.2E19 | C-V & G-V 10 |
|  | 5E11 ~ 5E12 | Conductance (C-V & G-V) 18 | 2E19 | C-V & G-V 41 |
|  | 5E11 | Conductance (C-V & G-V) 42 |  |  |
| InP/High-κ |  |  | 1E20 | C-V & G-V 41 |
| MoS2/Al2O3 | 2.4E12 | C-V 43 | 7.7E19 | 1/f noise 44 |
|  | 1.2E12 | C-V 45 | 2.3E19 | C-V & G-V 46 |
| MoS2/Y2O3 | 8E11 | C-V 47 |  |  |
| MoS2/HfO2 | 2E12 ~ 5E12 | Conductance (C-V & G-V) 48-50 | 3.2E20 | C-V & G-V 51 |
|  | 7E11 | C-V 52 |  |  |
| MoS2/PTCDA | 8E11 | C-V 53 |  |  |
| MoS2/CaF2 | 1.2E13 | SS equation 54 |  |  |
| CNT/Y2O3 | 1.04E13 | SS equation 55 |  |  |
|  | 4.63E12 | C-V 56 |  |  |
| CNT/LaOx | 1.68E13 | SS equation 57 |  |  |
| High-density A-CNT/HfO2 | 6.1E11 | Conductance (C-V & G-V) | 7E19 | C-V & G-V |
| Low-density A-CNT/HfO2 | 8.78E11 | Conductance (C-V & G-V) | 4.5E19 | C-V & G-V |

Supplementary Table 3 The benchmarking details of MOSFETs.

|  | Lg (nm) | ¦Vds¦ (V) | Ion (μA/μm) PMOS/ NMOS | gm (μS/μm) PMOS/ NMOS |
| --- | --- | --- | --- | --- |
| This work | 90 | 0.5 | 1205 | 1155 |
| This work | 90 | 0.7 | 1651 | 1692 |
| This work | 90 | 1 | 2242 | 2433 |
| This work | 150 | 0.5 | 916 | 1075 |
| This work | 150 | 0.7 | 1200 | 1334 |
| This work | 150 | 1 | 1394 | 1705 |
| A-CNT Ref.1 | 100 | 1 | 1300 | 900 |
| A-CNT Ref.3 | 85 | 0.9 | 1920 | 1400 |
| A-CNT Ref.58 | 85 | 0.8 | 1910 | 1640 |
| Si 32nm Ref.59 | 30 | 1 | 1210/1550 | 2200/3000 |
| Si 45nm Ref.60 | 35 | 1 | 1070/1360 | 1220/2120 |
| Si 65nm Ref.61 | 35 | 1.2 | 880/1460 | 1000/1600 |
| Si 90nm Ref.62 | 50 | 1.2 | 700/1260 | 685/1330 |
| Si 130nm Ref.63 | 70 | 1.3 | 600/1170 | 635/1200 |
| Si 180nm Ref.64 | 130 | 1.5 | 420/940 | 430/860 |
| Si 250nm Ref.65 | 200 | 1.8 | 350/755 | 260/550 |
| Si 350nm Ref.66 | 350 | 2.5 | 320/640 | 190/380 |

References

1	Liu, L. et al. Aligned, high-density semiconducting carbon nanotube arrays for high-performance electronics. Science 368, 850-856 (2020).

2	Zhang, Z. et al. Doping-free fabrication of carbon nanotube based ballistic CMOS devices and circuits. Nano Lett. 7, 3603-3607 (2007).

3	Shi, H. et al. Radiofrequency transistors based on aligned carbon nanotube arrays. Nat. Electron. 4, 405-415 (2021).

4	Lin, Y. et al. Enhancement-Mode Field-Effect Transistors and High-Speed Integrated Circuits Based on Aligned Carbon Nanotube Films. Adv. Funct. Mater. 32, 2104539 (2022).

5	Sato, M. et al. Study of a Negative Threshold Voltage Shift in Positive Bias Temperature Instability and a Positive Threshold Voltage Shift the Negative Bias Temperature Instability of Yttrium-Doped HfO2 Gate Dielectrics. Jpn. J. Appl. Phys. 49, 04DC24 (2010).

6	Jin, J. W. et al. Interpreting anomalies observed in oxide semiconductor TFTs under negative and positive bias stress. AIP Adv. 6, 085321 (2016).

7	Lin, D. H. C. et al. Beyond Silicon MOS: An Electrical Study on Interface and Gate Dielectrics with ac Admittance Techniques. In Mater. Sci. Technol.     1-16.

8	Yu, B. et al. Effect and extraction of series resistance in Al2O3-InGaAs MOS with bulk-oxide trap. Electron. Lett. 49, 492-493 (2013).

9	Nicollian, E. H. & Brews, J. R. MOS (metal oxide semiconductor) physics and technology.  (John Wiley & Sons, 2002).

10	Yuan, Y. et al. A Distributed Bulk-Oxide Trap Model for Al2O3 InGaAs MOS Devices. IEEE Trans. Electron Devices 59, 2100-2106 (2012).

11	Winter, R., Ahn, J., McIntyre, P. C. & Eizenberg, M. New method for determining flat-band voltage in high mobility semiconductors. Journal of Vacuum Science & Technology B 31, 030604 (2013).

12	Deng, J. & Wong, H. P. Modeling and Analysis of Planar-Gate Electrostatic Capacitance of 1-D FET With Multiple Cylindrical Conducting Channels. IEEE Trans. Electron Devices 54, 2377-2385 (2007).

13	Berglund, C. N. Surface states at steam-grown silicon-silicon dioxide interfaces. IEEE Trans. Electron Devices ED-13, 701-705 (1966).

14	Taoka, N. et al. Impact of Fermi level pinning inside conduction band on electron mobility of InxGa1− xAs MOSFETs and mobility enhancement by pinning modulation. In 2011 International Electron Devices Meeting. 27.22. 21-27.22. 24 (IEEE, 2011).

15	Wang, S. & Wang, X. MOS Interface Physics, Process and Characterization.  (CRC Press, 2021).

16	R. J. Hillard, J. M. H., D. A. Zier, P. Rai-Choudhury, D. K. Schroder. Direct and Rapid Method for Determining Flatband Voltage from Non-equilibrium Capacitance Voltage Data. In Diagnostic Techniques for Semiconductor Materials and Devices. 261–274 (Electrochem. Soc.).

17	Taoka, N. et al. AC response analysis of C–V curves and quantitative analysis of conductance curves in Al2O3/InP interfaces. Microelectron. Eng. 88, 1087-1090 (2011).

18	Engel-Herbert, R., Hwang, Y. & Stemmer, S. Comparison of methods to quantify interface trap densities at dielectric/III-V semiconductor interfaces. J. Appl. Phys. 108, 124101 (2010).

19	Brammertz, G. et al. Characteristic trapping lifetime and capacitance-voltage measurements of GaAs metal-oxide-semiconductor structures. Appl. Phys. Lett. 91, 133510 (2007).

20	Shockley, W. & Read Jr, W. Statistics of the recombinations of holes and electrons. Physical review 87, 835 (1952).

21	Xu, L., Qiu, C., Zhao, C., Zhang, Z. & Peng, L. M. Insight Into Ballisticity of Room-Temperature Carrier Transport in Carbon Nanotube Field-Effect Transistors. IEEE Trans. Electron Devices PP, 1-6 (2019).

22	Lin, H. C. et al. The Fermi-level efficiency method and its applications on high interface trap density oxide-semiconductor interfaces. Appl. Phys. Lett. 94, 153508 (2009).

23	Babadi, A. S., Lind, E. & Wernersson, L. E. Modeling of n-InAs metal oxide semiconductor capacitors with high-κ gate dielectric. J. Appl. Phys. 116, 214508 (2014).

24	Qiu, C. et al. Scaling carbon nanotube complementary transistors to 5-nm gate lengths. Science 355, 271-276 (2017).

25	Cao, Q. et al. Origins and Characteristics of the Threshold Voltage Variability of Quasiballistic Single-Walled Carbon Nanotube Field-Effect Transistors. ACS Nano 9, 1936-1944 (2015).

26	Knobloch, T. et al. Improving stability in two-dimensional transistors with amorphous gate oxides by Fermi-level tuning. Nat. Electron. 5, 356-366 (2022).

27	Eades, W. D. & Swanson, R. M. Calculation of surface generation and recombination velocities at the Si‐SiO2 interface. J. Appl. Phys. 58, 4267-4276 (1985).

28	Jakschik, S., Avellan, A., Schroeder, U. & Bartha, J. W. Influence of Al2O3 dielectrics on the trap-depth profiles in MOS devices investigated by the charge-pumping method. IEEE Trans. Electron Devices 51, 2252-2255 (2004).

29	Reed, M. L. & Plummer, J. D. Chemistry of Si‐SiO2 interface trap annealing. J. Appl. Phys. 63, 5776-5793 (1988).

30	Fleetwood, D. M. et al. Border traps: Issues for MOS radiation response and long-term reliability. Microelectron. Reliab. 35, 403-428 (1995).

31	Son, Y., Park, S., Kang, T., Oh, B. & Shin, H. Characterization of Border Trap Density With the Multifrequency Charge Pumping Technique in Dual-Layer Gate Oxide. IEEE Trans. Electron Devices 58, 2752-2758 (2011).

32	Lu, C. Y., Chang-Liao, K. S., Tsai, P. H. & Wang, T. K. Depth Profiling of Border Traps in MOSFET With High-κ Gate Dielectric by Charge-Pumping Technique. IEEE Electron Device Lett. 27, 859-862 (2006).

33	Manchanda, L. et al. Gate quality doped high K films for CMOS beyond 100 nm: 3-10 nm Al2O3 with low leakage and low interface states. In International Electron Devices Meeting 1998. Technical Digest (Cat. No.98CH36217). 605-608 (IEEE, 1998).

34	Dueñas, S. et al. The electrical-interface quality of as-grown atomic-layer-deposited disordered HfO2 on p- and n-type silicon. Semicond. Sci. Technol. 19, 1141-1148 (2004).

35	Jeon, I. S. et al. Post-Annealing Effects on Fixed Charge and Slow/Fast Interface States of TiN/Al2O3/p-Si Metal–Oxide–Semiconductor Capacitor. Jpn. J. Appl. Phys. 42, 1222-1226 (2003).

36	Fukuda, Y., Ueno, T., Hirono, S. & Hashimoto, S. Electrical Characterization of Germanium Oxide/Germanium Interface Prepared by Electron-Cyclotron-Resonance Plasma Irradiation. Jpn. J. Appl. Phys. 44, 6981-6984 (2005).

37	Kuzum, D. et al. Ge-Interface Engineering With Ozone Oxidation for Low Interface-State Density. IEEE Electron Device Lett. 29, 328-330 (2008).

38	Simoen, E. et al. Border Traps in Ge/III–V Channel Devices: Analysis and Reliability Aspects. IEEE Trans. Device Mater. Reliab. 13, 444-455 (2013).

39	Lin, D. et al. Beyond interface: The impact of oxide border traps on InGaAs and Ge n-MOSFETs. In 2012 International Electron Devices Meeting. 28.23.21-28.23.24 (IEEE, 2012).

40	Suzuki, R. et al. 1-nm-capacitance-equivalent-thickness HfO2/Al2O3/InGaAs metal-oxide-semiconductor structure with low interface trap density and low gate leakage current density. Appl. Phys. Lett. 100, 132906 (2012).

41	Heyns, M. et al. Advancing CMOS beyond the Si roadmap with Ge and III/V devices. In 2011 International Electron Devices Meeting. 13.11.11-13.11.14 (IEEE, 2011).

42	Hwang, Y., Engel-Herbert, R., Rudawski, N. G. & Stemmer, S. Analysis of trap state densities at HfO2/In0.53Ga0.47As interfaces. Appl. Phys. Lett. 96, 102910 (2010).

43	Liu, H. & Ye, P. D. MoS2 Dual-Gate MOSFET With Atomic-Layer-Deposited Al2O3 as Top-Gate Dielectric. IEEE Electron Device Lett. 33, 546-548 (2012).

44	Li, X. et al. Effect of Dielectric Interface on the Performance of MoS2 Transistors. ACS Appl. Mater. Interfaces 9, 44602-44608 (2017).

45	Wu, X. et al. Dual gate synthetic MoS2 MOSFETs with 4.56µF/cm2 channel capacitance, 320µS/µm Gm and 420 µA/µm Id at 1V Vd/100nm Lg. In 2021 IEEE International Electron Devices Meeting (IEDM). 7.4.1-7.4.4 (IEEE, 2021).

46	Zhao, P. et al. Understanding the Impact of Annealing on Interface and Border Traps in the Cr/HfO2/Al2O3/MoS2 System. ACS Appl. Electron. Mater. 1, 1372-1377 (2019).

47	Fang, N. & Nagashio, K. Band tail interface states and quantum capacitance in a monolayer molybdenum disulfide field-effect-transistor. J. Phys. D: Appl. Phys. 51, 065110 (2018).

48	Gaur, A. et al. Demonstration of 2e12cm−2eV−1 2D-oxide interface trap density on back-gated MoS2 flake devices with 2.5nm EOT. Microelectron. Eng. 178, 145-149 (2017).

49	Gaur, A. et al. Analysis of admittance measurements of MOS capacitors on CVD grown bilayer MoS2. 2D Mater. 6, 035035 (2019).

50	Gaur, A. et al. A MOS capacitor model for ultra-thin 2D semiconductors: the impact of interface defects and channel resistance. 2D Mater. 7, 035018 (2020).

51	Zhao, P. et al. Evaluation of border traps and interface traps in HfO2 MoS2 gate stacks by capacitance–voltage analysis. 2D Mater. 5, 031002 (2018).

52	Xia, P. et al. Impact and Origin of Interface States in MOS Capacitor with Monolayer MoS2 and HfO2 High-κ Dielectric. Sci. Rep. 7, 40669 (2017).

53	Li, W. et al. Uniform and ultrathin high-κ gate dielectrics for two-dimensional electronic devices. Nat. Electron. 2, 563-571 (2019).

54	Illarionov, Y. Y. et al. Ultrathin calcium fluoride insulators for two-dimensional field-effect transistors. Nat. Electron. 2, 230-235 (2019).

55	Ding, L., Zhang, Z., Su, J., Li, Q. & Peng, L.-M. Exploration of yttria films as gate dielectrics in sub-50 nm carbon nanotube field-effect transistors. Nanoscale 6, 11316-11321 (2014).

56	Xu, L., Gao, N., Zhang, Z. & Peng, L.-M. Lowering interface state density in carbon nanotube thin film transistors through using stacked Y2O3/HfO2 gate dielectric. Appl. Phys. Lett. 113, 083105 (2018).

57	Franklin, A. D., Bojarczuk, N. A. & Copel, M. Consistently low subthreshold swing in carbon nanotube transistors using lanthanum oxide. Appl. Phys. Lett. 102, 013108 (2013).

58	Lin, Y. et al. Scaling aligned carbon nanotube transistors to a sub-10 nm node. Nat. Electron. 6, 506-515 (2023).

59	Natarajan, S. et al. A 32nm logic technology featuring 2nd-generation high-k + metal-gate transistors, enhanced channel strain and 0.171μm2 SRAM cell size in a 291Mb array. In 2008 IEEE International Electron Devices Meeting. 1-3 (IEEE, 2008).

60	Mistry, K. et al. A 45nm Logic Technology with High-k+Metal Gate Transistors, Strained Silicon, 9 Cu Interconnect Layers, 193nm Dry Patterning, and 100% Pb-free Packaging. In 2007 IEEE International Electron Devices Meeting. 247-250 (IEEE, 2007).

61	Bai, P. et al. A 65nm logic technology featuring 35nm gate lengths, enhanced channel strain, 8 Cu interconnect layers, low-k ILD and 0.57 /spl mu/m/sup 2/ SRAM cell. In IEDM Technical Digest. IEEE International Electron Devices Meeting, 2004. 657-660 (IEEE, 2004).

62	Ghani, T. et al. A 90nm high volume manufacturing logic technology featuring novel 45nm gate length strained silicon CMOS transistors. In IEEE International Electron Devices Meeting 2003. 11.16.11-11.16.13 (IEEE, 2003).

63	Tyagi, S. et al. A 130 nm generation logic technology featuring 70 nm transistors, dual Vt transistors and 6 layers of Cu interconnects. In International Electron Devices Meeting 2000. Technical Digest. IEDM (Cat. No.00CH37138). 567-570 (IEEE, 2000).

64	Yang, S. et al. A high performance 180 nm generation logic technology. In International Electron Devices Meeting 1998. Technical Digest (Cat. No.98CH36217). 197-200 (IEEE, 1998).

65	Brand, A. et al. Intel’s 0.25 micron, 2.0 volts logic process technology. Intel Technology Journal Q 3, 1998 (1998).

66	Bohr, M. et al. A high performance 0.35/spl mu/m logic technology for 3.3 V and 2.5 V operation. In Proceedings of 1994 IEEE International Electron Devices Meeting. 273-276 (IEEE, 1994).