Supporting Information

Hydroxyl-rich KIr4O8 Nanowires Promote Acidic Water Oxidation Electrocatalysis with Industrial Current Density

Zhenyu Li,1 Xiang Li,1,2 Pengfei Wei,1 Ziqi Liao,1,3 Mengna Wang,1,2 Jingcheng Yu,1,3 Fang Lu,1 Tianfu Liu,1 Guoxiong Wang*,1

1State Key Laboratory of Catalysis, Dalian National Laboratory for Clean Energy, iChEM (Collaborative Innovation Center of Chemistry for Energy Materials), Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian, 100039, China

2College of Environmental and Chemical Engineering, Dalian Jiaotong University, Dalian, 116028, China

3College of Energy, University of Chinese Academy of Sciences, Beijing, 100039, China

Corresponding author

- mail: wanggx@dicp.ac.cn (G. Wang)

## Fig. S1 XRD pattern of IrO2 catalyst.

## Fig. S2 SEM image of IrO2 catalyst.

## Fig. S3 (a-b) HRTEM images of IrO2 catalyst.

## Fig. S4 TGA-MS curves of KIr4O8 and IrO2 catalysts.

## Fig. S5 (a) K 2p XPS spectrum of KIr4O8 catalyst. (b) O 1s XPS spectra of IrO2 and KIr4O8 catalysts.

## Fig. S6 (a-b) Cyclic voltammograms of KIr4O8 and IrO2 catalysts in the potential region of 0.7-0.9 V vs. RHE at various scan rates.

## Fig. S7 Faradaic efficiency of KIr4O8 catalyst at 20 mA/cm2 toward the OER.

## Fig. S8 Leached amount of Ir from KIr4O8 catalyst during OER electrocatalysis for 10 h in 0.5 M H2SO4.

## Fig. S9 (a-b) XRD pattern and HRTEM image of KIr4O8 after stability test toward the OER.

## Fig. S10 Cyclic voltammograms of IrO2 and KIr4O8 catalysts recorded at the scan rate of 1 mV/s in 0.5 M H2SO4.

## Fig. S11 Pulse voltammetry measurements and corresponding current responses for KIr4O8 and IrO2 catalysts.

## Fig. S12 DEMS signals of O2 products for 18O-labeled IrO2 catalyst in 0.5 M H2SO4 with H216O.

## Fig. S13 Electron paramagnetic resonance spectra of IrO2 and KIr4O8 catalysts in DMPO solution.

## Fig. S14 Theoretical models for IrO2 (110) and KIr4O8 (010).

## Fig. S15 Gibbs free energy diagram of lattice oxygen mechanism for KIr4O8.

## Fig. S16 Schematic explanation for the relative distance between the Ir d band center and oxygen 2p (O 2p) band center in KIr4O8.

## Fig. S17 Integrated crystal orbital Hamilton population (ICOHP) curves of OH bond covered on IrO2.

## Fig. S18 Charge density difference of OH covered on IrO2 and KIr4O8 models.

## Table S1. Comparison of OER performance of KIr4O8 with some representative Ir-based catalysts in acidic media.

| Catalysts | Loading amount (mg/cm2) | Overpotential at 10 mA/cm2 (mV) | Scan rate (mV/s) | Stability | Electrolyte | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| KIr4O8 | 0.281 | 266 | 1 | 100 h | 0.5 M H2SO4 | This work |
| 5 nm-thick Ir film/Ti substrate |  | 276 | 5 | 24 h | 0.5 M H2SO4 | 1 |
| Porous-Ir-SAs/C | 0.375 | 284 | 10 | 20 h | 0.1 M HClO4 | 2 |
| Ir3Pb | 0.084 | 307 | 10 | 2000 cycles | 0.1 M HClO4 | 3 |
| Pd@Ir/CNT | 0.285 | 266 | 10 | 2000 cycles | 0.5 M H2SO4 | 4 |
| IrCo alloy nanodendrites | 0.09 | 281 | 5 | 500 cycles | 0.1 M HClO4 | 5 |
| IrNi2 after 25 potential cycles | 0.024 | 315 | 5 |  | 0.05 M H2SO4 | 6 |
| IrCoNi multimetallic porous hollow nanocrystals | 0.01 | 309 | 5 | 1000 cycles | 0.5 M H2SO4 | 7 |
| IrCuNi deeply concave nanocubes | 0.006 | 273 | 10 | 1800 cycles | 0.1 M HClO4 | 8 |
| P-IrCux NCs | 0.06 mg | 311 | 10 | 10 h | 0.05 M H2SO4 | 9 |
| Ultrathin IrO2 nanoneedles | 0.25 | 313 | 10 | 2 h | 1 M H2SO4 | 10 |
| Porous IrOx nanoclusters | 0.4 | 290 | 5 | 27.7 | 0.5 M H2SO4 | 11 |
| Li-IrOx | 0.0204 | 290 | 1 | 10 h | 0.5 M H2SO4 | 12 |
| La3IrO7 | 0.467 | 296 | 5 | 16.7 h | 0.1 M HClO4 | 13 |
| 6H-SrIrO3 | 0.284 | 248 | 1 | 30 h | 0.5 M H2SO4 | 14 |
| HxIrO3 NSs | 0.255 | 277 |  | 12 | 0.5 M H2SO4 | 15 |

References

1. Park, N.-Y.; Kim, M.; Kim, Y.-H.; Ramesh, R.; Nandi, D. K.; Tsugawa, T.; Shigetomi, T.; Suzuki, K.; Harada, R.; Kim, M.; An, K.-S.; Shong, B.; Kim, S.-H. Atomic Layer Deposition of Iridium Using a Tricarbonyl Cyclopropenyl Precursor and Oxygen. Chem. Mater. 2022, 34 (4), 1533-1543.

2. Wang, Y.; Guo, X.; Wang, X.; Huang, J.; Yin, L.; Zhu, W.; Zhuang, Z. Construction of steady-active self-supported porous Ir-based electrocatalysts for the oxygen evolution reaction. Chem. Commun. 2023, 59 (13), 1813-1816.

3. Tian, H.; Zhu, W.; Shi, Q.; Ding, S.; Lyu, Z.; Xu, M.; Pan, X.; Engelhard, M. H.; Dan, D.; Lin, Y. Bimetallic IrxPb nanowire networks with enhanced electrocatalytic activity for the oxygen evolution reaction. J. Mater. Chem. A 2022, 10 (20), 11196-11204.

4. Xie, Y.; Chang, C.; Luo, F.; Yang, Z. Modulation in the d Band of Ir by Core-Shell Construction for Robust Water Splitting Electrocatalysts in Acid. ACS Appl. Mater. Interfaces 2023.

5. Fu, L.; Zeng, X.; Cheng, G.; Luo, W. IrCo Nanodendrite as an Efficient Bifunctional Electrocatalyst for Overall Water Splitting under Acidic Conditions. ACS Appl. Mater. Interfaces 2018, 10 (30), 24993-24998.

6. Pi, Y.; Shao, Q.; Zhu, X.; Huang, X. Dynamic Structure Evolution of Composition Segregated Iridium-Nickel Rhombic Dodecahedra toward Efficient Oxygen Evolution Electrocatalysis. ACS Nano 2018, 12 (7), 7371-7379.

7. Feng, J.; Lv, F.; Zhang, W.; Li, P.; Wang, K.; Yang, C.; Wang, B.; Yang, Y.; Zhou, J.; Lin, F.; Wang, G.-C.; Guo, S. Iridium-Based Multimetallic Porous Hollow Nanocrystals for Efficient Overall-Water-Splitting Catalysis. Adv. Mater. 2017, 29 (47), 1703798.

8.	Liu, D.; Lv, Q.; Lu, S.; Fang, J.; Zhang, Y.; Wang, X.; Xue, Y.; Zhu, W.; Zhuang, Z. IrCuNi Deeply Concave Nanocubes as Highly Active Oxygen Evolution Reaction Electrocatalyst in Acid Electrolyte. Nano. Lett. 2021, 21 (7), 2809-2816.

9. Pi, Y.; Guo, J.; Shao, Q.; Huang, X. Highly Efficient Acidic Oxygen Evolution Electrocatalysis Enabled by Porous Ir-Cu Nanocrystals with Three-Dimensional Electrocatalytic Surfaces. Chem. Mater. 2018, 30 (23), 8571-8578.

10. Lim, J. a., D.; Jeon, S. S.; Roh, C. W.; Choi, J.; Yoon, D.; Park, M.; Jung, H.; Lee, H. Ultrathin IrO2 Nanoneedles for Electrochemical Water Oxidation. Adv. Funct. Mater. 2018, 2018, 1704796-1704802.

11. Zhuang, L.; Xu, F.; Wang, K.; Li, J.; Liang, C.; Zhou, W.; Xu, Z.; Shao, Z.; Zhu, Z. Porous Structure Engineering of Iridium Oxide Nanoclusters on Atomic Scale for Efficient pH-Universal Overall Water Splitting. Small 2021, 17 (20), e2100121.

12. Gao, J.; Xu, C. Q.; Hung, S. F.; Liu, W.; Cai, W.; Zeng, Z.; Jia, C.; Chen, H. M.; Xiao, H.; Li, J.; Huang, Y.; Liu, B. Breaking Long-Range Order in Iridium Oxide by Alkali Ion for Efficient Water Oxidation. J. Am. Chem. Soc. 2019, 141 (7), 3014-3023.

13. Qin, Q.; Jang, H.; Wang, Y.; Zhang, L.; Li, Z.; Kim, M. G.; Liu, S.; Liu, X.; Cho, J. Gettering La Effect from La3IrO7 as a Highly Efficient Electrocatalyst for Oxygen Evolution Reaction in Acid Media. Adv. Energy Mater. 2020, 11 (5), 2003561.

14. Yang, L.; Yu, G.; Ai, X.; Yan, W.; Duan, H.; Chen, W.; Li, X.; Wang, T.; Zhang, C.; Huang, X.; Chen, J. S.; Zou, X. Efficient oxygen evolution electrocatalysis in acid by a perovskite with face-sharing IrO6 octahedral dimers. Nat. Commun. 2018, 9 (1), 5236.

15. Liu, Z.; Qi, J.; Zeng, H.; Zeng, Y.; Wang, J.; Gu, L.; Hong, E.; Yang, M.; Fu, Q.; Chen, J.; Yang, C. Electrochemical Preparation of Iridium Hydroxide Nanosheets with Ordered Honeycomb Structures for the Oxygen Evolution Reaction in Acid. ACS Appl. Energy Mater. 2022, 5 (6), 6869-687