Microwave radiation-induced interfacial gradient effect of 3D printing CF/PA12 composite for enhancing mechanical performance

Huifang Zhang1, 2,3, Jieying Zhi2,3, Xiaoxuan Lu2,3, Xuanzhi Peng1, 2,3, Xiaoqing Gao2,3, Yv Yang2,3*,   Zixuan Liu1, Yang Cao1, Qichao Liu1, Youyi Sun1*

1. School of Materials Science and Engineering, North University of China, Taiyuan 030051, China.

2. CAS Key Laboratory for Carbon Materials, Institute of Coal Chemistry, Chinese Academy of Sciences, Taiyuan 03001, China.

3. National Engineering Laboratory for Carbon Fiber Technology, Institute of Coal Chemistry, Chinese Academy of Sciences, Taiyuan 03001, China.

*Corresponding to : Youyi Sun (E-mail: syyi@pku.edu.cn)，Yv Yang (E-mail: yangyv2003@sxicc.ac.cn)

- sFig.1. Optical photos of 3D printing CF/PA12 composite with microwave radiation in the time of 90s.

sTable 1. Effect of microwave radiation time on the enthalpy of melting, the enthalpy of cold crystallization, and the calculated crystallinity.

| Microwave time | △Hm1(J/g) | △Hm2(J/g) | △Hc1(J/g) | △Hc2(J/g) | Xc(%) |
| --- | --- | --- | --- | --- | --- |
| without microwave | 38.56 | 6.31 | 6.02 | 30.71 | 26.81 |
| 30s | 40.22 | 6.43 | 5.53 | 32.51 | 27.87 |
| 60s | 44.67 | 6.31 | 4.93 | 31.18 | 30.46 |
| 80s | 40.31 | 6.98 | 5.79 | 27.23 | 28.26 |
| 90s | 43.41 | 8.35 | 6.65 | 30.98 | 30.93 |

sTable 2. Effect of microwave radiation time on melting temperature and cold crystallization temperature.

| Microwave time | Tm1(℃) | Tm2(℃) | Tcc1(℃) | Tcc2(℃) |
| --- | --- | --- | --- | --- |
| without microwave | 177.64 | 228.26 | 172.65 | 151.11 |
| 30s | 178.86 | 229.11 | 172.61 | 151.02 |
| 60s | 178.5 | 228.85 | 172.07 | 150.64 |
| 80s | 178.98 | 228.9 | 171.66 | 151.11 |
| 90s | 178.12 | 228.4 | 172.01 | 151.09 |