Fig. S1 pH-dependent borate speciation in boric acid solution (Total boron concentration: 0.3 mol·L-1)

Fig. S2 The C1s XPS spectra of the Fe3O4@SiO2-NH2 before and after boron adsorption.

Table S1 BET surface areas and pore structure parameters of Fe3O4 and Fe3O4@SiO2-NH2

| Sample name | specific surface area (m2·g-1) | Pore Diameter (nm) | total pore volume (cm3·g-1) |
| --- | --- | --- | --- |
| Fe3O4 | 49.07 | 54.85 | 0.284 |
| Fe3O4@SiO2-NH2 | 165.17 | 6.57 | 0.330 |

Table S2 Kinetic parameters of different models for boron adsorption on Fe3O4@SiO2-NH2

| qe,exp(mg·g-1) | Pseudo-first-order kinetic model |  |  | Pseudo-second-order kinetic model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qe,cal (mg·g-1) | k1(h-1) | R2 | qe,cal (mg·g-1) | k2(g·mg-1·h-1) | R2 |
| 23.39 | 0.90 | 0.4233 | 0.4045 | 23.53 | 0.7853 | 0.9998 |

Table S3 Parameters of two isotherm models for boron adsorption on Fe3O4@SiO2-NH2

| T (°C) | Langmuir model |  |  | Freundlich model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qm(mg·g-1) | KL | R2 | 1/n | KF | R2 |
| 288.15 | 56.54 | 2.33 | 0.988 | 0.6395 | 48.13 | 0.978 |
| 298.15 | 51.19 | 2.04 | 0.972 | 0.6181 | 39.85 | 0.980 |
| 308.15 | 36.880 | 2.78 | 0.979 | 0.5571 | 31.94 | 0.993 |
| 318.15 | 21.44 | 5.23 | 0.967 | 0.4274 | 21.36 | 0.970 |