Electronic Supplementary Material

| Toward flexible, stable and sensitive SERS substrate from Ag@ZIF-67 decorated cotton fabric for label-free detection of Phenol-soluble modulin |  |
| --- | --- |
| Jiangtao Xu1, Wei Gao2, Ping Zeng3, Shouxiang Jiang1*, Songmin Shang1* 1 Institute of Textiles and Clothing, The Hong Kong Polytechnic University, Hong Kong, 999077, China 2 Department of Applied Physics, The Hong Kong Polytechnic University, Hong Kong, 999077, China 3 Department of Applied Biology and Chemical Technology, The Hong Kong Polytechnic University, Hong Kong, 999077, China Corresponding authors: Shouxiang Jiang, kinor.j@polyu.edu.hk Songmin Shang, profshang@126.com |  |

1 FDTD simulation

To simulate the electrical field intensity on the surface around Ag nanoparticles and ZIF-67, FDTD was employed. The calculation model of Ag and Ag decorated ZIF-67 was established as shown in the figure. According to the statistical results of Image J from the SEM image, the parameters of size of Ag nanoparticle and mean gap among Ag nanoparticles were obtained, where mean particle size was 20 nm and mean gap was 6 nm. In the simulation, the wavelength of the incident light was set as a plane wave with a fixed wavelength of 532 nm and 785 nm which is matched with the laser used. The incident direction of the light is perpendicular to the X plane.

Figure S1 Optical images of prepared samples. (a) cotton fabric, (b) ZIF-67 coated cotton fabric, (c) Ag coated cotton fabric, (d) C-AZ5, (e) C-AZ30, (f) C-AZ60, (g) C-AZ90

Figure S2 SEM images of prepared samples. (a) and (b) cotton fabric, (c) and (d) ZIF-67 coated cotton fabric, (e) C-AZ5, (f) C-AZ30, (g) C-AZ60, and (h) C-AZ90

Figure S3 Raman spectra of substrate

Figure S4 (a)VB-XPS spectrum of ZIF-67; (b) light absorbance of ZIF-67; (c) Band gap of ZIF-67; and (d) HOMO and LUMO of ZIF-67