Figure 1. Mass spectrum of 1e (Ligand)

Figure 2. IR spectrum (KBr) of 1e (Ligand)

Figure 3. 1H NMR spectrum (400 MHz, DMSO-d6) of 1e (Ligand)

Figure 4. 13C NMR spectrum (126 MHz, DMSO-d6) of 1e (Ligand)

Figure 5. Mass spectrum of compound 1f

Figure 6. 1H NMR spectrum (400 MHz, DMSO-d6) of 1f

Figure 7. 13C NMR spectrum (126 MHz, DMSO-d6) of 1f

Figure. 8 IR spectrum (KBr) of 1f

Figure 9. Mass spectrum of compound 1g

Figure 10. 1H NMR spectrum (400 MHz, DMSO-d6) of 1g

Figure 11. 13C NMR spectrum (126 MHz, DMSO-d6) of 1g

Figure 12. IR spectrum (KBr) of 1g

Figure 13. Mass spectrum of compound 1h

Figure 14. 1H NMR spectrum (400 MHz, DMSO-d6) of 1h

Figure 15. 13C NMR spectrum (126 MHz, DMSO-d6) of 1h

Figure 16. IR spectrum of 1h

Figure 17. Mass spectrum of compound Pd-complex

Figure 18. IR spectrum (KBr) of Pd-complex

Figure 19. Mass spectrum of compound Co-complex

Figure 20. IR spectrum (KBr) of Co-complex

Figure 21. Mass spectrum of compound Ni-complex

Figure 22. IR spectrum (KBR) of Ni-complex

Figure 23. TGA Pd-COMPLEX

According to graph shown in Figure 23.

We got 65.40% degradation range of 00C-9000C temperature.

Now, molecular weight of complex = 516.9 gm/mol

If Molecular weight of 100 % complex is 516.9 gm/mol

Then molecular weight of 65.40% complex =?

= 65.4 X 516.9100

= 338.05 gm/mol

Therefore, calculated molecular weight of 65.40% the complex is 338.05gm/mol

Temperature range: 0oC-200oC

As shown in Figure 23, First weight loss found 10.17 %

10.17 % of 338.05 gm/mol

= 338.05 X 10.17100

= 34.37 gm/mol ≅ 35.5 (molecular weight of one chorine atom)

Therefore, 34.37 gm/mol shows loss of one chlorine atom.

Temperature range: 200oC-400oC

As shown in Figure 23, Second weight loss found 7.497%

7.497 % of 338.05 gm/mol

= 338.05 X 7.497100

= 25.44 gm/mol ≅ 30 (molecular weight of - NO)

Therefore, 25.34 gm/mol shows loss of -NO from NO2 group

Temperature range: 400oC-900oC

As shown in Figure 23, Third weight loss found 47.74%

47.74 % of 338.05 gm/mol

=  161.38 X 47.74100

= 161.38 gm/mol ≅ 169 (molecular weight of                       )

Therefore, 161.38 gm/mol shows loss of (C12H10N•) ligand.

Above 900oC residue of PdO

Figure 24. TGA Ni-COMPLEX

According to graph shown in Figure 24,

We got 59.41% degradation range of 0oC-900oC temperature.

Now, molecular weight of complex = 956.41 gm/mol

If Molecular weight of 100 % complex is 956.41 gm/mol

Then molecular weight of 59.41% complex =?

= 59.41 X 956.41100

= 568.2 gm/mol

Therefore, calculated molecular weight of 59.41% the complex is 568.2 gm/mol

Temperature range: 0oC-250oC

As shown in Figure 24, First weight loss found 12.17%

12.17 % of 568.2 gm/mol

= 568.2 X 12.17100

= 69.14 gm/mol ≅ 71 (molecular weight of 2 chlorine atoms)

Therefore, 69.14 gm/mol shows loss of 2-chlorine atom.

Temperature range: 250oC-500oC

As shown in Figure 24, Second weight loss found 25.78%

25.78 % of 568.2 gm/mol

= 568.2 X 25.78100

= 146.48 gm/mol ≅ 148.06 (molecular weight 	    )

Therefore, 146.48 gm/mol shows loss of (C8H8N2O2•) ligand.

Temperature range: 500oC-800oC

As shown in Figure 24, Third weight loss found 21.47%

21.47% of 568.2 gm/mol

= 568.2 X 21.47100

= 121.99gm/mol ≅ 122.02 (molecular weight of                             )

Therefor, 121.99 gm/mol shows loss of (C6H4NO2•) ligand.

Figure 25. TGA Co-complex

According to graph shown in Figure 25,

We got 59.41% degradation range of 0oC-900oC temperature.

Now, molecular weight of complex = 807.65 gm/mol

If Molecular weight of 100% complex is 807.65 gm/mol

Then molecular weight of 69.16% complex =?

= 69.16 X 807.65100

= 558.57 gm/mol

Therefore, calculated molecular weight of 69.16% the complex is 558.57 gm/mol

Temperature range: 0oC-300oC

As shown in Figure 25, First weight loss found 7.976%

7.976 % of 558.57 gm/mol

= 558.57 X 7.976100

= 44.55 gm/mol ≅ 45.99 (molecular weight of 1 –NO2 atom)

Therefore, 44.55 gm/mol shows loss of one –NO2 atom.

Temperature range: 300oC-900oC

As shown in Figure 25, second weight loss found 61.11%

61.11 % of 558.57 gm/mol

= 558.57 X 61.11100

= 341.34 gm/mol ≅ 339.20 (molecular weight of                           )

Therefore, 341.34 gm/mol shows loss of (C15H10CoN3O33•) ligand.

Photocatalytic activity:

Stock solution: weight 100 mg of Remazol Brilliant Blue R (RBBR) dye and dissolved in ultra-pure water and further diluted up to 100 ml. so final concentration of dye solution was 1000 ppm.

Standard solution: Standard 50, 100, 150, 200 ppm prepared from 1000 ppm stock solution.

Standard solution of 50-200 ppm RBBR

Photo-catalytic dye degradation was performed spectrophotometrically on visible light irradiation using Co, Ni and Pd complexes on RBBR dyes. It is well known that RBBR dyes are adsorbed and degraded simultaneously by the catalyst in an aqueous solution.

Absorbance spectra of   Standard solution of 50-200 ppm

The photo catalytic efficiency (%) is calculate using the formula:

% Degradation = A0- AF × 100A0

where A0 and AF are the initial (at 0h) and final (at 4h) concentration of the dye

the absorbance of RBBR was determined by a UV-vis spectrophotometer at the absorption wavelength of 595 nm

Calculation for Co-complex:

- Co 50 ppm = A0- AF × 100A0				2 . Co 100 ppm = A0- AF × 100A0

= 1.091- 0.582 × 1001.091						= 1.233- 0.637 × 1001.233

=   46.65 %							= 48.33 %

- Co 150 ppm = A0- AF × 100A0				4. Co 200 ppm = A0- AF × 100A0

=  2.045- 0.576 × 1002.045					= 1.779- 0.281 × 1001.779

=   71.83 %						= 84.20 %

Solution of RBBR dye 50, 100, 150, 200 ppm with Co-complex

at 0h					at 2h					at 4h

Graph: Photodegradation of RBBR dye

RBBR 50 ppm solution with 10mg Co-complex	            RBBR 100 ppm solution with 10mg Co-complex

RBBR 150 ppm solution with 10mg Co-complex            RBBR 200 ppm solution with 10mg Co-complex

Calculation for Ni-complex:

- Ni 50 ppm = A0- AF × 100A0			2     Ni 100 ppm = A0- AF × 100A0

=  0.576- 0.530 × 1000.576				 = 1.101- 1.041 × 1001.101

=   4.51 %						 = 5.40 %

- Ni 150 ppm = A0- AF × 100A0			4     Ni 200 ppm = A0- AF × 100A0

=  1.872- 1.691 × 1001.872				 = 0.789- 0.707 × 1000.789

=   9.66 %						 = 10.39 %

Solution of RBBR dye 50, 100, 150, 200 ppm with Ni-complex

RBBR 50 ppm solution with 10mg Ni-complex 	               RBBR 100 ppm solution with 10mg Ni-complex

RBBR 150 ppm solution with 10mg Ni-complex	            RBBR 200 ppm solution with 10mg Ni-complex

Calculation for Pd-complex:

- Pd 50 ppm = A0- AF × 100A0				2     Pd 100 ppm =A0- AF × 100A0

=  1.868- 1.799 × 1001.868						= 0.787- 0.757 × 1000.787

=   3.69 %                              				= 3.80 %

- Pd 150 ppm = A0- AF × 100A0				4     Pd 200 ppm = A0- AF × 100A0

=  0.437- 0.419 × 1000.437					= 1.105- 1.020 × 1001.105

=   4.10 %						= 7.69 %

Solution of RBBR dye 50, 100, 150, 200 ppm with Pd-complex

RBBR 50 ppm solution with 10mg pd-complex               RBBR 100 ppm solution with 10mg Pd-complex

RBBR 150 ppm solution with 10mg pd-complex              RBBR 200 ppm solution with 10mg pd-complex