Supplementary information

Assembly of Interfacial Polyelectrolyte Complexation Fiber Bundles with Mineralization Gradient for Physiologically-inspired Ligament Regeneration

Yu-Chung Liu1, Shih-Heng Chen2, Chen-Hsiang Kuan3,4,5, Shih-Hsien Chen2, Wei-Yuan Huang1, Hao-Xuan Chen1, Hsi-Chin Wu6, Tzu-Wei Wang1*

1Department of Materials Science and Engineering, National Tsing Hua University, Hsinchu, Taiwan.

2Division of Trauma Plastic Surgery, Dept. of Plastic & Reconstructive Surgery, Chang Gung Memorial Hospital, Linkou, Taoyuan City, Taiwan

3Division of Plastic Surgery, Department of Surgery, National Taiwan University Hospital; Taipei, Taiwan

4Graduate Institute of Clinical Medicine, College of Medicine, National Taiwan University; Taipei, Taiwan

5Research Center for Developmental Biology and Regenerative Medicine, National Taiwan University, Taipei, Taiwan

6Department of Mechanical ad Materials Engineering, Tatung University, Taipei, Taiwan

Co-first authors: These authors contribute equally to this work

*Corresponding Author

Tzu-Wei Wang, Ph.D.

Professor

Department of Materials Science and Engineering, National Tsing Hua University

101, Section 2, Kuang-Fu Road, Hsinchu, Taiwan

Tel: +886-3-5715131 ext. 33856   Email: twwang@mx.nthu.edu.tw

Supplementary Figure S1. Instrumental setup and design. (A)Photograph of customized IPC spinning instrument. (B) Photograph of the self-designed twisting device

Supplementary Figure S2. Surgical procedure and graft preparation for rabbit ACL reconstruction model. (A) In vivo experimental scheme. (B)Photograph of ACL reconstruction procedure. (B) Morphology of grafts in each group.

Supplementary Figure S3. FT-IR spectrum comparing the change of functiobnal groups of the scaffold before and after EDC/NHS crosslinking.

Supplementary Figure S4. CTGF release from IPC fibers. (A) Experimental design for CTGF loading inside IPC fibers. (B) Encapsulation and CTGF release profile from IPC fibers. (n=3)

Supplementary Figure S5. SBB autofluorescence quenching and Live/Dead assay. (a) Merged fluorescence images of the untreated IPC scaffold captured under FITC and Rhodamine filters. (b) Cell viability of MSCs co-cultured with IPC scaffold and SBB-treated scaffold assessed by CCK-8 assay (n=3, NS represents no significance difference vs control). (c) Live/dead staining results after 7 days incubation.

Supplementary Figure S6. Overview images and lower magnification images of histological analyses of bone tunnel sections. (A) H&E staining at 4 weeks. (B) H&E staining at 10 weeks. (C) Masson’s Trichrome staining at 4 weeks. (D) Masson’s Trichrome staining at 10 weeks.

Supplementary Figure S7. Load-deformation curve of the femur-ligament-tibia complex obtained from the biomechanical test at the 10-week time point.

Supplementary Table S1. Description of animal experimental groups.

| Groups | Description |
| --- | --- |
| Autograft | Partial tendon from the Achilles tendon. |
| LARS | A commercially available synthetic ligament made of PET material, which can be adjusted to 3 mm in width and 60 mm in length. |
| Scaffold | An IPC scaffold with collagen sheath crosslinked with EDC in the central zone and a gradual HAp coating at both ends. |
| Scaffold/CTGF | Scaffold incorporating 200ng CTGF-binded PCN within the collagen sheath. |
| Scaffold/CTGF/MSC | 2 × 106 rabbit MSCs were seeded onto Scaffold/CTGF for 1 weeks in advance. |

Supplementary Table S2. Mechanical properties of scaffolds pre- and post-crosslinking at various twisting angles

| Groups | Uncrosslinked | Crosslinked |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 0°/cm twisting | 0°/cm twisting | 22.5°/cm twisting | 45°/cm twisting | 90°/cm twisting |
| Ultimate tensile strength (MPa) | 1.24 (±0.25) | 4.33(±0.46) | 8.45 (±0.69) | 15.62 (±0.78) | 3.37 (±0.30) |
| Strain at break (%) | 44.38 (±5.79) | 23.40 (±3.84) | 26.50 (±3.30) | 38.99 (±1.30) | 19.59 (±0.71) |
| Young’s modulus (MPa) | 6.46 (±1.87) | 20.62 (±4.2) | 37.70 (±4.61) | 38.62 (±0.71) | 17.79 (±2.80) |

Supplementary Table S3. Comparison of strain parameters and creep deformation in different groups (n=3)

| Groups | IPC w/o COL | IPC w/ COL | Porcine ACL |
| --- | --- | --- | --- |
| Peak strain (εMax,%) | 23.77 (±0.64) | 14.23 (±0.56) | 11.72 (±0.40) |
| Permanent strain (εMin,%) | 13.79 (±1.72) | 1.42 (±0.09) | 1.12 (±0.07) |
| Recovery ratio (%) | 44.45 (±7.44) | 90.00 (±0.21) | 89.77 (±0.99) |
| Creep deformation. (%) | 9.85 (±0.83) | 4.22 (±0.24) | 1.57 (±0.39) |

Supplementary Table S4. Results of biomechanical test

| Groups | Autograft | LARs | Scaffold | Scaffold/CTGF | Scaffold/CTGF/MSC |
| --- | --- | --- | --- | --- | --- |
| Ultimate Tensile Force (N) | 11.79 | 10.02 | 4.55 | 6.12 | 9.98 |
| Ultimate Tensile Stress (MPa) | 2.22 | 3.18 | 1.15 | 1.84 | 2.4 |
| Stiffness (N/mm) | 3.15 | 2.35 | 2.53 | 2.16 | 2.56 |