Strategies towards submicron size and high performance magnetic PGMA@Fe3O4@SiO2-COOH microspheres with biological application

Tianhao Xiaa, Yunpeng Wanga, Pragati Awasthia, Wenkun Dongb, Mengting Lib, Xvsheng Qiaoa*, Dong Chenb, Shisheng Lingb and Xianping Fana

a State Key Laboratory of Silicon Materials & School of Materials Science and Engineering, Zhejiang University, Hangzhou 310058, China

b Assure Tech. (Hangzhou) Co., Ltd, Hangzhou 310015, China

* Corresponding Author, E-mail: qiaoxus@zju.edu.cn

Table S1 Experiment design for the preparation of PGMA@Fe3O4 microspheres

| Batch | GMA (mL) | NH3·H2O (mL) | Na3Cit (g) | Fe3+ (mol/L) | Fe2+ (mol/L) |
| --- | --- | --- | --- | --- | --- |
| A-1 | 2.25 | 1.0 | 0.050 | 0.1200 | 0.0750 |
| A-2 | 2.25 | 2.0 | 0.050 | 0.1200 | 0.0750 |
| A-3 | 2.25 | 3.0 | 0.050 | 0.1200 | 0.0750 |
| A-4 | 2.25 | 4.0 | 0.050 | 0.1200 | 0.0750 |
| A-5 | 2.25 | 5.0 | 0.050 | 0.1200 | 0.0750 |
| A-6 | 2.25 | 6.0 | 0.050 | 0.1200 | 0.0750 |
| B-1 | 2.25 | 3.0 | 0.025 | 0.1200 | 0.0750 |
| B-2 | 2.25 | 3.0 | 0.050 | 0.1200 | 0.0750 |
| B-3 | 2.25 | 3.0 | 0.075 | 0.1200 | 0.0750 |
| B-4 | 2.25 | 3.0 | 0.100 | 0.1200 | 0.0750 |
| B-5 | 2.25 | 3.0 | 0.125 | 0.1200 | 0.0750 |
| B-6 | 2.25 | 3.0 | 0.150 | 0.1200 | 0.0750 |
| C-1 | 2.25 | 3.0 | 0.050 | 0.0800 | 0.0500 |
| C-2 | 2.25 | 3.0 | 0.050 | 0.1000 | 0.0625 |
| C-3 | 2.25 | 3.0 | 0.050 | 0.1200 | 0.0750 |
| C-4 | 2.25 | 3.0 | 0.050 | 0.1400 | 0.0875 |
| C-5 | 2.25 | 3.0 | 0.050 | 0.1600 | 0.1000 |
| C-6 | 2.25 | 3.0 | 0.050 | 0.1800 | 0.1125 |
| D-1 | 2.25 | 3.0 | 0.050 | 0.1200 | 0.0750 |
| D-2 | 4.50 | 3.0 | 0.050 | 0.1200 | 0.0750 |
| D-3 | 6.75 | 3.0 | 0.050 | 0.1200 | 0.0750 |
| D-4 | 9.00 | 3.0 | 0.050 | 0.1200 | 0.0750 |

Fig. S1 FTIR spectra of PGMA and PGMA-NH2 microspheres

Fig. S2 Effects of ammonia volume (a, b), Na3cit amount (c, d), Fe3+ and Fe2+ concentration (e, f) on the saturation magnetization, magnetic content, grain size, residual magnetization, and coercive force of PGMA@Fe3O4 microspheres