Supplementary information

Advanced Composites and Hybrid Materials

High anti-corrosive barrier of poly(methyl methacrylate))-silica coatings explained: a thousand-days study

Mayara Carla Uvida1, Andressa Trentin1,2, Sandra Helena Pulcinelli1, Celso Valentim Santilli1, P. Hammer1*

1São Paulo State University, Institute of Chemistry, 14800–060, Araraquara/SP, Brazil

2VTT Technical Research Centre of Finland Ltd, Espoo, Finland

*Corresponding author: peter.hammer@unesp.br

# 1. Experimental: aluminum alloys composition

The nominal composition (wt%) of the AA2024-T3 and AA7075-T3 aluminum alloys used as substrates for the deposition of the PMMA-silica hybrid coatings is described in Table S1.

Table S1. The nominal composition of AA2024-T3 and AA7075-T3 aluminum alloys.

|  | Aluminum alloys composition (wt%) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cu | Mg | Mn | Si | Fe | Zn | Ti | Cr | Ni | Al |
| AA2024-T3 | 4.50 | 1.50 | 0.50 | - | - | - | - | - | - | 93.50 |
| AA7075-T3 | 1.48 | 2.60 | 0.30 | 0.09 | 0.37 | 5.64 | 0.20 | 0.24 | 0.05 | 89.03 |

# 2. Electrochemical barrier properties: EIS results obtained for duplicates

Fig. S1 Nyquist and Bode plots as a function of time for duplicates of PMMA-silica coatings (a) B001 on AA2024 and (b) B005 on AA7075 substrates.

# 3. Structural properties: FTIR, SAXS, and XPS analyses

Fig. S2 Deconvoluted FTIR spectra in the region of 900 ‒ 1100 cm‒1 before and after immersion of 60 days for (a) B001 and (b) B005 samples.

Fig. S3 13C NMR spectra of samples B001 (a) and B005 (b), before (a1, b1) and after (a1, b2) 200 days of immersion in 0.6 M NaCl. (c) Representative molecular structure of the PMMA-silica hybrid with the identification of carbon atoms.

Fig. S4 SAXS scattering profiles before and after 200 days of immersion of sample (a) B001 and (b) B005.

Fig. S5 XPS O 1s, C 1s, and Si 2p spectra of the B005 coating (a) before testing and (b) after exposure of 1004 days to 0.6 M NaCl solution.

Table S2. XPS surface composition of B001 and B005 samples before and after 1000 days of immersion.

| Samples | B001 |  |  |  | B005 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Intact | Immersed | Intact (at.%)* |  |  |  | Immersed |
| O 1s | 32.7 | 29.1 |  | 31.9 |  | 30.1 |  |
| C 1s | 55.8 | 63.0 |  | 56.9 |  | 60.1 |  |
| Si 2p | 11.5 | 7.9 |  | 11.2 |  | 9.8 |  |

*Error: 5%

Fig. S6 Time dependence of TG curves of B001 (a) and B005 (b) samples during the immersion in 0.6 M NaCl solution.