Simultaneously enhancing microelastic response and degradability for poly(butylene succinate) composite monofilaments by silanized microcrystalline cellulose

Yang Zhang1, He Liao2, Yue Zhang1*, Yumei Zhang1*

1College of Materials Science and Engineering, Donghua University, State Key Laboratory for Modification of Chemical Fibers and Polymer Materials, Shanghai 201620, China

2College of Mechanical Engineering, Donghua University, Shanghai 201620, China

* Correspondence to: Yumei Zhang, E-mail: zhangym@dhu.edu.cn, Tel/Fax: 0086˗21˗67792957; Yue Zhang, e-mail: zhangyue@dhu.edu.cn

Fig. S1 XPS curves of mMCC modified with different silane coupling agents

Tab.S1 XPS parameters of mMCC modified with different silane coupling agents

| Sample | O1s% | C1s% | Si% | O/C | D% |
| --- | --- | --- | --- | --- | --- |
| MCC | 42.73 | 57.27 | 0 | 0.746 |  |
| KH570-MCC | 42.43 | 56.84 | 0.73 | 0.746 | 6.1 |
| KH1231-MCC | 40.92 | 57.74 | 1.34 | 0.709 | 13.9 |
| KH1631-MCC | 38.48 | 59.71 | 1.8 | 0.644 | 22.3 |
| KH1831-MCC | 42.59 | 56.65 | 0.76 | 0.752 | 10.2 |

Fig. S2 (a) Schematic representation of different silane coupling agent modified cellulose before simulation, (b) Schematic representation of different concentration of KH1631 modified cellulose before simulation (cellulose: dark green, C: gray, Si: orange, H: white and O: red)

Fig. S3 XPS curves of mMCC modified with different concentrations of KH1631

Tab.S2 XPS parameters of mMCC modified with different concentrations of KH1631

| Sample | O1s% | C1s% | Si% | O/C | D% |
| --- | --- | --- | --- | --- | --- |
| 1:1.00 | 19.84 | 75.65 | 4.51 | 0.262 | 55.9 |
| 1:0.50 | 9.75 | 84.29 | 5.96 | 0.116 | 73.9 |
| 1:0.33 | 31.65 | 65.57 | 2.79 | 0.483 | 34.6 |
| 1:0.25 | 38.48 | 59.71 | 1.8 | 0.644 | 22.3 |
| 1:0.1 | 47.09 | 51.71 | 1.2 | 0.911 | 14.9 |

Fig. S4 (a) WAXD curves of mMCC/PBS C composite monofilaments，(b) DSC curves of mMCC/PBS composite monofilaments，(c) (1Ī0) crystal plane diffraction peak of mMCC in mMCC/PBS composite monofilaments，(d) (110) crystal plane diffraction peak of mMCC in mMCC/PBS composite monofilaments.

Fig. S5 Stress-strain curves of mMCC/PBS composite monofilaments