Supplementary Information

Large-Scale Synthesis of Transition Metal Dichalcogenides at Atmospheric Pressure in Air

Xinshui Zhang1, Hongzhou Pan1, Nan Zheng1, Yue Zhang1, Yinjie Lv1, Cong Wu1, Jiameng Yu1, Ran Wei1, Tianyi Gao1, Yi Yu1,2, Nan Yang1, Wei Liu1,2,3*

1School of Physical Science and Technology, ShanghaiTech University, Shanghai 201210, China

2Shanghai Key Laboratory of High-resolution Electron Microscopy, ShanghaiTech University; Shanghai, 201210, China

3Key Laboratory of Advanced Energy Materials Chemistry (Ministry of Education), Nankai University, Tianjin, 300071, China

Author information

Corresponding Author

*E-mail: liuwei1@shanghaitech.edu.cn

Supplementary Figure 1. Cross-sectional SEM images of the MoS2 precursor / KCl pellet and corresponding mapping images.

Supplementary Figure 2. (a) Photographs of the MoS2 precursor / KCl @ KBr after heated at different temperatures for different time, (b) and corresponding X-ray diffraction patterns of the products.

Supplementary Figure 3. Yield of the MoS2 with KCl (MoS2 precursor: KCl=6:6, mass ratio) heated at different temperatures for different time.

Supplementary Figure 4. SEM images of the final MoS2 products synthesized at different temperatures for different time.

Supplementary Figure 5. Photographs of the WS2 precursor / KCl @ KBr after heated at 600 ℃ for 2 h.

Supplementary Figure 6. (a) X-ray diffraction pattern and (b) SEM image of the WS2 synthesized at 600 ℃ for 2 h,

Supplementary Figure 7. TG and DTG curves of the MoS2 powder.

Supplementary Figure 8. Survey XPS spectra of MoS2 synthesized by dynamic salt capsulated method.

Supplementary Figure 9. SEM image shows the thickness of the nanosheet in MoS2 nanosphere.

Supplementary Figure 10. (a) Photographs of the MoS2 precursor @ KBr after heated at 600 ℃ for 2 h. (b) The XRD pattern of the products. (c) Yield of the MoS2 with no KCl heated at different temperatures.

Supplementary Figure 11. Optical image of the KBr shell after pressed at 4 MPa for 3 min.

Supplementary Figure 12. SEM images of the KBr shell after pressed at 4 MPa for 3 min.

Supplementary Figure 13. Photos and the corresponding XRD patterns of the products for (a) MoS2 precursor / KCl powder and (b) MoS2 precursor / KCl pellet heated at 600 ℃ for 2 h in air.

Supplementary Figure 14. (a) Schematics depicting the MoS2 precursor / KCl @ KBr heated in an Ar atmosphere. (b) Photographs of the MoS2 precursor / KCl @ KBr after heated at 600 ℃ for 2 h in an Ar atmosphere. (c) Yield of the MoS2 synthesized under different temperature. (d) SEM images of MoS2 in an Ar atmosphere.

Supplementary Figure 15. Application of MoS2 nanospheres synthesized by dynamic salt capsulation in Lithium-ion batteries. (a) Schematics depicting the MoS2 acted as the anode in Li ion batteries. (b) CV curves of the MoS2 electrode at a scanning rate of 0.1 mV/s during the initial five cycles. (c) Cycling performance of MoS2 synthesized by dynamic salt capsulation and commercial MoS2 within a voltage range of 0.01-3.0 V vs Li+/Li at 0.5 C. (d) Nyquist curves of Li/LE/MoS2 obtained before and after 100 cycles.

Supplementary Table 1. The relative density of the KBr shell.

Supplementary Table 2. Comparison of the overpotential required to get current density of 10 mA cm−2 and Tafel slope of various recent state-of-the-art MoS2 catalysts for HER.