Table 1  Optimization reaction conditions

Table 2  Knoevenagel condensation reaction of various aromatic aldehydes and 1,3-dicetones in the presence of the KCC-1-Bipy+22Cl-  under solvent free reaction conditions

Table 3  Comparison of efficiency of the present method in the Knoevenagel condensation reaction of  4- chlorobenzaldehyde and dimedone  with previous reports methods.

Table 1  Optimization reaction conditions

| Entry | Catalyst (mg) | Conditions Solvent/Tem.(οC)/Time (min) | Yield |
| --- | --- | --- | --- |
| 1 | No catalyst | Sf/80 οC/ 60 | No Reaction |
| 2 | KCC-1-Bipy+22Cl- (0.002 g) | Sf/80 οC/ 20 | No Reaction |
| 3 | KCC-1-Bipy+22Cl- (0.003 g) | Sf/80 οC/ 20 | In completed |
| 4 | KCC-1-Bipy+22Cl- (0.004 g) | Sf/80 οC/ 10 | 99% |
| 5 | KCC-1-Bipy+22Cl- (0.004 g) | Sf/r.t./ 60 | No Reaction |
| 6 | KCC-1-Bipy+22Cl- (0.004 g) | Sf/60 οC/ 60 | In completed |
| 7 | KCC-1-Bipy+22Cl- (0.004 g) | n-hexane/ Reflux/ 60 | In completed |
| 8 | KCC-1-Bipy+22Cl- (0.004 g) | EtOH/ Reflux/ 60 | 80% |
| 9 | KCC-1-Bipy+22Cl- (0.004 g) | H2O/ Reflux/ 60 | In completed |
| 10 | KCC-1 (0.004 g) | Sf/80 οC/ 60 | In completed |
| Sf: Solvent free |  |  |  |

Table 2  Knoevenagel condensation reaction of various aromatic aldehydes and 1,3-dicetones in the presence of the KCC-1-Bipy+22Cl-  under solvent free reaction conditions

| 2'a Time: 20 min, Yield: 60% mp: (183-185) mp (reported): [190-192] [9] | 2'b Time: 10 min, Yield: 99 % mp: (150-152) mp (reported): [125-127] [9] | 2'c Time: 15 min, Yield: 99 % mp: (183-185) mp (reported):[187-190] [10] | 2'd Time: 10 min, Yield: 95 % mp: (198-200) mp (reported): [202-204] [10] |
| --- | --- | --- | --- |
| 2'e Time: 20 min, Yield: 80% mp: (117-120) mp (reported): [127-129] [11] | 2'f Time: 80 min, Yield: 72% mp: (185-187) mp (reported): [185-187] [10] | 3'a Time: 10 min, Yield: 70% mp: (150-155) mp (reported): [152-155] [12] | 3'b Time: 60 min, Yield: 90% mp: ( 155-158) mp (reported): [154-156] [11] |
| 3'c Time: 30 min, Yield: 90% mp: (157-160 ) mp (reported): [159-161] [15] | 3'd Time: 40 min, Yield: 99% mp: (180-182) mp (reported): [190-193] [14] | 3'e Time: 20 min, Yield: 99% mp: (159-162) mp (reported): [174-177] [13] | 3'f Time: 10 min, Yield: 60% mp: (135-139) mp (reported): [133-134] [12] |
| 3'g Time: 20 min, Yield: 99% mp: (285-289) mp (reported): [297-298] [11] | 4'a Time: 10 min, Yield: 99% mp: (235-240) mp (reported): [234-236] [17] | 4'b Time: 35 min, Yield: 90% mp: 390 d mp (reported): mp > 300 [17] | 4'c Time: 20 min, Yield: 99% mp: (320-325) mp (reported): mp > 300 [16] |
| 4'd Time: 35 min, Yield: 99% mp: (325-330 ) mp (reported): mp > 300 [17] | 4'e Time: 25 min, Yield: 99% mp: (290-292) mp (reported): mp ≥300 [16] | 4'f Time: 35 min, Yield: 99% mp: (345-350) mp (reported): mp > 300 [16] | 4'g Time: 40 min, Yield: 90% mp: (210-215) mp (reported): [246-247] [17] |
| 5'a Time: 10 min, Yield: 80% mp: (143-147) mp (reported): [150] [18] | 5'b Time: 5 min, Yield: 95% mp: (178-179) mp (reported): [178] [18] | 5'c Time: 5 min, Yield: 98% mp: (112-115) mp (reported): [139-141] [19] | 5'd Time: 5 min, Yield: 80% mp: (151-155) mp (reported): [159] [18] |
| 5'e Time: 5 min, Yield: 53% mp: (203-205) mp (reported): [205] [18] | 5'f Time: 5 min, Yield: 73% mp: (200-204) mp (reported): [196] [21] | 5'g Time: 5 min, Yield: 76% mp: (214-216) mp (reported): [221] [21] | 5'h Time: 5 min, Yield: 92% mp: (145-150) mp (reported):[148-149] [20] |
| 5'i Time: 5 min, Yield: 95% mp: (255-258) mp (reported): [261-262] [20] | 5'j Time: 5 min, Yield: 95% mp: (215-220) mp (reported): [233-234] [20] | 5'k Time: 5 min, Yield: 95% mp: (202-205) mp (reported): [225] [21] | 5'l Time: 5 min, Yield: 52% mp: (212-214) mp (reported): [215] [21] |
| 5'm Time: 5 min, Yield: 92% mp: (251-252) mp (reported): [251-252] [18] | 5'n Time: 5 min, Yield: 95% mp: (228-230) mp (reported): [230-232] [18] |  |  |

Table 3  Comparison of efficiency of the present method in the Knoevenagel condensation reaction of  4- chlorobenzaldehyde and dimedone  with previous reports methods.

| Ref | Yield (%) | Reaction Condition Time (min)/Tem (℃)/Solvent | Catalyst | Entry |
| --- | --- | --- | --- | --- |
| [9] | 80 | 60 min/ reflux/ EtOH | Piperidine | 1 |
| [22] | 88 | 180 min / r.t/ H2O | [PEG(mim)2][OH]2 | 2 |
| [23] | 81 | 60 min/ r.t./ EtOH | Ni-nanoparticles | 3 |
| [24] | 63 | 30 min/ r.t./ Ionic Liquid | 2-hydroxyethylammonium formate | 4 |
| [25] | 92 | 10 min/ r.t./Ionic Liquid | IV- DES (deep eutectic solvents based on CeCl3.7H2O with urea) | 5 |
| Present | 99 | 10 min/80℃/ Solvent Free | KCC-1-Bipy+2 2Cl- | 6 |