Response surface methodology as optimization approach for tetrabromobisphenol A (TBBPA) removal in aqueous media using activated carbon derived from puck (Afroxtyrax lepidophyllus) shell: isotherms and kinetics adsorption

Gédéon Nzetchuen Kouahou1, Fredy Harcel Kamgang Djioko2, Cyrille Donlifack Atemkeng1, Cyrille Ghislain Fotsop1,3, Liouna Adoum Amola1, Aurelien Bopda1, Serges Bruno Lemoupi Ngomadé1,4*, Theophile Kamgaing1*

1Research unit of Noxious Chemistry and Environmental Engineering, Department of Chemistry, University of Dschang, Dschang, Cameroon.

2Africa Center of Excellence in Future Energies and Electrochemical Systems (ACE-FUELS), Federal University of Technology, Owerri, Imo State, Nigeria

3Institute of Chemistry, Faculty of Process and Systems Engineering, Universität Platz 2, 39106 Magdeburg, Germany.

4Biofuel division, CSIR-Indian institute of petroleum, Dehradum, India

*Corresponding author: Theophile Kamgaing, theokamgaing@yahoo.fr

Serges Bruno Lemoupi Ngomadé, sergesngomade848@gmail.com

Supporting information

Supplementary Table 1: Some characteristics of TBBPA

| molecular formula |  |
| --- | --- |
| chemical structure | C15H12Br4O2 |
| systematic name | 2,2-bis(3,5-dibromo-4-hydroxyphenyl)propane |
| λmax (nm) | 293 |
| pka | 7.5-8.5 |
| molecular mass | 543.87 |

Supplementary table 2:  absorbance obtained after spectrophotometer uv-vis analysis

| order of experiments | pH | mass (g) | C (mol/L) | t (min) | Ce (mol/L) | Absorbance |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 8 | 125 | 8.5 | 90 | 3.968 | 0.041 |
| 2 | 8 | 125 | 8.5 | 90 | 4.057 | 0.042 |
| 3 | 8 | 125 | 8.5 | 90 | 4.199 | 0.043 |
| 4 | 8 | 200 | 2 | 90 | 1.337 | 0.015 |
| 5 | 11 | 50 | 8.5 | 90 | 6.554 | 0.066 |
| 6 | 5 | 50 | 8.5 | 90 | 6.022 | 0.061 |
| 7 | 8 | 125 | 15 | 160 | 2.865 | 0.030 |
| 8 | 5 | 125 | 15 | 90 | 7.0275 | 0.071 |
| 9 | 11 | 125 | 15 | 90 | 7.912 | 0.080 |
| 10 | 11 | 125 | 8.5 | 160 | 7.281 | 0.073 |
| 11 | 8 | 200 | 8.5 | 160 | 4.528 | 0.046 |
| 12 | 8 | 125 | 2 | 20 | 1.089 | 0.012 |
| 13 | 5 | 200 | 8.5 | 90 | 5.418 | 0.055 |
| 14 | 11 | 125 | 8.5 | 20 | 6.329 | 0.064 |
| 15 | 11 | 125 | 2 | 90 | 1.739 | 0.018 |
| 16 | 8 | 50 | 8.5 | 20 | 4.9283 | 0.050 |
| 17 | 8 | 200 | 15 | 90 | 2.055 | 0.022 |
| 18 | 8 | 50 | 8.5 | 160 | 4.5237 | 0.046 |
| 19 | 8 | 125 | 15 | 20 | 3.9285 | 0.040 |
| 20 | 5 | 125 | 8.5 | 20 | 6.21265 | 0.063 |
| 21 | 11 | 200 | 8.5 | 90 | 6.477 | 0.065 |
| 22 | 8 | 50 | 15 | 90 | 4.704 | 0.048 |
| 23 | 8 | 125 | 2 | 160 | 1.44 | 0.015 |
| 24 | 5 | 125 | 2 | 90 | 1.5922 | 0.017 |
| 25 | 8 | 200 | 8.5 | 20 | 3.6465 | 0.037 |
| 26 | 5 | 125 | 8.5 | 160 | 5.9976 | 0.061 |
| 27 | 8 | 50 | 2 | 90 | 1.051 | 0.012 |

Supplementary Table 3:  Boehm titration of CRP

| AC |  | Carboxylic | lactone | phenol | Total acid | Total base |
| --- | --- | --- | --- | --- | --- | --- |
| CRP (meq/g) | 0.06 |  | 0.18 | 0.84 | 1.08 | 0.12 |

Supplementary Table 4: Validation of the experimental model

| Activated carbons | Adsorption conditions | Adsorption Percentage (%) |  |  |
| --- | --- | --- | --- | --- |
|  |  | Experimental value | Predicted value |  |  |
| CRP | A : 7.66 B (mg) : 200 C (mol/L) : 15 D (min) : 89 | 87.90 | 88.0647 |  |  |

293 nm

Supplementary Fig 1: UV-vis spectrum of  TBBPA at 30 mg/L concentration and TBBPA calibration lines.

Supplementary Fig 2: structure of activated carbon used for computational simulations

Supplementary Fig 3: effect of interfering ions on adsorption of TBBPA by CRP.

The desorption equation is given by supplementary equation 1

%Desorption = Cf-CrCr*100 								(S1)

Where Cf (mg/L) is the concentration of pollutant fixed on CRP and Cr the remaining concentration of pollutant on CRP after desorption.

a)

b)

c)

Fig 10: RDF plots of the AC/TBBPA system as a function of the medium a) neutral, b) basic, c) acid