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Figures:
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Fig. S1 (a) Particle size distribution and (b) photoluminescence diagram of the prepared carbon dots
[image: 图片S-2]
Fig. S2 (a) XRD pattern of the carbon points. (b) Zeta potential of the carbon pointsCDs modified MFC
Blank group MFC
(a)
(b)






Fig. S3 (a) and (b) Surface photographs of the MFC anode for the CDs-modified group and the blank group, respectively
Tables
Table S1 Average relative abundance (%) of dominant populations in the test group and the blank group at genus level
	Genus
	Blank group
	CDs modified group

	Kluyvera
	18.001
	21.457

	Dysgonomonascc
	20.894
	15.302

	Klebsiellacc
	16.396
	7.173

	Saccharimonadales
	2.805
	8.624

	Propionicicella
	7.537
	2.212

	Christensenellaceae_R-7_group
	2.396
	5.007

	Citrobactercc
	2.443
	3.790

	Saccharimonadaceaecc
	3.687
	1.558

	Pleomorphomonascc
	1.062
	1.603

	Petrimonas
	0.848
	1.731

	Propionicimonas
	1.045
	1.366

	Allorhizobium-Neorhizobium-Pararhizobium-Rhizobiumcc
	1.358
	0.923

	Propionivibriocc
	0.560
	1.681

	Flavobacterium
	0.778
	0.788

	Sporomusacc
	0.428
	0.829

	Anaerovoraxcc
	0.446
	0.698

	Geobacter
	0.398
	0.685

	Cellulomonas
	0.380
	0.703

	Oscillibacter
	0.691
	0.321

	Telmatospirillum
	0.343
	0.663

	WPS-2
	0.285
	0.685

	Ruminococcaceae_UCG-013
	0.231
	0.615

	Others
	16.988
	21.286



Table S2 At the genus level, the average relative abundance (%) of electric bacteria in the test group and the blank group
	Genus
	Blank group
	CDs modified group

	Kluyvera
	18.001
	21.457

	Klebsiella
	16.396
	7.173

	Christensenellaceae_R-7_group
	2.396
	5.007

	Citrobacter
	2.443
	3.790

	Petrimonas
Geobacter
Total
	0.848
0.398
40.482
	1.731
0.685
39.843
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