Supporting Information

Facilely prepared carbon dots as effective anode modifier for enhanced performance of microbial fuel cells

Hui-Xu Wei, Rui Qiu, Ai-Yi Li, Liu-Jie Liang, Yan-Nan Feng, Shu-Hua Li, Nan Li*

School of Chemistry and Chemical Engineering/Guangzhou Key Laboratory for Clean Energy and Materials, Guangzhou University, Guangzhou 510006, China.

Corresponding author E-mail:  nanli@gzhu.edu.cn

Figures:

(a)

Fig. S1 (a) Particle size distribution and (b) photoluminescence diagram of the prepared carbon dots

CDs modified MFC

Blank group MFC

(a)

(b)

Fig. S2 (a) XRD pattern of the carbon points. (b) Zeta potential of the carbon points

Fig. S3 (a) and (b) Surface photographs of the MFC anode for the CDs-modified group and the blank group, respectively

Tables

Table S1 Average relative abundance (%) of dominant populations in the test group and the blank group at genus level

| Genus | Blank group | CDs modified group |
| --- | --- | --- |
| Kluyvera | 18.001 | 21.457 |
| Dysgonomonascc | 20.894 | 15.302 |
| Klebsiellacc | 16.396 | 7.173 |
| Saccharimonadales | 2.805 | 8.624 |
| Propionicicella | 7.537 | 2.212 |
| Christensenellaceae_R-7_group | 2.396 | 5.007 |
| Citrobactercc | 2.443 | 3.790 |
| Saccharimonadaceaecc | 3.687 | 1.558 |
| Pleomorphomonascc | 1.062 | 1.603 |
| Petrimonas | 0.848 | 1.731 |
| Propionicimonas | 1.045 | 1.366 |
| Allorhizobium-Neorhizobium-Pararhizobium-Rhizobiumcc | 1.358 | 0.923 |
| Propionivibriocc | 0.560 | 1.681 |
| Flavobacterium | 0.778 | 0.788 |
| Sporomusacc | 0.428 | 0.829 |
| Anaerovoraxcc | 0.446 | 0.698 |
| Geobacter | 0.398 | 0.685 |
| Cellulomonas | 0.380 | 0.703 |
| Oscillibacter | 0.691 | 0.321 |
| Telmatospirillum | 0.343 | 0.663 |
| WPS-2 | 0.285 | 0.685 |
| Ruminococcaceae_UCG-013 | 0.231 | 0.615 |
| Others | 16.988 | 21.286 |

Table S2 At the genus level, the average relative abundance (%) of electric bacteria in the test group and the blank group

| Genus | Blank group | CDs modified group |
| --- | --- | --- |
| Kluyvera | 18.001 | 21.457 |
| Klebsiella | 16.396 | 7.173 |
| Christensenellaceae_R-7_group | 2.396 | 5.007 |
| Citrobacter | 2.443 | 3.790 |
| Petrimonas Geobacter Total | 0.848 0.398 40.482 | 1.731 0.685 39.843 |