Table 1 Advantages and disadvantages of PVA/PVP materials for water treatment and purification.

Table 2 FTIR bands of the hydrogels: a) HG, b) HG-Fe (before) and c) HG-F, d) HG-Fe-F (after) adsorption.

Table 3 Elemental analysis of the hydrogels: a) HG, b) HG-Fe (before) and c) HG-F, d) HG-Fe-F (after) adsorption.

Table 4 Kinetic parameters of F- adsorption by HG and HG-Fe at pH = 6.7.

Table 5 Adsorption capacities of adsorbent materials for fluoride ions from the literature.

Table 6 Parameters of the adsorption of F- by HG and HG-Fe at pH = 5

Table 7 Adsorption isotherm parameters calculated from the experimental data and the models of Langmuir, Freundlich and Langmuir-Freundlich.

Table 8 Thermodynamic parameters for the adsorption processes of fluoride ions by both HG and HG-Fe hydrogels

Table 1.

| Materials | Advantages | Disadvantages | Ref. |
| --- | --- | --- | --- |
| PVA/PVP/AAc hydrogels | Low cost and easy technical access | Low efficiency on the adsorption of dyes and metals | [24] |
| CS/PVA/PVP composite hydrogel | The material can be reused | Difficult synthesis | [25] |
| PVA-GO-NaAlg nanocomposite | Good properties antifouling | Limited to remove cationic dyes | [26] |
| PVP-PEK copolymer from PVOH oxidation | Biodegradable material | High quantities of ware are consumed during the synthesis | [27] |
| Porous TiO2/PVA composite sphere | Good photoactive property and recovery during its application in large-scale wastewater treatment. | The synthesis is a very low temperature | [28] |
| TiO2 Immobilized Polymeric Photocatalyst | Crack-free composite surface | The pH should be controlled during degradation of dye. | [29] |
| PVA/PVP/α-MnO2-stearic acid nanocomposites | Easy synthesis | Ultrasonic irradiation must be constantly controlled to avoid agglomeration. | [30] |
| PVA-PVP-Chitosan microspheres | Useful to remove other organic pollutants such as pesticides. | Low thermal stability. | [31] |

Table 2.

| Functional group | Wavelength (1/cm) |  |  |  |
| --- | --- | --- | --- | --- |
|  | HG | HG-Fe | HG-F | HG-Fe-F |
| O-H (υ) | 3320 | 3345 | 3350 | 3340 |
| -CH (υ) | 2940 | 2925 | 2932 | 2923 |
| C=O (υ) | 1728, 1640 | 1735, 1650 | 1728, 1658 | 1736, 1658 |
| C-H (δ) | 1424, 1372 | 1420, 1373 | 1426, 1373 | 1426, 1373 |
| C-N (υ) | 1260 | 1232 | 1240 | 1240 |

Table 3.

| Element | %-weight |  |  |  |
| --- | --- | --- | --- | --- |
|  | HG | HG-Fe | HG-F | HG-Fe-F |
| C | 63.3±0.87 | 61.9±1.12 | 61.7±0.96 | 62.0±1.31 |
| O | 36.7±1.77 | 37.4±0.95 | 38.3±1.00 | 37.0±1.46 |
| Fe | --- | 0.7±0.56 | --- | 1.0±0.33 |

Table 4.

| Sample | Pseudo first order (Lagergren) |  |  |  | Second order (Elovich) |  |  |  | Pseudo second order (Ho-McKay) |  |  |  | Experimental |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qe mg/g | KL 1/h | R2 |  | a mg/g h | b g/mg | R2 |  | qe mg/g | K2 g/mg h | R2 |  | qe mg/g |
| HG | 0.35 | 43.85 | 0.894 |  | 2.7E+07 | 65.18 | 0.996 |  | 0.35 | 211.43 | 0.934 |  | 0.35 |
| HG-Fe | 0.46 | 49.91 | 0.960 |  | 3.3E+12 | 74.37 | 0.994 |  | 0.47 | 224.12 | 0.982 |  | 0.47 |

Table 5.

| Material | qmax. (mg/g) | Reference |
| --- | --- | --- |
| Heat Treated Eggshells | 258.28 | [55] |
| Biopolymer-based nanohydroxyapatite composites | 135 | [56] |
| Granulated and calcined alum sludge | 0.033 | [57] |
| Stratified voids of MIL-53 (Al)-NH2 (MOFs) | 1014 | [58] |
| Chitosan composite impregnated with Fe(OH)3/CaO nanoparticles | 2.52 | [59] |
| Polypyrrole-based magnetic nanocomposite | 24.7 | [60] |
| Cow dung carbon impregnated with Ca - Fe (ICDC) | 9 | [61] |
| Magnetically charged cationic hydrogel with La | 136.78 | [62] |
| Cupric oxide nanoparticles | 3152 | [63] |
| Zr(IV)/Chitosan | 48.3 | [64] |
| Aluminum Modified Zeolite | 10.25 | [65] |
| Money plant (Epipremnum aureum) | 1.54 | [66] |
| Lemon leaf adsorbent | 1.4 | [67] |
| Fungus Pleurotus eryngii | 66.6 | [68] |
| Tamarind shell activated with ammonium carbonate | 19.5 | [69] |
| Acid Treated Bentonite | 0.103 | [70] |
| Hematite with Al(OH)3 | 0.54 | [71] |
| Calcined MgAlCO3 layered double hydroxides | 213.8 | [72] |
| PVA/PVP hydrogels modified with FeCl3 | 0.46 | This work |

Table 6.

| Sample | Pseudo first order (Lagergren) |  |  |  | Second order (Elovich) |  |  |  | Pseudo second order (Ho-McKay) |  |  |  | Experimental |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qe mg/g | KL 1/h | R2 |  | a mg/g h | b g/mg | R2 |  | qe mg/g | K2 g/mg h | R2 |  | qe mg/g |
| HG | 0.35 | 2.58 | 0.991 |  | 10.67 | 23.48 | 0.916 |  | 0.36 | 10.62 | 0.968 |  | 0.35 |
| HG-Fe | 0.35 | 1.90 | 0.924 |  | 5.48 | 20.88 | 0.927 |  | 0.37 | 7.35 | 0.966 |  | 0.36 |

Table 7.

|  |  | Calculated constants of Langmuir, Freundlich, and L–F |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorbent |  | Langmuir |  |  |  | Freundlich |  |  |  | Langmuir-Freundlich (L-F) |  |  |  |
|  | T K | KL L/mg | qm mg/g | R2 |  | KF (mg/g)(L/mg)1/n | n | R2 |  | a mg/g | KLF L/mg | n | R2 |
| HG | 293 | 1.78 | 12.30 | 0.983 |  | 0.13 | 2.81 | 0.922 |  | 0.89 | 10.98 | 0.5 | 0.984 |
|  | 298 | 3.02 | 11.02 | 0.991 |  | 0.16 | 1.96 | 0.965 |  | 1.05 | 5.87 | 0.4 | 0.989 |
|  | 308 | 6.09 | 4.78 | 0.977 |  | 0.20 | 1.78 | 0.973 |  | 2.46 | 11.78 | 0.4 | 0.977 |
|  | 318 | 5.79 | 3.97 | 0.994 |  | 0.32 | 2.88 | 0.972 |  | 0.54 | 2.16 | 0.3 | 0.994 |
| HG-Fe | 293 | 2.55 | 11.40 | 0.991 |  | 0.13 | 2.24 | 0.967 |  | 0.76 | 8.74 | 0.3 | 0.991 |
|  | 298 | 3.37 | 10.06 | 0.992 |  | 0.16 | 1.72 | 0.954 |  | 1.90 | 10.44 | 0.35 | 0.993 |
|  | 308 | 5.05 | 8.85 | 0.997 |  | 0.18 | 1.58 | 0.975 |  | 2.21 | 11.17 | 0.25 | 0.997 |
|  | 318 | 5.04 | 3.65 | 0.993 |  | 0.25 | 2.19 | 0.926 |  | 2.27 | 8.28 | 0.45 | 0.992 |

Table 8.

| Material | Parameter | Temperature (K) |  |  |
| --- | --- | --- | --- | --- |
|  |  | 293 | 298 | 308 |
| HG | ΔG° J/mol | 55707 | 56657 | 58558 |
|  | ΔS° J/mol K | -190.13 |  |  |
|  | ΔH° J/mol | -0.0096 |  |  |
| HG-Fe | ΔG° J/mol | 29546 | 30050 | 31059 |
|  | ΔS° J/mol K | -100.84 |  |  |
|  | ΔH° J/mol | -0.0054 |  |  |