Supplemental information

Fostering the Waste Management: Environmental-resource Interacting Attribute

List of contents

Text S1 Estimation of recyclability and removability	S1

Text S2: The determination of the grade of recyclability (D) and removability (D’) for chemically combined substances: the case of Fe, FeS, and Fe2O3	S2

Table S1 Value of crustal abundance and cut-off grade. For more details, see the cited references.	S3

Table S2 Determination of the Hi, Di, and Di’of gold cyanide tailing in elements (compounds) recycling process	S5

Table S3 Determination of the Hi, Di, and Di’of copper tailing in elements (compounds) recycling process	S5

Table S4 Determination of the Hi, Di, and Di’of iron tailing in elements (compounds) recycling process	S6

Table S5 Determination of the Hi, Di, and Di’of non-ferrous metal tailing in elements (compounds) recycling process	S7

Table S6 Determination of the Hi, Di, and Di’of iron and steel slag in elements (compounds) recycling process	S8

Table S7 Determination of the Hi, Di, and Di’of copper slag in elements (compounds) recycling process	S9

Table S8 Determination of the Hi, Di, and Di’of lead-zinc slag in elements (compounds) recycling process	S10

Table S9 Determination of the Hi, Di, and Di’of red mud in elements (compounds) recycling process	S10

Table S10 Determination of the Hi, Di, and Di’of coal gangue in elements (compounds) recycling process	S11

Table S11 Determination of the Hi, Di, and Di’of coal fly ash in elements (compounds) recycling process	S12

Table S12 Determination of the Hi, Di, and Di’of desulfurization gypsum in elements (compounds) recycling process	S12

Table S13 Determination of the Hi, Di, and Di’of phosphogypsum in elements (compounds) recycling process	S13

Table S14 Determination of the Hi, Di, and Di’of gold cyanide tailing in downcycling use	S13

Table S15 Determination of the Hi, Di, and Di’of copper tailing in downcycling use	S14

Table S16 Determination of the Hi, Di, and Di’of iron tailing in downcycling use	S15

Table S17 Determination of the Hi, Di, and Di’of non-ferrous metal tailing in downcycling use	S15

Table S18 Determination of the Hi, Di, and Di’of iron and steel slag in downcycling use	S17

Table S19 Determination of the Hi, Di, and Di’of copper slag in downcycling use	S17

Table S20 Determination of the Hi, Di, and Di’of lead-zinc slag in downcycling use	S18

Table S21 Determination of the Hi, Di, and Di’of red mud in downcycling use	S19

Table Determination of the Hi, Di, and Di’of coal gangue in downcycling use	S19

Table S23 Determination of the Hi, Di, and Di’of coal fly ash in downcycling use	S20

Table S24 Determination of the Hi, Di, and Di’of desulfurization gypsum in downcycling use	S20

Table S25 Determination of the Hi, Di, and Di’of the phosphogypsum in downcycling use	S21

Table S26 Determination of the Di’of the IW in landfill	S22

Table S27 ERIA of typical IW in elements recycling scenario	S24

Table S28 ERIA of typical IW in compounds recycling scenario	S24

Table S29 ERIA of typical IW in downcycling scenario	S25

Table S30 ERIA of typical IW in landfill scenario	S26

Fig. S1 Elements analyzed in this study	S27

Fig. S2 Box-and-whisker plot for recyclability, removability, and ERIA of IW by categories.	S27

Fig. S3 ERIA assessment for different scenarios: case of gold cyanide tailing	S29

Fig. S4 Effect of n missing on the stability of environmental-resource interacting attribute evaluation models	S29

SI References	S29

# Text S1 Estimation of recyclability and removability

Recyclability and removability reflect the recycling and removing difficulty in industrial solid waste, respectively. Based on previous research (1, 2), recyclability and removability were determined by the following equations:

where pi is the concentration of substance i (%), n is the total number of the substance in the IW sample and H is the entropy of the IW sample (bit). D and R are the grade and recyclability of the IW sample, respectively, and the details of the parameter in Eqs. (2) and (3) refer to Zeng’s study (1).

where D’ is the removal grade of the IW sample, m’ is the number of the metal removed from the IW sample, ji’ is the stability of the valence of the metal ranks from low to high, N’ is the total number of metal valences, R’ is the removability of the IW sample (bit-1), and 100 is the coefficient of amplification.

# Text S2: The determination of the grade of recyclability (D) and removability (D’) for chemically combined substances: the case of Fe, FeS, and Fe2O3

i. iron in a certain solid waste generally has three valences (i.e., 0, +2, +3)

ii. if the iron was only in the singlet form and consistent with the target phase, m = i = 1, N = 3, j = 1, and D = 1;

iii. if the iron was only in the FeS form and the target phase was monomeric iron, m = i = 1, N = 3, j = 2, and D = 2/3;

iv. if the iron was only in the Fe2O3 form and the target phase was monomeric iron, m = i = 1, N = 3, j = 3, and D = 1/3;

v. if the solid waste is a mixture containing 20% Fe, 30% FeS, and 50% Fe2O3 (mass fraction), D = 1×20% + 2/3×30% +1/3×50% = 17/30.

vi. grad of the removability calculation is the same as that of recyclability. But the values of m’ and j’ are taken differently, referring to Text S1.

# Table S1 Value of crustal abundance and cut-off grade. For more details, see the cited references.

| Metal | Crustal abundance (3) (%) | Cut-off grade (%) |
| --- | --- | --- |
| Lead (Pb) | 1.4E-03 | 0.2 |
| Hydrargyrum (Hg) | 8.5E-06 | 0.005 |
| Cadmium (Cd) | 1.5E-05 | 0.001 |
| Chromium (Cr) | 1.0E-02 | 5 |
| Arsenic (As) | 1.8E-04 | 0.02 |
| Nickel (Ni) | 8.4E-03 | 0.1 |
| Copper (Cu) | 6.0E-03 | 0.05 |
| Zinc (Zn) | 7.0E-03 | 0.4 |
| Silver (Ag) | 7.5E-06 | 0.0001 |
| Vanadium (V) | 1.2E-02 | 0.15 |
| Manganese (Mn) | 9.5E-02 | 4 |
| Cobalt (Co) | 2.5E-03 | 0.01 |
| Thallium (Tl) | 8.5E-05 | 0.001 |
| Antimony (Sb) | 2.0E-05 | 0.4 |
| Lithium (Li) | 2.0E-03 | 0.02 |
| Beryllium (Be) | 2.8E-04 | 0.03 |
| Boron (B) | 1.0E-03 | 1 |
| Aluminum (Al) | 8.2E+00 | 40 |
| Titanium (Ti) | 5.6E-01 | 5 |
| Iron (Fe) | 5.6E+00 | 10 |
| Gallium (Ga) | 1.9E-03 | 0.001 |
| Germanium (Ge) | 1.5E-04 | 0.001 |
| Selenium (Se) | 5.0E-06 | 0.0006 |
| Strontium (Sr) | 3.7E-02 | 12 |
| Zirconium (Zr) | 1.7E-02 | 0.04 |
| Niobium (Nb) | 2.0E-03 | 0.004 |
| Molybdenum (Mo) | 1.2E-04 | 0.01 |
| Indium (In) | 2.5E-05 | 0.001 |
| Tin (Sn) | 2.3E-04 | 0.03 |
| Tellurium (Te) | 1.0E-07 | 0.0002 |
| Barium (Ba) | 4.3E-02 | 8 |
| Hafnium (Hf) | 3.0E-04 | 0.0001 |
| Tantalum (Ta) | 2.0E-04 | 0.004 |
| Tungsten (W) | 1.3E-04 | 0.02 |
| Rhenium (Re) | 7.0E-08 | 0.001 |
| Gold (Au) | 4.0E-07 | 0.00001 |
| Bismuth (Bi) | 8.5E-07 | 0.01 |
| Palladium (Pd)a | 4.1E-07 | 0.000008 |
| Platinum (Pt)a | 4.1E-07 | 0.000008 |
| Irdium (Ir)a | 4.1E-07 | 0.000008 |
| Ruthenium (Ru)a | 4.1E-07 | 0.000008 |
| Lanthanum (La)a | 6.3E-03 | 0.05 |
| Yttrium (Y)a | 6.3E-03 | 0.05 |
| Scandium (Sc)a | 6.3E-03 | 0.05 |
| Magnesium (Mg) | 2.33 | 19 |
| Carbon (C) | 0.048 | / |
| Silicon (Si) | 28.2 | / |
| Phosphorus (P) | 0.105 | 1 |
| Sulfur (S) | 0.035 | 1 |

Note:

a Crustal abundance and metal market prices of PGM and REE use their mean values.

# Table S2 Determination of the Hi, Di, and Di’of gold cyanide tailing in elements (compounds) recycling process

| Element | Crustal abundance (%) | Cut-off grade (%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' |  | Di | Di' |
| Pb | 0.0014 | 0.2 | 3 | 3 | 2 | 0.45 | 0.035 | 0.33 | 1 |  | 1 | 1 |
| Cu | 0.006 | 0.05 | 3 | 3 | 3 | 0.14 | 0.013 | 0.33 | 1 |  | 1 | 1 |
| Zn | 0.007 | 0.4 | 2 | 2 | 2 | 0.15 | 0.014 |  | 0.5 |  |  | 0.5 |
| Ag | 0.0000075 | 0.0001 | 2 | 2 | 2 | 0.001 | 0.00017 | 0.5 | 1 |  | 1 | 1 |
| Al | 8.23 | 40 | 2 | 2 | 2 | 7.06 | 0.27 |  |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 3.91 | 0.18 |  |  |  |  |  |
| Au | 0.0000004 | 0.00001 | 2 | 1 | 1 | 0.0003 | 5.5E-05 | 1 | 1 |  | 1 | 1 |
| C | 0.048 | / |  |  |  | 4.52 | 0.20 |  |  |  |  |  |
| O | 46.1 | / |  |  |  | 52.31 | 0.49 |  |  |  |  |  |
| Si | 28.2 | / |  |  |  | 21.26 | 0.48 |  |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 2.29 | 0.13 | 1 | 1 |  | 1 | 1 |
| Other |  |  |  |  |  | 7.9087 | 0.29 |  |  |  |  |  |

# Table S3 Determination of the Hi, Di, and Di’of copper tailing in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Pb | 0.0014 | 0.2 | 3 | 3 | 2 | 0.01 | 0.0013 |  | 0.67 |  | 0.67 |
| Cd | 0.000015 | 0.001 | 3 | 3 | 3 | 0.0002 | 3.8E-05 |  | 0.33 |  | 0.33 |
| Cr | 0.0102 | 5 | 3 | 3 | 2 | 0.002 | 0.00031 |  |  |  |  |
| As | 0.00018 | 0.02 | 3 | 3 | 2 | 0.01 | 0.0013 |  | 0.67 |  | 0.67 |
| Ni | 0.0084 | 0.1 | 3 | 3 | 2 | 0.004 | 0.00058 |  |  |  |  |
| Cu | 0.006 | 0.05 | 3 | 3 | 3 | 0.29 | 0.024 | 0.333333 | 1 | 1 | 1 |
| Zn | 0.007 | 0.4 | 2 | 2 | 2 | 0.05 | 0.0055 |  | 0.5 |  | 0.5 |
| V | 0.012 | 0.15 | 5 | 5 | 5 | 0.006 | 0.00084 |  |  |  |  |
| Mn | 0.095 | 4 | 3 | 3 | 3 | 0.15 | 0.014 |  | 0.33 |  | 0.33 |
| Co | 0.0025 | 0.01 | 3 | 3 | 2 | 0.006 | 0.00084 |  | 0.67 |  | 0.67 |
| Al | 8.23 | 40 | 2 | 2 | 2 | 5.5 | 0.23 |  |  |  |  |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 0.3 | 0.025 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 13.09 | 0.38 | 0.33 | 1 | 1 | 1 |
| Se | 0.000005 | 0.0006 | 4 | 4 | 3 | 0.0002 | 3.8E-05 |  | 0.5 |  | 0.5 |
| Sr | 0.037 | 12 | 2 | 2 | 2 | 0.004 | 0.00058 |  |  |  |  |
| K | 2.09 | 2 |  |  |  | 2.2 | 0.12 |  |  |  |  |
| Na | 2.36 | 10 |  |  |  | 1 | 0.066 |  |  |  |  |
| Ca | 4.15 | 48 |  |  |  | 3.6 | 0.17 |  |  |  |  |
| Mg | 2.33 | 19 |  |  |  | 1.6 | 0.095 |  |  |  |  |
| O | 46.1 | / |  |  |  | 41.67 | 0.53 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 23 | 0.49 |  |  |  |  |
| P | 0.105 | 1 |  |  |  | 0.09 | 0.0091 |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 1 | 0.066 | 1 | 1 | 1 | 1 |
| Other |  |  |  |  |  | 6.4176 | 0.25 |  |  |  |  |

# Table S4 Determination of the Hi, Di, and Di’of iron tailing in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Cr | 0.0102 | 5 | 3 | 3 | 2 | 0.02 | 0.0025 |  | 0.67 |  | 0.67 |
| Cu | 0.006 | 0.05 | 3 | 3 | 3 | 0.01 | 0.0013 |  | 0.33 |  | 0.33 |
| Zn | 0.007 | 0.4 | 2 | 2 | 2 | 0.004 | 0.00058 |  |  |  |  |
| Mn | 0.095 | 4 | 3 | 3 | 3 | 0.06 | 0.0064 |  |  |  |  |
| Al | 8.23 | 40 | 2 | 2 | 2 | 1.03 | 0.068 |  |  |  |  |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 0.02 | 0.0025 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 11.039 | 0.35 | 0.33 | 1 | 1 | 1 |
| K | 2.09 | 2 |  |  |  | 0.21 | 0.019 |  |  |  |  |
| Na | 2.36 | 10 |  |  |  | 0.22 | 0.019 |  |  |  |  |
| Ca | 4.15 | 48 |  |  |  | 1.06 | 0.070 |  |  |  |  |
| Mg | 2.33 | 19 |  |  |  | 1.76 | 0.10 |  |  |  |  |
| O | 46.1 | / |  |  |  | 48.54 | 0.51 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 35.79 | 0.53 |  |  |  |  |
| P | 0.105 | 1 |  |  |  | 0.09 | 0.0091 |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 0.08 | 0.0082 |  | 0.75 |  | 0.75 |
| Cl | 0.0145 | / | 2 | 1 | 2 | 0.06 | 0.0064 |  | 0.5 |  | 0.5 |
| Other |  |  |  |  |  | 0.007 | 0.00097 |  |  |  |  |

Note: * 50% of each valence

# Table S5 Determination of the Hi, Di, and Di’of non-ferrous metal tailing in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Pb | 0.0014 | 0.2 | 3 | 3 | 2 | 0.05 | 0.0055 |  | 0.67 |  | 0.67 |
| Cd | 0.000015 | 0.001 | 3 | 3 | 3 | 0.0003 | 5.5E-05 |  | 0.33 |  | 0.33 |
| Cr | 0.0102 | 5 | 3 | 3 | 2 | 0.01 | 0.0013 |  |  |  |  |
| Ni | 0.0084 | 0.1 | 3 | 3 | 2 | 0.02 | 0.0025 |  | 0.67 |  | 0.67 |
| Cu | 0.006 | 0.05 | 3 | 3 | 3 | 0.005 | 0.00071 |  |  |  |  |
| Zn | 0.007 | 0.4 | 2 | 2 | 2 | 0.02 | 0.0025 |  | 0.5 |  | 0.5 |
| Mn | 0.095 | 4 | 3 | 3 | 3 | 0.11 | 0.011 |  | 0.33 |  | 0.33 |
| Al | 8.23 | 40 | 2 | 2 | 2 | 6.54 | 0.26 |  |  |  |  |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 0.41 | 0.033 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 4.43 | 0.20 |  |  |  |  |
| Sr | 0.037 | 12 | 2 | 2 | 2 | 0.17 | 0.016 |  | 0.5 |  | 0.5 |
| Zr | 0.0165 | 0.04 | 2 | 2 | 2 | 0.026 | 0.0031 |  | 0.5 |  | 0.5 |
| Mo | 0.00012 | 0.01 | 2 | 2 | 2 | 0.03 | 0.0035 | 0.5 | 1 | 1 | 1 |
| Ba | 0.0425 | 8 | 2 | 2 | 2 | 0.098 | 0.0098 |  | 0.5 |  | 0.5 |
| K | 2.09 | 2 |  |  |  | 4.22 | 0.19 |  |  |  |  |
| Na | 2.36 | 10 |  |  |  | 1.08 | 0.071 |  |  |  |  |
| Ca | 4.15 | 48 |  |  |  | 4.28 | 0.19 |  |  |  |  |
| Mg | 2.33 | 19 |  |  |  | 1.16 | 0.075 |  |  |  |  |
| O | 46.1 | / |  |  |  | 46 | 0.52 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 29.7 | 0.52 |  |  |  |  |
| P | 0.105 | 1 |  |  |  | 0.12 | 0.012 |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 0.72 | 0.051 |  | 0.75 |  | 0.75 |
| Other |  |  |  |  |  | 0.8007 | 0.056 |  |  |  |  |

# Table S6 Determination of the Hi, Di, and Di’of iron and steel slag in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Al | 8.23 | 40 | 2 | 2 | 2 | 2.47 | 0.13 |  |  |  |  |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 0.41 | 0.033 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 24.29 | 0.50 | 0.33 | 1 | 1 | 1 |
| Ca | 4.15 | 48 |  |  |  | 21.71 | 0.48 |  |  |  |  |
| Mg | 2.33 | 19 |  |  |  | 7.86 | 0.29 |  |  |  |  |
| O | 46.1 | / |  |  |  | 34.29 | 0.53 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 6.39 | 0.25 |  |  |  |  |
| P | 0.105 | 1 |  |  |  | 0.14 | 0.013 |  |  |  |  |
| Other |  |  |  |  |  | 2.44 | 0.13 |  |  |  |  |

# Table S7 Determination of the Hi, Di, and Di’of copper slag in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Pb | 0.0014 | 0.2 | 3 | 3 | 2 | 1.78 | 0.10 | 0.33 | 1 | 1 | 1 |
| Ni | 0.0084 | 0.1 | 3 | 3 | 2 | 0.25 | 0.022 | 0.33 | 1 | 1 | 1 |
| Cu | 0.006 | 0.05 | 3 | 3 | 3 | 10.6 | 0.34 | 0.33 | 1 | 1 | 1 |
| Zn | 0.007 | 0.4 | 2 | 2 | 2 | 0.47 | 0.036 | 0.5 | 1 | 1 | 1 |
| Al | 8.23 | 40 | 2 | 2 | 2 | 0.55 | 0.041 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 40.2 | 0.53 | 0.33 | 1 | 1 | 1 |
| Ca | 4.15 | 48 |  |  |  | 0.2 | 0.018 |  |  |  |  |
| O | 46.1 | / |  |  |  | 17.45 | 0.44 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 12.27 | 0.37 |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 1.9 | 0.11 | 1 | 1 | 1 | 1 |
| Other |  |  |  |  |  | 14.33 | 0.40 |  |  |  |  |

# Table S8 Determination of the Hi, Di, and Di’of lead-zinc slag in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Pb | 0.0014 | 0.2 | 3 | 3 | 2 | 0.92 | 0.062 | 0.33 | 1 | 1 | 1 |
| Zn | 0.007 | 0.4 | 2 | 2 | 2 | 3.2 | 0.16 | 0.5 | 1 | 1 | 1 |
| Mn | 0.095 | 4 | 3 | 3 | 3 | 1.39 | 0.086 |  | 0.33 |  | 0.33 |
| Al | 8.23 | 40 | 2 | 2 | 2 | 5.99 | 0.24 |  |  |  |  |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 0.36 | 0.029 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 20.84 | 0.47 | 0.33 | 1 | 1 | 1 |
| K | 2.09 | 2 |  |  |  | 0.93 | 0.063 |  |  |  |  |
| Na | 2.36 | 10 |  |  |  | 2.41 | 0.13 |  |  |  |  |
| Ca | 4.15 | 48 |  |  |  | 9.67 | 0.33 |  |  |  |  |
| Mg | 2.33 | 19 |  |  |  | 3.67 | 0.17 |  |  |  |  |
| O | 46.1 | / |  |  |  | 34.23 | 0.53 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 12.94 | 0.38 |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 2.15 | 0.12 | 1 | 1 | 1 | 1 |
| Other |  |  |  |  |  | 1.3 | 0.081 |  |  |  |  |

# Table S9 Determination of the Hi, Di, and Di’of red mud in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Al | 8.23 | 40 | 2 | 2 | 2 | 12.39 | 0.37 |  | 0.5 |  | 0.5 |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 2.64 | 0.14 |  | 0.75 |  | 0.75 |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 10.99 | 0.35 | 0.33 | 1 | 1 | 1 |
| Na | 2.36 | 10 |  |  |  | 6.97 | 0.276 |  |  |  |  |
| Ca | 4.15 | 48 |  |  |  | 9.5 | 0.32 |  |  |  |  |
| Mg | 2.33 | 19 |  |  |  | 0.78 | 0.055 |  |  |  |  |
| O | 46.1 | / |  |  |  | 34.41 | 0.53 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 8.91 | 0.31 |  |  |  |  |
| Other |  |  |  |  |  | 13.41 | 0.39 |  |  |  |  |

# Table S10 Determination of the Hi, Di, and Di’of coal gangue in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling | Compound recycling |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di' | Di' |
| Mn | 0.095 | 4 | 3 | 3 | 3 | 0.01 | 0.0013 |  |  |
| Al | 8.23 | 40 | 2 | 2 | 2 | 20.55 | 0.47 | 0.5 | 0.5 |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 0.59 | 0.044 | 0.75 | 0.75 |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 0.18 | 0.016 |  |  |
| K | 2.09 | 2 |  |  |  | 0.07 | 0.0073 |  |  |
| Na | 2.36 | 10 |  |  |  | 0.02 | 0.0025 |  |  |
| Ca | 4.15 | 48 |  |  |  | 0.11 | 0.011 |  |  |
| Mg | 2.33 | 19 |  |  |  | 0.05 | 0.0055 |  |  |
| O | 46.1 | / |  |  |  | 42.83 | 0.52 |  |  |
| Si | 28.2 | / |  |  |  | 20.98 | 0.47 |  |  |
| P | 0.105 | 1 |  |  |  | 0.01 | 0.0013 |  |  |
| Other |  |  |  |  |  | 14.6 | 0.41 |  |  |

# Table S11 Determination of the Hi, Di, and Di’of coal fly ash in elements (compounds) recycling process

| Element | Crustal abundance(%) | Cut-off grade(%) | N (N') | j | j' | Content (%) | Hi | Element recycling | Compound recycling |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di' | Di' |
| Al | 8.23 | 40 | 2 | 2 | 2 | 11.7 | 0.36 | 0.5 | 0.5 |
| Ti | 0.56 | 5 | 4 | 2 | 2 | 0.38 | 0.031 |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 5.83 | 0.24 | 0.33 | 0.33 |
| K | 2.09 | 2 |  |  |  | 0.37 | 0.030 |  |  |
| Ca | 4.15 | 48 |  |  |  | 1.84 | 0.10606 |  |  |
| Mg | 2.33 | 19 |  |  |  | 0.55 | 0.041 |  |  |
| O | 46.1 | / |  |  |  | 45.61 | 0.52 |  |  |
| Si | 28.2 | / |  |  |  | 26.98 | 0.51 |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 0.29 | 0.024 | 0.75 | 0.75 |
| Other |  |  |  |  |  | 6.45 | 0.26 |  |  |

# Table S12 Determination of the Hi, Di, and Di’of desulfurization gypsum in elements (compounds) recycling process

| Element | Crustal abundance (%) | Cut-off grade (%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Al | 8.23 | 40 | 2 | 2 | 2 | 0.95 | 0.064 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 0.33 | 0.027 |  |  |  |  |
| Ca | 4.15 | 48 |  |  |  | 29.68 | 0.52 |  |  |  |  |
| O | 46.1 | / |  |  |  | 45 | 0.52 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 1.33 | 0.083 |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 20.41 | 0.47 | 1 | 1 | 1 | 1 |
| Other |  |  |  |  |  | 2.3 | 0.13 |  |  |  |  |

# Table S13 Determination of the Hi, Di, and Di’of phosphogypsum in elements (compounds) recycling process

| Element | Crustal abundance (%) | Cut-off grade (%) | N (N') | j | j' | Content (%) | Hi | Element recycling |  | Compound recycling |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Di | Di' | Di | Di' |
| Mn | 0.095 | 4 | 3 | 3 | 3 | 0.002 | 0.00031 |  |  |  |  |
| Al | 8.23 | 40 | 2 | 2 | 2 | 0.12 | 0.012 |  |  |  |  |
| Fe | 5.63 | 10 | 3 | 3 | 3 | 0.09 | 0.0091 |  |  |  |  |
| K | 2.09 | 2 |  |  |  | 0.07 | 0.0073 |  |  |  |  |
| Na | 2.36 | 10 |  |  |  | 0.03 | 0.0035 |  |  |  |  |
| Ca | 4.15 | 48 |  |  |  | 21.3 | 0.48 |  |  |  |  |
| Mg | 2.33 | 19 |  |  |  | 0.03 | 0.0035 |  |  |  |  |
| O | 46.1 | / |  |  |  | 38.92 | 0.53 |  |  |  |  |
| Si | 28.2 | / |  |  |  | 4.4 | 0.20 |  |  |  |  |
| P | 0.105 | 1 |  |  |  | 0.51 | 0.039 |  |  |  |  |
| S | 0.035 | 1 | 4 | 1 | 2 | 16.34 | 0.43 | 1 | 1 | 1 | 1 |
| F | 0.0585 | 5 | 2 | 1 | 2 | 0.52 | 0.039 |  | 0.5 |  | 0.5 |
| Cl | 0.0145 | / | 2 | 1 | 2 |  |  |  |  |  |  |
| Other |  |  |  |  |  | 17.668 | 0.44 |  |  |  |  |

# Table S14 Determination of the Hi, Di, and Di’of gold cyanide tailing in downcycling use

| GCT | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| Fe2O3 | 3.91 |  | 0.0391 |  |
| SiO2 | 21.26 |  | 0.2126 |  |
| Al2O3 | 7.06 |  | 0.0706 |  |
| SO3 | 2.29 |  |  | 0.0229 |
| Au | 0.00033 |  |  | 0.0000033 |
| Ag | 0.00092 |  |  | 0.0000092 |
| Cu | 0.14 |  |  | 0.0014 |
| Pb | 0.45 |  |  | 0.0045 |
| Zn | 0.15 |  |  | 0.0015 |
| Si-Ca-Al-Fe | 32.23 | 0.53 |  |  |
| other | 67.77 | 0.38 |  |  |

# Table S15 Determination of the Hi, Di, and Di’of copper tailing in downcycling use

| CT | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 5.1000 |  | 0.051 |  |
| Fe2O3 | 18.7000 |  | 0.19 | 0.19 |
| SiO2 | 49.4940 |  | 0.49 |  |
| TiO2 | 0.5000 |  |  |  |
| Al2O3 | 10.3000 |  | 0.10 |  |
| K2O | 2.6000 |  |  |  |
| Na2O | 1.3000 |  |  |  |
| MgO | 2.7000 |  |  |  |
| SO3 | 2.6000 |  |  | 0.026 |
| MnO | 0.2000 |  |  | 0.0020 |
| As | 0.0115 |  |  | 0.00012 |
| Cd | 0.0002 |  |  | 0.0000020 |
| Co | 0.0060 |  |  | 0.000060 |
| Cu | 0.2940 |  |  | 0.0029 |
| Cr | 0.0016 |  |  |  |
| Ni | 0.0039 |  |  |  |
| Pb | 0.0117 |  |  | 0.00012 |
| Se | 0.0002 |  |  | 0.0000020 |
| Sr | 0.0039 |  |  |  |
| V | 0.0059 |  |  |  |
| Zn | 0.0481 |  |  | 0.00048 |
| Si-Ca-Al-Fe | 83.5940 | 0.22 |  |  |
| other | 16.4060 | 0.43 |  |  |

# Table S16 Determination of the Hi, Di, and Di’of iron tailing in downcycling use

| IT | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| Fe2O3 | 12.34 |  | 0.12 | 0.12 |
| SiO2 | 76.65 |  | 0.77 |  |
| Al2O3 | 2.54 |  | 0.025 | 0.025 |
| Si-Ca-Al-Fe | 91.53 | 0.12 |  |  |
| other | 8.47 | 0.30 |  |  |

# Table S17 Determination of the Hi, Di, and Di’of non-ferrous metal tailing in downcycling use

| NFT | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 5.99 |  | 0.060 |  |
| Fe2O3 | 6.33 |  | 0.063 |  |
| P2O5 | 0.28 |  |  |  |
| SiO2 | 63.65 |  | 0.64 |  |
| TiO2 | 0.69 |  |  |  |
| Al2O3 | 12.36 |  | 0.12 |  |
| K2O | 5.08 |  |  |  |
| Na2O | 1.46 |  |  |  |
| MgO | 1.94 |  |  |  |
| SO3 | 1.80 |  |  | 0.018 |
| MnO | 0.07 |  |  | 0.00070 |
| NiO | 0.02 |  |  | 0.00020 |
| SrO | 0.12 |  |  | 0.0012 |
| ZnO | 0.01 |  |  | 0.00010 |
| BaO | 0.11 |  |  | 0.0011 |
| ZrO | 0.03 |  |  | 0.00030 |
| PbO | 0.03 |  |  | 0.00030 |
| MoO3 | 0.02 |  |  | 0.00020 |
| Cd | 0.00 |  |  | 0.0000026 |
| Cu | 0.01 |  |  |  |
| Cr | 0.01 |  |  |  |
| Ni | 0.01 |  |  | 0.000059 |
| Pb | 0.02 |  |  | 0.00020 |
| Sr | 0.07 |  |  | 0.00068 |
| Zn | 0.01 |  |  | 0.000084 |
| Mn | 0.06 |  |  | 0.00055 |
| Mo | 0.01 |  |  | 0.00014 |
| Si-Ca-Al-Fe | 88.33 | 0.16 |  |  |
| other | 11.67 | 0.36 |  |  |

# Table S18 Determination of the Hi, Di, and Di’of iron and steel slag in downcycling use

| I&S | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 30.40 |  | 0.30 |  |
| Fe2O3 | 34.70 |  | 0.35 | 0.35 |
| P2O5 | 0.32 |  |  |  |
| SiO2 | 13.70 |  | 0.14 |  |
| TiO2 | 0.68 |  |  |  |
| Al2O3 | 4.67 |  | 0.047 |  |
| MgO | 13.10 |  |  |  |
| Si-Ca-Al-Fe | 83.47 | 0.22 |  |  |
| other | 16.53 | 0.43 |  |  |

# Table S19 Determination of the Hi, Di, and Di’of copper slag in downcycling use

| CS | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 0.28 |  | 0.0028 |  |
| Fe2O3 | 40.2 |  | 0.40 | 0.40 |
| SiO2 | 26.3 |  | 0.26 |  |
| Al2O3 | 1.04 |  | 0.010 |  |
| SO3 | 4.75 |  |  | 0.048 |
| Cu | 10.6 |  |  | 0.11 |
| Ni | 0.25 |  |  | 0.0025 |
| Pb | 1.78 |  |  | 0.018 |
| Zn | 0.47 |  |  | 0.0047 |
| Si-Ca-Al-Fe | 67.82 | 0.38 |  |  |
| other | 32.18 | 0.53 |  |  |

# Table S20 Determination of the Hi, Di, and Di’of lead-zinc slag in downcycling use

| NFS | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 13.54 |  | 0.14 |  |
| Fe2O3 | 26.97 |  | 0.27 | 0.27 |
| SiO2 | 27.72 |  | 0.28 |  |
| TiO2 | 0.6 |  |  |  |
| Al2O3 | 11.32 |  | 0.11 |  |
| K2O | 1.12 |  |  |  |
| Na2O | 3.25 |  |  |  |
| MgO | 6.12 |  |  |  |
| SO3 | 2.15 |  |  | 0.022 |
| MnO | 1.79 |  |  | 0.018 |
| Pb | 0.92 |  |  | 0.0092 |
| Zn | 3.2 |  |  | 0.032 |
| Si-Ca-Al-Fe | 79.55 | 0.26 |  |  |
| other | 20.45 | 0.47 |  |  |

# Table S21 Determination of the Hi, Di, and Di’of red mud in downcycling use

| RM | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 13.3 |  | 0.13 |  |
| Fe2O3 | 15.7 |  | 0.16 | 0.16 |
| P2O5 |  |  |  |  |
| SiO2 | 19.1 |  | 0.19 |  |
| TiO2 | 4.4 |  |  | 0.044 |
| Al2O3 | 23.4 |  | 0.23 | 0.23 |
| K2O |  |  |  |  |
| Na2O | 9.4 |  |  |  |
| MgO | 1.3 |  |  |  |
| SO3 |  |  |  |  |
| Si-Ca-Al-Fe | 71.5 | 0.35 |  |  |
| other | 28.5 | 0.52 |  |  |

# Table Determination of the Hi, Di, and Di’of coal gangue in downcycling use

| CG | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 0.15 |  | 0.0015 |  |
| Fe2O3 | 0.26 |  | 0.0026 |  |
| P2O5 | 0.03 |  |  |  |
| SiO2 | 44.95 |  | 0.45 |  |
| TiO2 | 0.99 |  |  | 0.0099 |
| Al2O3 | 38.81 |  | 0.39 | 0.39 |
| K2O | 0.09 |  |  |  |
| Na2O | 0.03 |  |  |  |
| MgO | 0.09 |  |  |  |
| MnO | 0.01 |  |  |  |
| Si-Ca-Al-Fe | 84.17 | 0.21 |  |  |
| other | 15.83 | 0.42 |  |  |

# Table S23 Determination of the Hi, Di, and Di’of coal fly ash in downcycling use

| CFA | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 2.57 |  | 0.026 |  |
| Fe2O3 | 8.33 |  | 0.083 | 0.083 |
| P2O5 |  |  |  |  |
| SiO2 | 57.82 |  | 0.58 |  |
| TiO2 | 0.64 |  |  | 0.0064 |
| Al2O3 | 22.1 |  | 0.22 | 0.22 |
| K2O | 0.45 |  |  |  |
| Na2O |  |  |  |  |
| MgO | 0.91 |  |  |  |
| SO3 | 0.73 |  |  | 0.0073 |
| Si-Ca-Al-Fe | 90.82 | 0.13 |  |  |
| other | 9.18 | 0.32 |  |  |

# Table S24 Determination of the Hi, Di, and Di’of desulfurization gypsum in downcycling use

| DG | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 41.55 |  | 0.42 |  |
| Fe2O3 | 0.47 |  | 0.0047 | 0.0047 |
| SiO2 | 2.86 |  | 0.029 |  |
| Al2O3 | 1.8 |  | 0.018 | 0.018 |
| SO3 | 51.02 |  |  | 0.51 |
| Si-Ca-Al-Fe | 46.68 | 0.51 |  |  |
| other | 53.32 | 0.48 |  |  |

# Table S25 Determination of the Hi, Di, and Di’of the phosphogypsum in downcycling use

| PG | Content (%) | Hi | Di | Di' |
| --- | --- | --- | --- | --- |
| CaO | 29.82 |  | 0.30 |  |
| Fe2O3 | 0.132 |  | 0.0013 | 0.0013 |
| P2O5 | 1.17 |  |  |  |
| SiO2 | 9.43 |  | 0.094 |  |
| TiO2 |  |  |  |  |
| F | 0.52 |  |  | 0.0052 |
| Al2O3 | 0.236 |  | 0.0024 | 0.0024 |
| K2O | 0.086 |  |  |  |
| Na2O | 0.043 |  |  |  |
| MgO | 0.055 |  |  |  |
| SO3 | 40.86 |  |  | 0.41 |
| MnO | 0.002 |  |  | 0.000020 |
| Si-Ca-Al-Fe | 39.618 | 0.53 |  |  |
| other | 60.382 | 0.44 |  |  |

# Table S26 Determination of the Di’of the IW in landfill

| Element | Crustal abundance (%) | N' | j' | Content (%) |  |  |  |  |  |  |  |  |  |  |  | D' |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | GCT | CT | IT | NFT | I&S | CS | NFS | RM | CG | CFA | DG | PG | GCT | CT | IT | NFT | I&S | CS | NFS | RM | CG | CFA | DG | PG |
| Pb | 0.0014 | 3 | 2 | 0.45 | 0.01 |  | 0.05 |  | 1.78 | 0.92 |  |  |  |  |  | 0.67 | 0.67 |  | 0.67 |  | 0.67 | 0.67 |  |  |  |  |  |
| Cd | 0.000015 | 3 | 3 |  | 0.0002 |  | 0.0003 |  |  |  |  |  |  |  |  |  | 0.33 |  | 0.33 |  |  |  |  |  |  |  |  |
| Cr | 0.0102 | 3 | 2 |  |  | 0.02 |  |  |  |  |  |  |  |  |  |  |  | 0.67 |  |  |  |  |  |  |  |  |  |
| As | 0.00018 | 3 | 2 |  | 0.01 |  |  |  |  |  |  |  |  |  |  |  | 0.67 |  |  |  |  |  |  |  |  |  |  |
| Ni | 0.0084 | 3 | 2 |  |  |  | 0.02 |  | 0.25 |  |  |  |  |  |  |  |  |  | 0.67 |  | 0.67 |  |  |  |  |  |  |
| Cu | 0.006 | 3 | 3 | 0.14 | 0.29 | 0.01 |  |  | 10.6 |  |  |  |  |  |  | 0.33 | 0.33 | 0.33 |  |  | 0.33 |  |  |  |  |  |  |
| Zn | 0.007 | 2 | 2 | 0.15 | 0.05 |  | 0.02 |  | 0.47 | 3.2 |  |  |  |  |  | 0.5 | 0.5 |  | 0.5 |  | 0.5 | 0.5 |  |  |  |  |  |
| Ag | 0.0000075 | 2 | 2 | 0.001 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |  |  |  |  |  |  |  |  |  |  |  |
| Mn | 0.095 | 3 | 3 |  | 0.15 |  | 0.11 |  |  | 1.39 |  |  |  |  |  |  | 0.33 |  | 0.33 |  |  | 0.33 |  |  |  |  |  |
| Co | 0.0025 | 3 | 2 |  | 0.006 |  |  |  |  |  |  |  |  |  |  |  | 0.67 |  |  |  |  |  |  |  |  |  |  |
| Al | 8.23 | 2 | 2 |  |  |  |  |  |  |  | 12.39 | 20.55 | 11.7 |  |  |  |  |  |  |  |  |  | 0.5 | 0.5 | 0.5 |  |  |
| Ti | 0.56 | 4 | 2 |  |  |  |  |  |  |  | 2.64 | 0.59 |  |  |  |  |  |  |  |  |  |  | 0.75 | 0.75 |  |  |  |
| Fe | 5.63 | 3 | 3 |  | 13.09 | 11.039 |  | 24.29 | 40.2 | 20.84 | 10.99 |  | 5.83 |  |  |  | 0.33 | 0.33 |  | 0.33 | 0.33 | 0.33 | 0.33 |  | 0.33 |  |  |
| Se | 0.000005 | 4 | 3 |  | 0.0002 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |  |  |  |  |  |  |  |  |  |  |
| Sr | 0.037 | 2 | 2 |  |  |  | 0.17 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |  |  |  |  |  |  |  |  |
| Zr | 0.0165 | 2 | 2 |  |  |  | 0.026 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |  |  |  |  |  |  |  |  |
| Mo | 0.00012 | 2 | 2 |  |  |  | 0.03 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |  |  |  |  |  |  |  |  |
| Ba | 0.0425 | 2 | 2 |  |  |  | 0.098 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |  |  |  |  |  |  |  |  |
| Au | 0.0000004 | 2 | 1 | 0.0003 |  |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  |  |  |  |  |  |  |
| S | 0.035 | 4 | 2 | 2.29 | 1 | 0.08 | 0.72 |  | 1.9 | 2.15 |  |  | 0.29 | 20.41 | 16.34 | 0.75 | 0.75 | 0.75 | 0.75 |  | 0.75 | 0.75 |  |  | 0.75 | 0.75 | 0.75 |
| F | 0.0585 | 2 | 2 |  |  |  |  |  |  |  |  |  |  |  | 0.52 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |
| Cl | 0.0145 | 2 | 2 |  |  | 0.06 |  |  |  |  |  |  |  |  |  |  |  | 0.5 |  |  |  |  |  |  |  |  |  |

# Table S27 ERIA of typical IW in elements recycling scenario

| Source/Categories |  | n | H (bit) | m | m' | D | D' | R (bit-1) | R' (bit-1) | A (bit-1) |  | θ (°) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tailings | GCT | 12±4 | 2.29±0.28 | 4±2 | 6±4 | 2.50±1.30 | 4.92±2.93 | 8.78±4.48 | 16.34±6.63 |  | 18.65±7.70 |  | 26.79±7.41 |
|  | CT | 15±7 | 2.18±0.19 | 2±1 | 6±3 | 1.11±0.34 | 4.58±1.81 | 3.73±1.06 | 15.61±7.70 |  | 16.17±7.46 |  | 16.17±10.39 |
|  | IT | 12±4 | 1.92±0.18 | 1±1 | 3±1 | 0.22±0.17 | 1.76±0.83 | 1.30±1.36 | 8.09±2.96 |  | 8.24±3.11 |  | 7.36±7.04 |
|  | NFT | 14±5 | 2.43±0.24 | 2±2 | 5±2 | 1.06±0.96 | 3.64±1.31 | 3.49±3.43 | 10.91±2.94 |  | 11.67±3.81 |  | 14.81±11.90 |
| Smelting slag | I&S | 9±2 | 2.35±0.08 | 1±0 | 1±0 | 0.27±0.15 | 0.80±0.45 | 1.20±0.70 | 3.60±2.09 |  | 3.79±2.20 |  | 32.75±32.00 |
|  | CS | 11±0 | 1.96±0.50 | 4±2 | 5±2 | 1.77±0.72 | 4.77±1.62 | 8.63±4.32 | 23.69±12.54 |  | 25.25±13.18 |  | 20.42±3.41 |
|  | NFS | 12±4 | 2.59±0.20 | 3±1 | 5±2 | 1.39±0.46 | 4.50±1.21 | 4.67±1.31 | 14.88±2.93 |  | 15.64±2.95 |  | 17.54±5.22 |
| Red mud | RM | 9±1 | 2.48±0.18 | 1±0 | 3±1 | 0.28±0.14 | 2.18±0.50 | 1.29±0.65 | 9.98±1.93 |  | 10.08±1.93 |  | 7.36±4.13 |
| Coal-based solid waste | CG | 9±3 | 2.04±0.07 | 0±0 | 2±1 | 0.00±0.00 | 0.95±0.67 | 0.00±0.00 | 4.68±2.32 |  | 4.68±2.32 |  | 0.00±0.00 |
|  | CFA | 10±1 | 2.15±0.13 | 0±0 | 2±1 | 0.17±0.41 | 1.51±0.42 | 0.63±1.55 | 7.54±2.02 |  | 7.80±1.47 |  | 7.50±18.37 |
| Industrial by-product gypsum | DG | 10±2 | 1.87±0.18 | 1±0 | 2±1 | 0.80±0.45 | 1.20±0.45 | 4.39±2.83 | 6.54±2.12 |  | 8.19±2.49 |  | 32.31±19.75 |
|  | PG | 12±1 | 2.12±0.10 | 1±0 | 2±1 | 1.00±0.00 | 1.33±0.26 | 4.08±0.45 | 5.43±1.20 |  | 6.81±1.09 |  | 37.46±5.84 |

# Table S28 ERIA of typical IW in compounds recycling scenario

| Source/Categories |  | n | H (bit) | m | m' | D | D' | R (bit-1) | R' (bit-1) | A (bit-1) |  | θ (°) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tailings | GCT | 12±4 | 2.29±0.28 | 4±2 | 6±4 | 4.20±2.17 | 4.92±2.93 | 14.52±5.92 | 16.34±6.63 |  | 21.89±8.79 |  | 41.93±3.78 |
|  | CT | 15±7 | 2.18±0.19 | 2±1 | 6±3 | 2.33±0.82 | 4.58±1.81 | 8.38±4.72 | 15.61±7.70 |  | 17.75±8.94 |  | 28.16±5.34 |
|  | IT | 12±4 | 1.92±0.18 | 1±1 | 3±1 | 0.67±0.52 | 1.76±0.83 | 3.91±4.08 | 8.09±2.96 |  | 9.31±4.27 |  | 19.58±17.66 |
|  | NFT | 14±5 | 2.43±0.24 | 2±2 | 5±2 | 2.00±1.67 | 3.64±1.31 | 6.61±6.05 | 10.91±2.94 |  | 13.27±5.41 |  | 25.60±18.51 |
| Smelting slag | I&S | 9±2 | 2.35±0.08 | 1±0 | 1±0 | 0.80±0.45 | 0.80±0.45 | 3.60±2.09 | 3.60±2.09 |  | 5.09±2.95 |  | 54.00±20.12 |
|  | CS | 11±0 | 1.96±0.50 | 4±2 | 5±2 | 4.40±1.52 | 4.77±1.62 | 21.92±11.75 | 23.69±12.54 |  | 32.29±17.15 |  | 42.85±2.25 |
|  | NFS | 12±4 | 2.59±0.20 | 3±1 | 5±2 | 3.33±0.82 | 4.50±1.21 | 11.40±3.54 | 14.88±2.93 |  | 18.82±4.22 |  | 36.86±6.24 |
| Red mud | RM | 9±1 | 2.48±0.18 | 1±0 | 3±1 | 0.83±0.41 | 2.18±0.50 | 3.87±1.96 | 9.98±1.93 |  | 10.85±1.99 |  | 20.67±11.26 |
| Coal-based solid waste | CG | 9±3 | 2.04±0.07 | 0±0 | 2±1 | 0.00±0.00 | 0.95±0.67 | 0.00±0.00 | 4.68±2.32 |  | 4.68±2.32 |  | 0.00±0.00 |
|  | CFA | 10±1 | 2.15±0.13 | 0±0 | 2±1 | 0.17±0.41 | 1.51±0.42 | 0.63±1.55 | 7.54±2.02 |  | 7.80±1.47 |  | 7.50±18.37 |
| Industrial by-product gypsum | DG | 10±2 | 1.87±0.18 | 1±0 | 2±1 | 0.80±0.45 | 1.20±0.45 | 4.39±2.83 | 6.54±2.12 |  | 8.19±2.49 |  | 32.31±19.75 |
|  | PG | 12±1 | 2.12±0.10 | 1±0 | 2±1 | 1.00±0.00 | 1.33±0.26 | 4.08±0.45 | 5.43±1.20 |  | 6.81±1.09 |  | 37.46±5.84 |

# Table S29 ERIA of typical IW in downcycling scenario

| Source/Categories |  | n | H (bit) | m | m' | D | D' | R (bit-1) | R' (bit-1) | A (bit-1) |  | θ (°) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tailings | GCT | 2 | 0.93±0.06 | 4 | 6±4 | 0.54±0.17 | 0.26±0.16 | 29.46±10.19 | 14.03±9.36 |  | 33.03±12.59 |  | 66.92±11.49 |
|  | CT | 2 | 0.76±0.17 | 4 | 7±3 | 0.61±0.28 | 0.24±0.07 | 44.54±28.27 | 16.05±4.71 |  | 48.18±26.94 |  | 64.91±14.50 |
|  | IT | 2 | 0.38±0.08 | 4 | 4±1 | 0.93±0.02 | 0.21±0.06 | 127.44±34.80 | 27.84±7.94 |  | 130.66±34.71 |  | 77.35±3.92 |
|  | NFT | 2 | 0.76±0.25 | 4 | 7±5 | 0.70±0.20 | 0.14±0.14 | 54.88±31.77 | 8.42±8.68 |  | 56.65±30.54 |  | 77.45±15.27 |
| Smelting slag | I&S | 2 | 0.69±0.11 | 4 | 1±0 | 0.81±0.06 | 0.23±0.14 | 60.00±11.97 | 17.67±10.70 |  | 63.00±13.70 |  | 74.97±8.81 |
|  | CS | 2 | 0.80±0.23 | 4 | 5±2 | 0.62±0.24 | 0.45±0.22 | 46.28±38.63 | 33.11±27.70 |  | 285.46±47.25 |  | 56.41±8.73 |
|  | NFS | 2 | 0.72±0.15 | 4 | 5±2 | 0.78±0.09 | 0.38±0.10 | 57.13±17.06 | 27.54±9.12 |  | 63.57±18.78 |  | 64.61±4.66 |
| Red mud | RM | 2 | 0.77±0.14 | 4 | 3±1 | 0.77±0.07 | 0.48±0.18 | 52.75±18.00 | 33.19±15.81 |  | 62.90±22.06 |  | 59.09±9.98 |
| Coal-based solid waste | CG | 2 | 0.73±0.19 | 4 | 2±1 | 0.78±0.09 | 0.31±0.06 | 59.54±26.94 | 22.62±7.61 |  | 63.85±27.54 |  | 68.48±4.02 |
|  | CFA | 2 | 0.48±0.20 | 4 | 4±1 | 0.88±0.09 | 0.37±0.05 | 106.76±41.51 | 42.37±12.61 |  | 115.05±42.77 |  | 67.32±4.41 |
| Industrial by-product gypsum | DG | 2 | 0.98±0.02 | 4 | 4±1 | 0.43±0.05 | 0.41±0.22 | 21.95±1.93 | 21.20±11.17 |  | 31.80±5.35 |  | 49.05±21.07 |
|  | PG | 2 | 0.95±0.04 | 4 | 4±1 | 0.41±0.10 | 0.42±0.05 | 21.50±4.47 | 22.21±3.19 |  | 31.25±2.25 |  | 43.86±9.14 |

# Table S30 ERIA of typical IW in landfill scenario

| Source/Categories |  | n | H (bit) | m' | D' | R' (bit-1) | A (bit-1) |  | θ (°) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tailings | GCT | 1 | 0 | 6±4 | 2.37±2.17 | 2.37±2.17 |  | 2.37±2.17 |  | 0 |
|  | CT | 1 | 0 | 6±3 | 2.81±1.33 | 2.81±1.33 |  | 2.81±1.33 |  | 0 |
|  | IT | 1 | 0 | 3±1 | 0.99±0.73 | 0.99±0.73 |  | 0.99±0.73 |  | 0 |
|  | NFT | 1 | 0 | 5±2 | 2.53±0.38 | 2.53±0.38 |  | 2.53±0.38 |  | 0 |
| Smelting slag | I&S | 1 | 0 | 1±0 | 0.00±0.00 | 0.00±0.00 |  | 0.00±0.00 |  | 0 |
|  | CS | 1 | 0 | 5±2 | 2.68±1.25 | 2.68±1.25 |  | 2.68±1.25 |  | 0 |
|  | NFS | 1 | 0 | 5±2 | 2.90±1.02 | 2.90±1.02 |  | 2.90±1.02 |  | 0 |
| Red mud | RM | 1 | 0 | 3±1 | 0.25±0.39 | 0.25±0.39 |  | 0.25±0.39 |  | 0 |
| Coal-based solid waste | CG | 1 | 0 | 2±1 | 0.15±0.34 | 0.15±0.34 |  | 0.15±0.34 |  | 0 |
|  | CFA | 1 | 0 | 2±1 | 0.75±0.00 | 0.75±0.00 |  | 0.75±0.00 |  | 0 |
| Industrial by-product gypsum | DG | 1 | 0 | 2±1 | 0.70±0.11 | 0.70±0.11 |  | 0.70±0.11 |  | 0 |
|  | PG | 1 | 0 | 2±1 | 1.08±0.26 | 1.08±0.26 |  | 1.08±0.26 |  | 0 |

# Fig. S1 Elements analyzed in this study

# Fig. S2 Box-and-whisker plot for recyclability, removability, and ERIA of IW by categories

Note: (a), (b), (c), and (d) recyclability, removability, ERIA (A) and ERIA (θ) of IW in elements recycling scenario, (e), (f), (g), and (h) recyclability, removability, ERIA (A) and ERIA (θ) of IW in compounds recycling scenario, (i), (j), (k), and (l) recyclability, removability, ERIA (A) and ERIA (θ) of IW in downcycling scenario, (m) removability and ERIA (A) of IW in landfill scenario.

# Fig. S3 ERIA assessment for different scenarios: case of gold cyanide tailing

# Fig. S4 Effect of n missing on the stability of environmental-resource interacting attribute evaluation models

# SI References

1.	X. Zeng, J. Li, Measuring the recyclability of e-waste: an innovative method and its implications. Journal of Cleaner Production 131, 156-162 (2016).

2.	W. B. Huang, J. H. Li, X. L. Zeng, Accurately quantifying the detoxication of solid waste and its scientific insights: The case of typical industrial waste. Chinese Science Bulletin-Chinese 67, 685-696 (2022).

3	John R. Rumble, ed., CRC Handbook of Chemistry and Physics, 103rd Edition (Internet Version 2022), CRC Press/Taylor & Francis, Boca Raton, FL.