Supplementary Material

Intrinsic Piezoelectric Anisotropy of Tetragonal ABO3 Perovskites: A High-Throughput Study

Fanhao Jia,1,2 Shaowen Xu,3 Shunbo Hu,4,5,1* Jianguo Chen1, Yongchen Wang,1 Yuan Li, 2 Wei Ren,1* and Jinrong Cheng1*

1School of Materials Science and Engineering; Department of Physics, International Centre of Quantum and Molecular Structures, Shanghai University, Shanghai 200444, China

2Department of Physics, School of Sciences, Hangzhou Dianzi University, Hangzhou 310018, China

3School of Physics and Optoelectronic Engineering, Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, Hangzhou 310024, China

4Institute for the Conservation of Cultural Heritage, School of Cultural Heritage and Information Management, Shanghai University, Shanghai 200444, China

5Key Laboratory of Silicate Cultural Relics Conservation (Shanghai University), Ministry of Education, China

*E-mail: shunbohu@shu.edu.cn; renwei@shu.edu.cn; jrcheng@shu.edu.cn

Figure S1. (a) Schematic of tetragonal ABO3 perovskite, where the arrows in the right panel are spin directions of the antiferromagnetic configuration used in this study.  (b) The born effective charge Z33 of A-site, B-site, O1/O2 and O3 as a function of interatomic displacement amplitude.

Figure S2. Lattice volume as a function of c/a ratio.

Elasticity

In view of P4mm symmetry relations, the 4th-rank elastic stiffness tensor (in Voigt notation) of tetragonal perovskite can be given by:

C=c11c12c13000c12c11c13000c13c13c33000000c44000000c44000000c66,#1

which is consistent by six independent elastic constants, namely c11, c33, c44, c66, c12, and c13. The tension can produce not only normal strains but also shear strains, and it will be convenient to describe the directional elastic properties in the spherical coordinates with basis set [1],

a=sinθcosφsinθsinφcosθ, 0≤θ≤π,0≤φ≤2π#2

b=cosθcosφcosγ-sinφsinγcosθsinφcosγ-cosφsinγ-sinθcosγ,0≤γ≤2π#3

Then, the fourth order elastic compliance tensor S transforms in a new basis set following the rule:

Sαβγδ'=rαirαirαirαiSijkl,#4

where Einstein’s summation rule (i.e., when an index occurs twice in the same term, summation with respect to that index is applied) is adopted and the rαi are the components of the rotation matrix (or direction cosines). Once the S' is determined, the Young’s modulus E(a), linear compressibility β(a) (or multiplicative inverse of bulk modulus B(a) of the normal stress along a can be easily written by

Ea=Eθ,φ=1S11'θ,φ=1aiajakalSijkl,#5

βa=1Ba=aiajakakSijkk=aiajSijkk.#6

Shear modulus G and Poisson’s ratio ν are not as straightforward to represent and depend on two directions (a and b) at the same time, with

Ga,b=Gθ,φ, γ=141aibjakblSijkl,#7

νa,b=νθ,φ, γ=-aiajbkblSijklaiajakalSijkl.#8

Table SI. The calculated elastic constants cij (in GPa) of tetragonal ABO3 systems.

| System | c11 | c33 | c44 | c66 | c12 | c13 |
| --- | --- | --- | --- | --- | --- | --- |
| BaTiO3 | 299 211a | 136 160 | 116 56 | 125 127 | 113 107 | 90 114 |
| KNbO3 | 380 | 163 | 88 | 93 | 83 | 82 |
| PbTiO3 | 252 237b | 55 60 | 56 69 | 100 104 | 105 90 | 76 70 |
| PbVO3 | 231 | 33 | 53 | 43 | 48 | 51 |
| BiCoO3 | 204 | 89 | 23 | 53 | 40 | 38 |

aRef [2]; bRef [3];

Table SⅡ. The calculated elastic moduli (in GPa) along crystal axes of tetragonal ABO3 systems. G and ν are shear modulus and Poisson's ratio represented by Marmier manner. An overall anisotropy index of property X (Young’s modulus E and linear compressibility β) can be defined by AX= max(X(θ, φ, γ))/min(E(θ, φ, γ)).

| System | BaTiO3 | KNbO3 | PbTiO3 | PbVO3 | BiCoO3 |
| --- | --- | --- | --- | --- | --- |
| Ea | 228 | 334 | 145 | 148 | 185 |
| Ec | 97 | 134 | 23 | 15 | 78 |
| Ea/Ec | 2.4 | 2.5 | 6.3 | 9.9 | 2.4 |
| AE | 3.1 | 2.5 | 9.8 | 12.0 | 2.8 |
| βa | 1.1 | 1.3 | 3.3 | 4.2 | 2.9 |
| βc | 6.1 | 4.9 | 28.6 | 42.9 | 9.4 |
| βa/βc | 5.5 | 3.8 | 8.6 | 10.2 | 3.2 |
| Aβ | 5.4 | 3.8 | 8.6 | 10.2 | 3.2 |
| Gamax | 126 | 94 | 100 | 53 | 53 |
| Gamin | 116 | 88 | 56 | 43 | 23 |
| Gcmax | 116 | 88 | 56 | 53 | 23 |
| Gcmin | 116 | 88 | 56 | 53 | 23 |
| νamax | 0.52 | 0.44 | 1.42 | 1.81 | 0.37 |
| νamin | 0.22 | 0.12 | -0.01 | -0.19 | 0.13 |
| νcmax | 0.22 | 0.18 | 0.21 | 0.19 | 0.15 |
| vcmin | 0.22 | 0.18 | 0.21 | 0.19 | 0.15 |

Piezoelectricity

“Piezoelectric stress constant” is written as:

eαj=∂Pα∂ηjε=∂σj∂εαη.#9

“Piezoelectric strain constant” is written as:

dαj=∂Pα∂σjε=∂ηj∂εασ.#10

They can be converted by the thermodynamic relations:

dαj=Sjkeαk,#11

eαj=Cjkdαk.#12

Figure S3. Piezoelectric constant d33 as a function of polarization.

Figure S4. Piezoelectric constants e33 and e31 as a function of c/a ratio.

Figure S5. |e33/e31| ratio as a function of c/a ratio.

Table SⅢ. The calculated piezoelectricity (eαj in C/m2, dαj in pC/N,) of tetragonal ABO3 systems.

| System | Phase | e33 | e31 | ¦e33/e31¦ | d33 | d31 | ¦d33/d31¦ |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BaTiO3 | P4mm | 4.85 5.48a | 0.57 -3.88a | 8.5 1.4 | 49.0 | -9.2 | 5.3 |
| KNbO3 | P4mm | 5.20 | -0.31 | 16.5 | 40.1 | -7.7 | 5.2 |
| PbTiO3 | P4mm | 4.86 5.0b | 1.57 2.1 | 3.1 2.5 | 209.0 | -40.3 | 5.2 |
| PbVO3 | P4mm | 1.36 | 2.29 | 1.7 | 120.9 | -17.1 | 7.1 |
| BiCoO3 | P4mm | 2.97 | 2.88 | 1.0 | 26.7 | 8.7 | 3.1 |

aRef [2]; bRef [3]

REFERENCE

[1]	A. Marmier, Z. A. D. Lethbridge, R. I. Walton, C. W. Smith, S. C. Parker, and K. E. Evans, Computer Physics Communications 181, 2102 (2010).

[2]	Z. Li, S. K. Chan, M. Grimsditch, and E. Zouboulis, Journal of Applied Physics 70, 7327 (1991).

[3]	A. Kalinichev, J. Bass, B. Sun, and D. Payne, Journal of materials research 12, 2623 (1997).