Supplementary information

Supplementary Figure 1

Sup.Fig.1 Compositional analysis of the edge-dislocation, SF and LCD in 0.19N.

Cr content was measured to be ~25 at%, ~35 at%, ~35 at% and ~60 at% in the matrix, edge-dislocation, SF and LCD, respectively.

Supplementary Figure 2

Sup.Fig.2 Mass spectrum obtained from 0.19N deformed up to 20% strain, where N atoms are detected as CrN molecules due to their attractive chemical interactions with Cr atoms.

Supplementary Table 1

Sup.Table 1 Compositions of segregated impurities around the defect by APT.

| No. | Mn | Ni | Fe | Cr | Si | V | N | C |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.12 -3.35 | 8.67 -13.5 | 41.3 -51.3 | 27.4 -41.9 | 0.559 -4.94 | 0.230 -1.12 | 0.758 -2.23 | 0.0777 -0.201 |
| 2 | 0.224 -1.60 | 6.12 -12.2 | 40.8 -52.5 | 26.9 -44.9 | 1.79 -5.69 | 0.218 -0.728 | 0.604 -2.98 | 0.0330 -0.881 |
| 3 | 0.777 -3.79 | 8.55 -13.1 | 41.7 -51.5 | 28.5 -40.2 | 0.758 -4.99 | 0.247 -0.838 | 0.614 -1.30 | 0.0617 -0.240 |
| 4 | 0.667 -1.55 | 7.33 -13.1 | 40.8 -51.3 | 28.2 -42.7 | 1.33 -5.17 | 0.178 -.267 | 0.215 -1.44 | 0.0669 -1.33 |
| 5 | 0.962 -1.42 | 8.40 12.7 | 40.4 -51.2 | 28.6 -42.4 | 3.92 -6.40 | 0.227 -1.26 | 0.646 -1.18 | 0.0568 -0.444 |
| 6 | 0.850 -1.72 | 12.2 -14.7 | 44.7 -53.0 | 27.1 -32.4 | 4.08 -5.77 | 0.262 -0.668 | 0.459 -1.63 | 0.0656 -0.227 |
| Matrix (-4.9 nm~ -1.5 nm) | 1.20 ±0.06 | 14.1 ±0.25 | 55.1 ±0.43 | 23.7 ±0.26 | 5.12 ±0.15 | 0.114 ±0.02 | 0.394 ±0.10 | 0.0466 ±0.03 |