Supporting Information

ORIGINAL RESEARCH

Electrodeposition of polyaniline on reduced graphene oxide/cotton yarn with tunable electrochemical performance for flexible textile supercapacitors

Lin Li · Dou Du · Chengen He · Kun Han · Weilin Xu · Liangjun Xia · Guangming Cai · Xun Cui · Yihuang Chen · Lianqing Yu · Lingxue Kong

L. Li · C. He ()· K. Han · W. Xu · L. Xia · G. Cai · X. Cui · L. Yu ()

State Key Laboratory of New Textile Materials and Advanced Processing Technologies, Wuhan Textile University, Wuhan 430200, China.

e-mail：cehe@wtu.edu.cn

L. Yu

e-mail：yulq@wtu.edu.cn

D. Du

National Center for Computational Design and Discovery of Novel Materials (MARVEL), École Polytechnique Fédérale de Lausanne, CH-1015, Lausanne, Switzerland.

Y. Chen

College of Chemistry and Materials Engineering, Wenzhou University, Wenzhou, Zhejiang 325035, China.

L. Li · L. Kong ()

Institute for Frontier Materials, Deakin University, Geelong, Victoria 3216, Australia.

e-mail：lingxue.kong@deakin.edu.au

Fig. S1 The capacitive contribution for PRC15-50% electrode. (a) Calculated proportion of the surface-controlled process and diffusion-controlled process at various scan rate. (b-d) The capacitive contribution to charge storage at 5 mV s−1 to 100 mV s−1

Fig. S2 CV curves of RC (a), PRC15-30% (b), and PRC15-70% (c) at various scan rates

Fig. S3 GCD shapes of RC (a), PRC15-30% (b), and PRC15-70% (c) at various current densities

Fig. S4 CV curves of PRC9-50% (a), PRC12-50% (b), and PRC18-50% (c) at various scan rates

Fig. S5 GCD shapes of PRC9-50% (a), PRC12-50% (b), and PRC18-50% (c) at various current densities

Fig. S6 (a) CV and (b) GCD curves of RC supercapacitor

Fig. S7 Length capacitances from the CV measurement for PRC15-50% and RC supercapacitor

Fig. S8 Areal and Volumetric energy density and power density of the PRC15-50% yarn supercapacitor

Table. S1 An experimental design for the synthesis design of RC composites

| Samples | Current sweep cycle | ANI content | PANI content (mg) |
| --- | --- | --- | --- |
| PRC15-30% | 15 | 30% | 1.1 |
| PRC15-50% | 15 | 50% | 2.3 |
| PRC15-70% | 15 | 70% | 1.4 |
| PRC 9 -50% | 9 | 50% | 1.0 |
| PRC12-50% | 12 | 50% | 1.2 |
| PRC15-50% | 15 | 50% | 2.3 |
| PRC18-50% | 18 | 50% | 2.9 |

Table. S2 Summary of different textile Fiber based electrode for use in wearable supercapacitor

| Conductive Materials | Fiber | Capacitence (mF cm−2) | Energy Density (µWh cm−2) | Power Density (µW cm−2) | Ref. |
| --- | --- | --- | --- | --- | --- |
| PPy | Cotton | 74.0 at 0.42 mA cm−2 | 7.5 | 22.4 | (Wei et al., 2017) |
| Ni/RGO | Polyester | 24.4 at 1 V s−1 | 1.60 | 2420 | (Pu et al., 2016) |
| ZnO/Gold | Plastic /Kevlar | 2.4 at 100 mV s−1 | 0.027 | 14 | (Bae et al., 2011) |
| NiCo2S4/NiCoLDH/Au | Cotton | 37.2 at 0.4 mA cm−2 | 3.6 | 163.2 | (Wang et al., 2019) |
| Ni/RGO | Cotton | 5.34 at 10 mV s−1 | 0.30 | 2 | (Huang et al., 2020) |
| MXene | Polyester | 13.23 at 0.25 mA cm−2 | 0.38−0.67 | 90−390 | (Shao et al., 2018) |
| NiCo−OH /ZnO-NR | CNT | ~ | 0.897−1.38 | 117−647 | (Le et al., 2020) |
| PANI/RGO | Cotton | 62.90−35.01 at 0.25−1.91 mA cm−2 | 8.74 | 127 | This work |

- Reference

Bae J, Song MK, Park YJ, Kim JM, Liu M, Wang ZL (2011) Fiber supercapacitors made of nanowire-fiber hybrid structures for wearable/flexible energy storage. Angew Chem Int Ed 50: 1683-1687. https://doi.org/10.1002/anie.201006062.

Huang Q, Wang D, Hu H, Shang J, Chang J, Xie C, Yang Y, Lepró X, Baughman RH, Zheng Z (2020) Additive functionalization and embroidery for manufacturing wearable and washable textile supercapacitors. Adv Funct Mater 30: 1910541. https://doi.org/10.1002/adfm.201910541.

Le TS, Truong TK, Huynh VN, Bae J, Suh D (2020) Synergetic design of enlarged surface area and pseudo-capacitance for fiber-shaped supercapacitor yarn. Nano Energy 67: 104198. https://doi.org/10.1016/j.nanoen.2019.104198.

Pu X, Li L, Liu M, Jiang C, Du C, Zhao Z, Hu W, Wang ZL (2016) Wearable Self-Charging Power Textile Based on Flexible Yarn Supercapacitors and Fabric Nanogenerators. Adv Mater 28: 98-105. https://doi.org/10.1002/adma.201504403.

Shao W, Tebyetekerwa M, Marriam I, Li W, Wu Y, Peng S, Ramakrishna S, Yang S, Zhu M (2018) Polyester@MXene nanofibers-based yarn electrodes. J Power Sources 396: 683-690. https://doi.org/10.1016/j.jpowsour.2018.06.084.

Wang YF, Wang HT, Yang SY, Yue Y, Bian SW (2019) Hierarchical NiCo2S4@Nickel-Cobalt Layered Double Hydroxide nanotube arrays on metallic cotton yarns for flexible supercapacitors. ACS Appl Mater Interfaces 11: 30384-30390. https://doi.org/10.1021/acsami.9b06317.

Wei C, Xu Q, Chen Z, Rao W, Fan L, Yuan Y, Bai Z, Xu J (2017) An all-solid-state yarn supercapacitor using cotton yarn electrodes coated with polypyrrole nanotubes. Carbohydr Polym 169: 50-57. https://doi.org/10.1016/j.carbpol.2017.04.002.