Supporting Information

Origins of polysaccharide conformation and viscoelasticity in miscible heterogenous solvent

Pallab Kumar Boraha, Amir H. Iranib,c, Joshua E. S. J. Reida, Thomas MacCalmand, Benjamin Westberrye, Vlad Dinud, Philippe Prochassonf, Michael W. Boehmf, Stephen E. Hardingd, Reed A. Nicholsonf, Martin A. K. Williamse, Stefan K. Baierf,g, Gleb E. Yakubova*

a Food and Biomaterials Group, School of Biosciences, University of Nottingham, LE12 5RD, United Kingdom

b Department of Anaesthesia, Te Whatu Ora, Waikato Hospital, Hamilton 3204, New Zealand

c School of Engineering, University of Waikato, Hamilton 3240, New Zealand

d National Centre for Macromolecular Hydrodynamics, School of Biosciences, University of Nottingham, LE12 5RD, United Kingdom

e School of Fundamental Sciences, Massey University, Palmerston North 4442, New Zealand

f Motif FoodWorks Inc, 27 Drydock Avenue, Boston, MA 02210, United States of America.

g School of Chemical Engineering, The University of Queensland, Brisbane, QLD 4072, Australia.

*Corresponding author:

Gleb E. Yakubov, Associate Professor of Food Physics, Division of Food, Nutrition and Dietetics, School of Biosciences, University of Nottingham, LE12 5RD, United Kingdom.

S1. Characterisation of weight average molar mass

Weight average molar mass (Mw) was estimated by Size Exclusion Chromatography coupled to Multiangle Laser Light Scattering system (Wyatt Technology, USA), as described elsewhere.1 Briefly, samples (1 mg mL-1) were filtered through a 5 µm Whatman syringe filter and injected using a Spark-Holland Marathon Basic autosampler. A phosphate buffer (0.1M, pH 7) at a flow rate of 0.5 mL min-1 was maintained on a Shodex LB-805 column, equipped with a Shodex LB-G6B guard column coupled on-line to Dawn Heleos-II MALS, a ViscoStar-II differential pressure viscometer and Optilab rEX refractive index detector (Wyatt Technology, USA). Mw was calculated by using a linear fit to the Zimm model as, KcRθ=1Mw+2Bc1+16π2Rg23λ2sin2θ2, where K is a wavelength-dependant experimental constant, dndc pectin ≈0.146, B is the second virial coefficient, Rθ is the Rayleigh ratio, and Rg is the radius of gyration. Thermodynamic nonideality correction was ignored reasonably due to the high dilutions on the SEC columns based on reasons described previously.2

Elution profiles revealed multimodal molar mass distributions that correspond to different pectin Mw species (Figure S5a). Partially overlapping peaks were observed and therefore the profile was subjected to baseline correction and Gaussian peak fitting using the Levenberg–Marquardt algorithm until convergence to uncover the relative abundance of Mw (Figure S5b). The MW ranges from 4.3 × 106 - 2.0 × 107 g mol-1 (Table S3). We uncovered that ca. 70% of the total pectin was 1.1 × 107 g mol-1, and in close agreement with previous literature.3 As described earlier,4 we estimated lp and ML using the Yamakawa-Fujii and the Bushin–Bohdanecky equations based on the minimisation of a target function, Δ which takes into account intrinsic viscosity, [η] over the entire molecular weight distribution.

S2. Characterisation of monosaccharide composition

The monosaccharide composition was determined from acid digestion of the okra pectin and subsequent quantification of the product monosaccharides. The okra pectin was dispersed in ultrapure water at a concentration of 10 mg mL-1 and hydrolysed according to two different methods: 1) 1:1 mixture with 4M trifluoroacetic acid, 120°C, 60 minutes (for neutral sugars quantification) and 2) 1:1 mixture with concentrated sulfuric acid, 105°C, 20 minutes (for galacturonic acid quantification). Afterwards, samples were removed from the heating block and an aliquot of the hydrolysis solution (20 μL) was diluted in 10 mM NaOH buffer for subsequent monosaccharide analysis.

The neutral sugars analysis is performed on to a High-Performance Anion Exchange Chromatography with Pulsed Amperometric Detection (Dionex, UK). The instrument used is a Dionex ICS 6000 equipped with a CarboPac PA210 column (250mm x 4mm) and CarboPac PA210 guard (50mm x 4mm) equilibrated at 30°C. The mobile phase was composed of four eluents at varying ratios and were all prepared using ultrapure water obtained using a Suez Select Fusion ultrapure water deionisation unit which had been degassed under vacuum using a sonicating water bath for at least 30 minutes. The four eluents were 1) 100% H2O, 2) 100 mM sodium hydroxide (NaOH), 3) 200 mM NaOH and 4) 100 mM NaOH + 500 mM sodium acetate (NaOAc). For all injections, a sample loop volume of 25 μL was used on a push-full method.

For each sample, two injections were made using two different buffer combinations; the first intended to resolve all neutral monosaccharides (excluding arabinose and rhamnose) and galacturonic acid (method 1), the second to resolve arabinose and rhamnose (method 2). The buffer conditions for each of these methods are summarised in the table below.

Table S1.1. Mobile phase gradient method for monosaccharide separation (excluding arabinose and rhamnose).

| Time / min | Flow rate / mL min-1 | % Eluent 1 | % Eluent 2 | % Eluent 3 | % Eluent 4 |
| --- | --- | --- | --- | --- | --- |
|  |  | (H2O) | (100 mM NaOH) | (200 mM NaOH) | (100 mM NaOH + 500 mM NaOAc) |
| -10.0 | 0.2 | 99 | 1 | 0 | 0 |
| 0.0* | 0.2 | 99 | 1 | 0 | 0 |
| 10.0 | 0.2 | 90 | 10 | 0 | 0 |
| 15.0 | 0.2 | 90 | 10 | 0 | 0 |
| 22.5 | 0.2 | 0 | 0 | 0 | 50 |
| 27.5 | 0.2 | 0 | 0 | 0 | 50 |
| 32.5 | 0.2 | 0 | 0 | 100 | 0 |
| 36.0 | 0.2 | 0 | 0 | 100 | 0 |

Table S1.2. Mobile phase gradient method for separation of arabinose and rhamnose.

| Time / min | Flow rate / mL min-1 | % Eluent 1 | % Eluent 2 | % Eluent 3 | % Eluent 4 |
| --- | --- | --- | --- | --- | --- |
|  |  | (H2O) | (100 mM NaOH) | (200 mM NaOH) | (100 mM NaOH + 500 mM NaOAc) |
| -10.0 | 0.2 | 75 | 25 | 0 | 0 |
| 0.0* | 0.2 | 75 | 25 | 0 | 0 |
| 10.0 | 0.2 | 90 | 10 | 0 | 0 |
| 15.0 | 0.2 | 90 | 10 | 0 | 0 |
| 15.1 | 0.2 | 0 | 0 | 100 | 0 |
| 20.0 | 0.2 | 0 | 0 | 100 | 0 |

For calibration, a standard solution containing each of the following monosaccharides was prepared to a concentration of 100 mg L-1 in ultrapure water: arabinose, rhamnose, galactose, glucose, xylose, mannose, fructose, galacturonic acid. The solution was then diluted to a monosaccharide concentration of 1 mg L-1 in 10 mM NaOH buffer and then subsequently serial diluted to a final monosaccharide concentration of 0.0625 mg L-1. A linear correlation of monosaccharide peak area and concentration was obtained, with the fitting parameters used for quantitation of monosaccharides from the hydrolysis of the okra polysaccharide. A summary of the fitting parameters and statistics of the linear fitting can be found in the Table S1.3. Monosaccharide composition of polysaccharide is reported in Table S1.4.

Table S1.3: Fitting parameters and their statistical significance from the least squares method for the linear calibration plot of peak area (y-axis) to sugar concentration in the analysed samples (x-axis) in the form y = mx + b. Method 1 = §, method 2 = *. Values reported to four significant figures (two decimal places reported).

|  | Rha | Ara | Gal | Glu | Xyl | Man | Fru | GalA |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Retention time | 3.13* | 3.45* | 5.52§ | 6.16§ | 7.14§ | 7.39§ | 8.88* | 24.07§ |
| Value (m) | 4.37 | 7.69 | 4.022 | 5.30 | 4.15 | 3.35 | 0.78 | 2.42 |
| Value (b) | 0.14 | 0.11 | 0.15 | 0.30 | 0.26 | 0.07 | 0.01 | 0.05 |
| R2 | 0.99 | 0.99 | 0.99 | 0.99 | 0.99 | 0.99 | 0.99 | 0.99 |
| LOD | 0.085 | 0.06 | 0.15 | 0.17 | 0.19 | 0.08 | 0.05 | 0.04 |
| LOQ | 0.25 | 0.19 | 0.46 | 0.54 | 0.60 | 0.26 | 0.16 | 0.14 |

GalA, galacturonic acid; Rha, rhamnose; Ara, arabinose; Gal, galactose; Glu, glucose; Xyl, xylose; Man, mannose; Fru, Fructose

Table S1.4. Monosaccharide composition of polysaccharide.

| Okra pectin yield | GalA | Rha | Ara | Gal | Glu | Xyl | Man | Fru | Total pectic sugars | Total RG-I region | HGA/RG-I |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| g/g% | % | % | % | % | % | % | % | % | % | % | % Ratio |
| 2.85 ± 1.0 | 24.7 | 10.5 | 1.7 | 7.9 | 9.1. | 0.4 | 0.3 | ND | 46% | 20% | 1.23 |

GalA, galacturonic acid; Rha, rhamnose; Ara, arabinose; Gal, galactose; Glu, glucose; Xyl,  xylose; Total pectic sugars = GalA + Rha + Ara + Gal + Glu + Xyl; Total RG-I region = Rha + Ara + Gal; HGA/RG-I = GalA/(Rha + Ara + Gal), which represents the ratio of pectin HGA region to pectin RG-I region; ND, not detected.

Table S2. Account of water and glycerol used in the simulations.

| Simulation | Water | Glycerol | Solution density (Experimental) | Solution density (Simulation) |
| --- | --- | --- | --- | --- |
|  | number of molecules | number of molecules | kg m-3 | kg m-3 |
| ϕ0 | 3985 | 0 | 996.48 ± 0.23 | 988.66 |
| ϕ20 | 3293 | 128 | 1051.23 ± 0.13 | 1018.48 |
| ϕ40 | 2658 | 255 | 1104.86 ± 0.18 | 1049.73 |
| ϕ60 | 2074 | 383 | 1158.65 ± 0.23 | 1074.54 |
| ϕ80 | 1571 | 511 | 1207.86 ± 0.21 | 1104.88 |

ϕ0, okra pectin + water; ϕ20, okra pectin + 20% aqueous glycerol; ϕ40, okra pectin + 40% aqueous glycerol; ϕ60, okra pectin + 60% aqueous glycerol; ϕ80, okra pectin + 80% aqueous glycerol. Experimental densities are measured in ϕ0→80, c, 0.01 wt.%. For the simulations, the triclinic box volume was 124.18 nm3 and polysaccharide chain volume was 4.65 nm3. At ϕ100, the box contained 639 glycerol molecules. Glycerol molecules were randomly placed inside the box and then filled with water. Note that glycerol molecules were not inserted in areas where the distance between any existing atom and any atom of the inserted molecule was less than the sum of their van der Waals radii. Note, 0.58 van der Waals scaling applies, providing ca. 1000 kg m-3 for protein in water.

Table S3. The weight average molar masses and molar mass distribution of okra pectin in water.

| Peak Assignment | Molar mass | Relative abundance |
| --- | --- | --- |
|  | g∙mol-1 | Peak height integration |
| 1 | 2.006 × 107 | 15.09 % |
| 2 | 1.151 × 107 | 67.40 % |
| 3 | 3.393 × 106 | 2.86 % |
| 4 | 4.301 × 106 | 14.63 % |

Peak assignments and peak height integration correspond to Figure S5a, b.

Table S4.  Partial charges of methyl esterified galacturonic acid at C6 position and rhamnose sugars utilised in the simulations.

|  | Partial charges |  |
| --- | --- | --- |
| Atom | methyl esterified galacturonic acid | rhamnose |
| C1 | 0.3329 | 0.2759 |
| C2 | 0.1241 | 0.4278 |
| C3 | 0.0801 | 0.1091 |
| C4 | 0.1021 | 0.0811 |
| C5 | 0.1221 | 0.1101 |
| C6 | 0.6021 | -0.0981 |
| C7 | 0.1237 | _ |
| O2 | -0.5818 | -0.3875 |
| O3 | -0.6038 | -0.5728 |
| O4 | -0.4376 | -0.5998 |
| O5 | -0.4256 | -0.4216 |
| 06a | -0.5330 | _ |
| 06b | -0.4329 | _ |
| H1 | 0.1237 | _ |
| H2 | 0.4220 | 0.0567 |
| H3 | 0.4150 | 0.0877 |
| H4 | 0.0887 | 0.0667 |
| H5 | 0.1217 | 0.0717 |
| H61 | _ | 0.0523 |
| H62 | _ | 0.0523 |
| H63 | _ | 0.0523 |
| H71 | 0.0540 | _ |
| H72 | 0.0540 | _ |
| H73 | 0.0540 | _ |
| HO2 | 0.0897 | _ |
| H03 | 0.0937 | 0.4240 |
| HO4 | _ | 0.4150 |

Galacturonic acid is methyl esterified at C6 position.

Figure S1. Root-mean squared distance (RMSD) of the pectin chains as a function of time (a). Radius of gyration,  Rg, of the pectin chains as a function of time (b). Polysaccharide solutions are indicated as ϕ0, black; ϕ20, red; ϕ40, green; ϕ60, blue; and ϕ80, orange.

Figure S2. Shear viscosity (η) as a function of shear rate (.γ) in okra pectin solutions, ϕ0, (a); ϕ20, (b); ϕ40, (c); ϕ60, (d); and ϕ80, (e) at 25 ◦C. Legends indicate okra pectin concentrations in wt.%.

Figure S3. Shear stress (τ) as a function of shear rate (.γ) in okra pectin solutions, ϕ0, (a); ϕ20, (b); ϕ40, (c); ϕ60, (d); and ϕ80, (e) at 25 ◦C. Legends indicate okra pectin concentrations in wt.%.

Figure S4. Shear viscosity, η of 0.5 wt.% okra pectin solutions, ϕ0→80 as a function of shear rate, .γ at 25 ◦C. Legends indicate okra pectin solutions ϕ0, ◼; ϕ20, ●; ϕ40, ▲; ϕ60, ▼; and ϕ80, ♦. Red dashed lines show Power law model fits. Inset show FENE coefficient as a function of ϕ0→80 (a). Evaluation of the intrinsic viscosity [η] of okra pectin solutions ϕ0, ◼; ϕ20, ●; ϕ40, ▲; ϕ60, ▼; and ϕ80, ♦ at 25 ◦C (n = 10) as a function of polysaccharide concentration, c. Blue dashed lines represent the solutions to ηred approximation for extremely dilute polysaccharide solutions where inter-chain aggregations are absent because of Coulombic repulsions as, ηspc=1+η∙c∙1+k∙cCa+c-1c.5 Red dashed lines represent the Huggins fitting extrapolated to infinite dilutions to eliminate non-ideality effects, where Huggin’s constant were 0.29, 0.49, 0.44, 0.34, and 0.37, respectively, for ϕ0→80 (b). Intrinsic viscosity as a function of polysaccharide concentration, c showing Huggin’s fitting, ηred=η1+kH∙η∙c, Kraemer fitting, ηinh=η1-kK∙η∙c, and Solomon-Ciuta fitting, η≅1c∙2ηsp-2lnηrel12 extrapolated to infinite dilutions to eliminate non-ideality effects. Huggins is indicated with ■, Kraemer is indicated with ●, and Solomon-Ciuta is indicated with ▲ with colour indications ϕ0, black; ϕ20, red; ϕ40, green; ϕ60, blue; and ϕ80, orange (c).

Figure S5. SEC-MALS elution profiles for the okra polysaccharide in water, ϕ0 showing relative scale and weight average molar masses (Mw) (a). Gaussian peak fitting on baseline-corrected elution profiles showing the relative abundance of Mw, detailed in Table S3 (b).

Figure S6. Capillary breakup extensional rheology of okra pectin solutions represented by decay of the normalised filament diameter (dd0) as a function filament duration in ϕ0 (a), ϕ20 (b), ϕ0 (c), ϕ60 (d), and ϕ80 (e). Legends indicate okra pectin concentrations in wt.%.

Figure S7. Surface tension (σ) analysed from the shape profile of a pendant drop formed at the tip of a capillary in air as a function of time in ϕ0 (a), ϕ20 (b), ϕ40 (c), ϕ60 (d), and ϕ80 (e). Legends indicate okra pectin concentrations in wt.%. Inset shows a pendant drop formed at the tip of a capillary in air (a). Solution density (ρ) as a function of okra pectin concentration, c in ϕ0, ◼; ϕ20, ●; ϕ40, ▲; ϕ60, ▼; and ϕ80, ♦. Okra pectin concentration ranges were ϕ0, 0.2 – 0.8 wt.%; ϕ20, 0.06 – 0.4 wt.%; ϕ40, 0.04 – 0.2 wt.%; ϕ60, 0.08 – 0.2 wt.%; and ϕ80, 0.02 – 0.08 wt.%. (f).

Figure S8. Comparison of average end-to-end distance, R of polysaccharide chain in ϕ0→80, using AMBER (■) and CHARMM22 (■) forcefield for glycerol.

References

1	Chun, T. et al. Hydrodynamic Compatibility of Hyaluronic Acid and Tamarind Seed Polysaccharide as Ocular Mucin Supplements. Polymers 12, doi:10.3390/polym12102272 (2020).

2	Almutairi, F. M. et al. Hydrodynamic characterisation of chitosan and its interaction with two polyanions: DNA and xanthan. Carbohydrate Polymers 122, 359-366, doi:10.1016/j.carbpol.2014.09.090 (2015).

3	Kpodo, F. M. et al. Pectin isolation and characterization from six okra genotypes. Food Hydrocolloids 72, 323-330, doi:10.1016/j.foodhyd.2017.06.014 (2017).

4	Morris, G. A., Adams, G. G. & Harding, S. E. On hydrodynamic methods for the analysis of the sizes and shapes of polysaccharides in dilute solution: A short review. Food Hydrocolloids 42, 318-334, doi:10.1016/j.foodhyd.2014.04.014 (2014).

5	Yang, H., Zheng, Q. & Cheng, R. New insight into “polyelectrolyte effect”. Colloids and Surfaces A: Physicochemical and Engineering Aspects 407, 1-8, doi:10.1016/j.colsurfa.2012.05.031 (2012).