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Figure S1 XRD patterns of xRu-SBA15.
Figure S2 XRD pattern (A) and H2-TPR profile (B) of 3Ru-SBA-15-imp.
Figure S3 TEM image of 3Ru-SBA-15 used after six batches.
Table S1 Conversions and apparent activation energies of EL hydrogenation on 3Ru-SBA-15 catalysts prepared by deposition-precipitation and impregnation methods. 
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Figure S2 XRD pattern (A) and H2-TPR profile (B) of 3Ru-SBA-15-imp. 
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Figure S3 TEM image of 3Ru-SBA-15 used after six batches. 















Table S1 Conversions and apparent activation energies of EL hydrogenation on 3Ru-SBA-15 catalysts prepared with different methods. 
	Catalysts
	Temp. (oC)
	Time (min)
	Conv. (%)
	Ea (kJ/mol)

	3Ru-SBA15
	24
	20
	24
	20

	
	34
	20
	33
	

	
	50
	10
	23
	

	3Ru-SBA15-imp
	25
	90
	10
	68

	
	35
	40
	14
	

	
	51
	30
	20
	


[bookmark: OLE_LINK23][bookmark: OLE_LINK24][bookmark: OLE_LINK26]Reaction conditions: 10 mL of 0.25 mol/L EL aqueous solution; 0.5 MPa H2 pressure; 20 mg catalyst (3 wt.% Ru); 1000 rpm.
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